## Slide 1: Cornell Theory
P. N. Koufalis
Cornell University

## Slide 2
Part I: Collective Weak Pinning of Trapped Magnetic Flux
D. Liarte
J. P. Sethna
Part II: Gurevich Theory of AQS & Discussion of QP Overheating
J. T. Maniscalco
T. Arias
N. Sitaraman

## Slide 3
Part I: Collective Weak Pinning of Trapped Magnetic Flux
D. Liarte
J. P. Sethna
Part II: Gurevich Theory of AQS & Discussion of QP Overheating
J. T. Maniscalco
T. Arias
N. Sitaraman

## Slide 4
Relation between power dissipation in superconductor with surface resistance:
Here we consider only the component of the residual resistance due to trapped magnetic flux,
Collective Weak Pinning
depth into superconductor
simple geometry simplifies theoretical analysis
Previous theories do not account for this linear dependence

## Slide 5
Vortex lines are subject to the collective action of many impurities (point defects); only fluctuations in the density of impurities or individual pinning forces can pin vortices
When the vortex trades elastic energy to deform to a new stationary configuration
Bardeen-Stephen equation of motion describes the dynamical properties of vortex lines:
Bardeen-Stephen model can describe the linear dependence of the sensitivity to trapped flux on applied field
Bardeen-Stephen Model
pinning
elastic
Lorentz
viscous
vortex line
impurities (point defects)
Notes: At the critical length, the vortex can trade elastic energy to derfom to find a new stationary configuration
Lower case f is force per unit length
F_pin = accumulated pinning force over the depinning length L_c
F_i = individual pinning force

## Slide 6
Two regimes of losses exist: hysteretic losses (low fields) and viscous losses (high fields)
Crossover between two regimes occurs at
We can derive material dependent approximate analytical solutions for and .
Hysteretic and Viscous Losses
Hysteretic losses:
dominates
Viscous losses:
dominates
Notes: Crossover field is a function of depinning current and inverse frequency

## Slide 7
This solution uses a mean-field approach to solve for the pinning force: (hysteretic regime)
The sensitivity slope, and crossover field, , are proportional to:
Where is the rf frequency, is the GL parameter, is the critical magnetic field, is the de-pinning current, and is the normal state electrical resistivity
Mean Field Approach
Notes: y> is the displacement far into the bulk (the stationary portion of the vortex line) and y< is the displacement close to the surface (i.e. the moving portion of the vortex line) and z* is the point at which the vortex line is ‘unzipped’
vortex oscillates slowly so that we can ignore the viscous term
Assumptions: vortex oscillates slowly so that we can ignore the viscous term and point force approximation (replace exponential decay of Lorentz force with delta function); the latter approximation is valid when the vortex oscillates over larger distances than the penetration depth

## Slide 8
Local Disordered Potential Approach
Numerical simulation that adds the randomness of the impurities back in; used to corroborate the results of the mean field approach
The vortex line is discretized and a random local disordered potential is used to solve the equation of motion
Nb3Sn (1.3 GHz)
NbCu (100 MHz)
Mean field approach
Local Disordered Potential
Data
Nb3Sn (1.3 GHdfdfdfdfd
CO-Infusion
(1.3 GHz)
Notes: Discrepancy can be due to vortex misalignment near the equator.

## Slide 9
Part I: Collective Weak Pinning of Trapped Magnetic Flux
D. Liarte
J. P. Sethna
Part II: Gurevich Theory of AQS & Discussion of QP Overheating
J. T. Maniscalco
T. Arias
N. Sitaraman

## Slide 10
In the dirty limit ( nm) and the right temperature and frequency regime, surface currents modify the electron density of states, ‘smearing’ the normally sharp peak at the Fermi level in such a way that the overall surface resistance decreases as the field increases (‘Q-rise’)
Thermal effects are important:
    Surface resistance is highly dependent on temperature  and power dissipated in the RF surface causes an increase in temperature of the quasiparticles (normal conducting electrons) over the phonon background temperature
    The extent of the quasiparticle overheating is characterized by the overheating parameter which is highly material dependent
    Lower  better energy transfer from quasiparticles to phonons  less overheating  stronger ‘Q-rise’
A. Gurevich. Reduction of Dissipative Nonlinear Conductivity of Superconductors by Static and Microwave Magnetic Fields. Phys. Rev. Lett. 113(087001), 2014.
J. T. Maniscalco, D. Gonnella, M. Liepe. The Importance of the Electron Mean Free Path for Superconducting Radio-Frequency Cavities. J. Appl. Phys. 121(043910), 2017.
Gurevich Theory: Overview

## Slide 11
Mean Free Path Dependence
Example of Experimental Data with Theoretical Fit
Experimentally, it is observed that a shorter mean free path  stronger ‘Q-rise’
High-temperature nitrogen-doped cavity data at with different mean free path values; theory works agrees with data better when is small
Conclusion: impurities reduce mean free path and transfer energy from electrons to phonons

## Slide 12
Overheating parameter was fit for many high-temperature nitrogen-doped cavities:
Linear correlations between and ; low temperature infusion results are consistent with the linear behavior found in high temperature nitrogen doped cavity data
Theory vs. Experiment
J. T. Maniscalco, D. Gonnella, M. Liepe. J. Appl. Phys. 121(043910), 2017.
stronger doping
less overheating
Stronger Q-rise

## Slide 13
DFT Calculations
DFT calculations by T. Arias and N. Sitaraman show that 2 at. % of C present in Nb, increases the electron-phonon coupling by a factor of 4; N and O increase the coupling even more
Impurities increase e-ph coupling  increases energy transfer  reduces overheating  stronger ‘Q-rise’
The strength of the electron-phonon coupling varies with species:
Chart: Impurity Species
Clean Nb | 24
C | 97
N | 165
O | 279
Nb
N
O
C
2 at. %

## Slide 14
Frequency Dependence
The Gurevich theory works well at 1.3 GHz. However, at 2.6 GHz, there is an even stronger reduction of
This cannot, at the moment, be as accurately modeled by the theory as well as the 1.3 GHz data
Work at Fermilab shows that at 3.9 GHz an even stronger reduction of is present
See also: M. Martinello et al, “Advancement in the understanding of the field and frequency dependent microwave surface resistance of niobium,” in Proceedings of SRF2017, Lanzhou, China, 2017.

## Slide 15
THANK YOU FOR LISTENING
Please refer all questions to the appropriate people