## Slide 1: Sample Analysis: Understanding the RF performance of SRF cavities
TTC Meeting 2018
26-29 June 2018
RIKEN Nishina Center
Pashupati Dhakal,
G. Ciovati (JLAB)
S. Chetri, S. Balachandran and PJ Lee (NHMFL, FSU)

## Slide 2: Motivations
SRF cavities research is mostly recipe based in order to achieve high Q and Eacc
Although it resulted in the higher Q and Eacc, the fundamental understanding is still lacking, for examples:
 Role of low temperature baking
 Role of doping and infusion
 Role of flux expulsion and its dependence on cool down rate
 Quench mechanism and cause of higher residual resistance
 and so on
When we try some recipe, we process sample coupons along with SRF cavity for microstructure and magnetization studies, to better evaluate and relate the role of recipe/process modification on SRF cavity performance (either bad or good).
Analytical tool such as SEM, EBSD, XPS, magnetization, susceptibility, SIMS, PTC techniques are used.

## Slide 3: Pre-doping Era (understanding Q-slope, residual loss, hot and cold spot)
Ciovati et al., PRSTAB, 13, 022002 (2010)

## Slide 4: Doping Era (Ti Doping)
Ti diffused ~ 2 mm
Better superconducting gap
Traces seen with XRD to confirm the presence of Ti
Higher low field Q may be related to the trapping of hydrogen by Ti which prevents the formation of hydrides
 Q-rise phenomenon was explained in terms of the broadening of DOS of quasiparticles in dirty limit
Dhakal et al., PRSTAB,16, 042001 (2013)

## Slide 5: Doping Era (N-doping)
N diffused much deeper and surface NbN needed to be removed by EP
Higher low field Q may be related to the trapping of hydrogen by N (similar to Ti) which prevents the formation of hydrides
 Q-rise phenomenon similar to Ti-doping
Dhakal et. al., IEEE Transactions on Applied Superconductivity ( Volume: 25, Issue: 3, June 2015 )

## Slide 6: Doping Era (N-doping)
~15 µm
800 C/3h ( No Nitrogen)
Longitudinal surface
As worked ->800 C+ 20 min N doping
GB
Longitudinal surface
Nitrides on wire surface.
Hydrides close to surface
Near surface hydride debris absent in N doped sample- First direct evidence- Cross sectional microscopy

## Slide 7: Magnetization/N-doping
1hBCP
1hBCP+ 800°C/3h
1hBCP+ 800°C/3h +20N30
20N30+ 10μmEP
20N30+ 20μmEP
20N30+ 30μmEP
Chart: Hc2 (mT)
| 1hBCP | 1hBCP +800°C | 1hBCP +800°C +20N30 | 20N30 +10μmEP | 20N30 +20μmEP | 20N30 +30μmEP
 | 275 | 280 | 330 | 310 | 300 | 300
No N2
N2 doped
Pure Nb
1hBCP
1hBCP+800°C
20N30
+10μmEP
+20μmEP
+30μmEP
Trapped Field
Hc2 increased by N-doping.
EP reduces Hc2 and also the trapped field.
Note: The “trapped fields” here are orders of magnitude greater than in SRF cavities
20N30
S. Chetri, ASC 2016
T = 4.2 K

## Slide 8: N treatment at low temperature/Jlab
P. Dhakal et al., PRAB 21 032001 (2018)

## Slide 9: Coupon samples: N-Infusion/ Jlab, Microscopy/NHMFL/FSU
800°C
800°C+N2@120°C
800°C+N2@140°C
800°C+N2@160°C
Contrast in SEM Back scatter images is due to contributions from changes in crystallographic orientations (including defects), and atomic number
P. Dhakal et al., PRAB 21 032001 (2018)

## Slide 10: XPS Studies: SRF coupon analysis
800 °C/3h+N2 160 °C/48h
800 °C/3h+N2 140 °C/48h
800 °C/3h+N2120 °C/48h
Nitride (397 eV)
Nitrogen peaks detected in samples after 140 °C/48h, 160 °C/48h N infusion treatments but not for the 120 °C/48h N infusion
The in-grain surface structures could indicate nitride phases.
N1s spectrum at 75° takeoff angle
Surface analysis by XPS: Presence of nitrogen in the form of nitride detected for ≥ 140 °C N infusion

## Slide 11: XPS Studies- Take off angle 75°, interaction depth ~7nm
NbN1-xOx
NbN1-xOx
Nb2O5
Nb2O5
800 °C
+N2@160 °C
800 °C
+N2@140 °C
800 °C
+N2@120 °C
800 °C
Nb peak is absent => thicker dirty layer
Nb
Nb
NbN1-xOx is found on Nb baked at 140-160 °C in N atmosphere

## Slide 12: XPS: Differences in take-off angle probes near surface layers
800 °C+N2@140 °C
800 °C+N2@120 °C
In 140-160 °C N-infused Nb,
lesser Nb2O5 concentration on the surface
Formation of NbN1-xOx phase
No bulk Nb observed up to 8 nm depth (thicker dirty layer).
Take-off angle (θ) | Information depth, x (nm)
15° | 1.94
30° | 3.75
45° | 5.30
60° | 6.50
75° | 7.24
In 120 °C “N-not-infused”
NbO appears
800 °C
800 °C+N2@160 °C

## Slide 13: AC susceptibility: Surface sensitive superconducting measurements-FSU/NHMFL
800 °C+N2@120 °C
800 °C+N2@160 °C
T=4.2K
T=4.2K
Hc2
(bulk Nb)
Hc3
Hc3
Increasing AC amplitude from 0.1 Oe to 6 Oe probes thicker surface layers.
Determination of penetration depth of AC fields are in progress.
AC susceptibility measurements show correspondence with XPS data.
* Bulk Hc2 of Nb (240 mT) reached with 6 Oe AC amplitude
* Hc2 value is higher than 240mT after 6 Oe AC amplitude, indicating a dirty layer.

## Slide 14: Bulk Magnetization measurements on cylindrical coupons-FSU/NHMFL
No significant difference in bulk pinning centers…
Hc2~280 mT
Hc2~430 mT (for F12)
Areas between the magnetization loop are almost identical (bulk pinning).
Bulk Hc2 is increased in case of N-infusion at 140 °C and 160 °C. Infusion effect may be deep enough to affect bulk Hc2.
P. Dhakal et al., PRAB 21 032001 (2018)
T = 4.2 K

## Slide 15: SIMS Studies on coupon samples- NCSU data
P. Dhakal et al., PRAB 21 032001 (2018)
Oxygen profile consistence with earlier studies of LTB
SIMS detection limits:
Element | Atomic percent (%) | Weight in ppm
O | 0.05 | 93
C | 0.02 | 23
N | 0.02 | 27
Higher N concentration for 140 and 160C/48hrs treatments.

## Slide 16: Summary
Analytical tools are very valuable in order to understand effect of recipe modification to the performance of SRF cavities.
Understanding of SRF Nb surface is possible from coupon sample analysis, there are correlations found between cavity performance (large area averages) versus local measurements on coupons. Quantitative data, and statistics, are key.
XPS analysis on coupon samples are showing clear differences in Nb surface layer compositions depending on treatment.
  Presence of thick oxy-nitride layers present only after 140°C, 160°C N infusion.
  Sub-oxide layer compositions differ with treatments, presence of NbO detected in near surface layers after 120°C N infusion.
Superconducting measurements on coupon samples which include: PCT, AC susceptibility, and bulk magnetization measurements provides a length scale over which SRF surfaces can be characterized.
  AC susceptibility indicates the level of dirtiness of the surface Nb layers, these measurements show correlations with XPS data in N infused samples.
  Bulk magnetization measurements on N infused also indicate increased bulk Hc2
P. Dhakal et al., PRAB 21 032001 (2018)

## Slide 17: Acknowledgements
This work was supported by the U.S. Department of Energy (Award Numbers DE-SC0009962 and DE-SC0009960). A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1157490 (-2017) DMR-1644779 (2018-) and the State of Florida

## Slide 18
Nb
N2
Ti
Recipe for high Q and high gradient
Thank you !!