## Slide 1: Sample analysis at KEK
Taro Konomi (KEK)

## Slide 2: Contents
The vacuum furnace at J-PARC.
Surface composition analysis by using SIMS and XPS.
DC Magnetic property measurement using MPMS.

## Slide 3: J-PARC furnace
Turbo pump 3unints: SIMADZU TMP3202M (3000L/sec x3)
Cryopump 1unint: ANELVA CAP220 (10000L/sec)
J-PARC furnace has oil free pumps (3 TMP and 1 Cryopump).
After annealing, pressure reaches ~3E-6 Pa

## Slide 4: N-Infusion results
We tried N-infusion 6 times. In 5th and 6th trial, we installed two cavities each.
There are 2 type QE curves. In case of failure Q drops from ~10 MV/m.
# | Result | Series | Treatment | Cavity material
1 | Fail | R-2 | N-Infusion(800x3h+120x48h | FG (TD)
2 | Success | R-8c | N-Infusion(800x3h+120x48h) | FG(TD)
From 2nd infusion, base pressure during infusion was improved from 1E-2Pa to 1E-5Pa by changing the pumping unit. |  |  |  | 
3 | Success | R-9b | N-Infusion(800x3h+125x48h) | FG(TD)
N2 bottle was changed. Titanium bellows were annealed at 650 oC x10 hours |  |  |  | 
4 | Fail | R-2 | N-Infusion(800x3h+160x48h) | FG(TD)
5 | Fail | R-9 | N-Infusion(800x3h+120x48h) | FG(TD)
5 | Success | R-10b |  | LG(CBMM)
N2 inlet line was baked again. |  |  |  | 
6 | Fail | R-2 | N-Infusion(800x3h+120x48h) | FG(TD)
6 | Fail | R-9b |  | FG(TD)

## Slide 5: Sample analysis by D-SIMS @ULVAC
－93Nb －14N+ 93Nb －1H －12C －16O －18O －19F
800℃ Annealing
1st N-infusion
(Failure)
2nd N-infusion
(Success)
15
0
5
10
15
0
5
10
15
0
5
10
Depth (nm)
Depth (nm)
Depth (nm)
Oxygen and Carbon profiles seems to have the relationship with the maximum gradient and Qo.

## Slide 6: XPS measurement @ULVAC
800 oC annealing
1st trial N-infusion (failure)
2nd trial N-infusion (success)
~23nm
~23nm
~23nm
―C1s ― O1s ― Nb3d ― N1s ― Cs3d
Samples of 800oC annealing, 1st and 2nd N-infusion were measured by XPS (ULVAC Inc.)
The depth profile of atomic concentration was measure by sputtering (sputter rate was 2.3 nm/min)
Oxygen depth profile is agree with the SIMS data.

## Slide 7: TOF-SIMS @ NIMS
106.898
106.912
NbN powder
Nb: 92.90638
N: 14.0067
C: 12.0107
H: 1.00794
Nb-N: 106.909
Nb-CH2: 106.922
N-dope sample
Atomic Weight
Δ=0.13
Measurement of the TOF-SIMS @NIMS has started.
The mass resolution is ~0.01 (D-SIMS @ULVAC resolution is ~1)
From this measurement, ~107 mass in KEK sample seems Nb-CH2.
  The peak thought to be Nb-N in D-SIMS measurement may be Nb-CH2.
This peak is not Nb-N

## Slide 8: MPMS @Tohoku Univ.
Φ2mm sphere sample
Fabrication error 2±0.005mm
We measured Hc1(Hvp) and Hc2 of N-dope and N-infusion by using sphere shape sample.
  We could get very sharp edge at Hc1 (Hvp) which first flux enter to the sample.
    Enhancement factor of square samples are unknown.
  Enhancement factor at the sample equator is 150±1.5 %.

## Slide 9: MPMS @Tohoku Univ.
Hc1 (Hvp)/1.5
Hc1 (Hvp) is the edge in the (M-H)/H curve and calculated by multiplying by 1.5 factor.
Hc1 increases in order of N-dope < Anneal < N-infusion.
 | Hc1（Hvp） | Hc2
800℃ anneal +20um CP | 1740 G | ~3800 G
N-infusion (5th ) | 1770 G | ~3800 G
20min N-dope +10um CP | 1530 G | ~3800 G
Transform (M-H)/H calculation

## Slide 10: Summary
N-infusion at J-PARC has the both successful and failed case .
We compared each sample by D-SIMS and XPS.
Carbon and Oxygen seems has the relation with Successful and failure case
From the TOF SIMS measurement. NbN peak measured in D-SIMS seems to be the Nb-CH2 peak.
Hc1 was measured with 2mm sphere sample by SQUID MPMS
Hc1 increases in order of N-dope < Anneal < N-infusion.