## Slide 1: Surface study of nitrogen-infused Nb samples
- Arti Dangwal Pandey, DESY Hamburg
Notes: Our observation:
NbN : 203.8 eV, NbC : 203.3 eV, NbO: 204.0 eV

## Slide 2: Optical inspection of as-received material
W. Singer et al, Phys. Rev. ST Accel. Beams 16, 012003 (2013)
(100)
Samples:
Single crystal Nb(100) : systematic XPS investigation results
  - Nanopolishing – etch profiles were not observable in SEM
Tri-crystal Nb (100) (110) and (111) sample : microscopic observation
  - Nanopolishing + ~100 micro m EP at FNAL
Material : LG Nb from Heraeus: RRR > 300
(100)
(110)
(111)
Notes: One of the remaining disks from LG cavity production described in the paper:

## Slide 3
Nb 3d
XPS of Nb
Chemically polished Nb
N 1s
O 1s
C 1s
Nb2O5
NbO2
NbO
Nb
A. Dangwal Pandey et al., J Material Science (2018) 53:10411–10422
Notes: X-ray photoelectron spectroscopy , Our observation:
NbN : 203.8 eV, NbC : 203.3 eV, NbO: 204.0 eV

## Slide 4: in-situ XPS on UHV-annealed Nb (100)
Nb 3d
NbO
Nb-C
Nb
NbxO
O 1s
C 1s
N 1s
T = 600 °C for 1.5 hours
P600°C < 2 e-8 – 8 e-9 mbar
Pbase = 8 e-10 mbar
Nb-C
Nbx-O
sp3 C
Nb-O
sp2 C
A simplified case as a starting point
Notes: - Figure 1 presents a typical photoemission spectrum of the Nb 3d levels of a Nb ~110! sample annealed at 1400 K for ;20 min with 260 eV photons. This spectrum exhibits four peaks A, B, C, D at the following binding energies: 202.3, 203.7, 205.1, and 206.5 eV, respectively.
Variation of the binding energy of the Nb 3d5/2 level as a function of the valence of Nb atoms. Valence states of Nb atoms corresponding to peaks 2 and 3 are deduced.
- As oxygen atoms occupy interstitial sites in the bcc Nb lattice,23 we infer that the shifted Nb 3d levels in peak A could correspond to Nb6O and Nb4O compounds associated with the octahedral and tetrahedral sites, respectively ~Fig. 5!. Therefore, our analysis of photoemission spectra shows that oxygen dissolved in a Nb single crystal segregates during annealing in UHV and forms a NbOlike
overlayer covering a thin Nb metal layer enriched with interstitial oxygen atoms.

## Slide 5
Nb-C
sp3 C
O 1s
C 1s
N 1s
T = 600 °C for 1.5 hours
P600°C < 2 e-8 – 8 e-9 mbar
Pbase = 8 e-10 mbar
Air-exposed : 1hour
Nbx-O
Nb-O
Nb 3d
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
UHV annealed Nb(100)– after 1hr in air
Notes: - Figure 1 presents a typical photoemission spectrum of the Nb 3d levels of a Nb ~110! sample annealed at 1400 K for ;20 min with 260 eV photons. This spectrum exhibits four peaks A, B, C, D at the following binding energies: 202.3, 203.7, 205.1, and 206.5 eV, respectively.
Variation of the binding energy of the Nb 3d5/2 level as a function of the valence of Nb atoms. Valence states of Nb atoms corresponding to peaks 2 and 3 are deduced.
- As oxygen atoms occupy interstitial sites in the bcc Nb lattice,23 we infer that the shifted Nb 3d levels in peak A could correspond to Nb6O and Nb4O compounds associated with the octahedral and tetrahedral sites, respectively ~Fig. 5!. Therefore, our analysis of photoemission spectra shows that oxygen dissolved in a Nb single crystal segregates during annealing in UHV and forms a NbOlike
overlayer covering a thin Nb metal layer enriched with interstitial oxygen atoms.

## Slide 6
Nb-C
sp3 C
O 1s, 70°
C 1s, 70°
Nb 3d, 70°
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb-O
N 1s, 70°
UHV annealed Nb(100)– after 1hr in air
NbxO with BE @ 202.6 eV :
- is extending on top surface together with Nb2O5
Notes: - Figure 1 presents a typical photoemission spectrum of the Nb 3d levels of a Nb ~110! sample annealed at 1400 K for ;20 min with 260 eV photons. This spectrum exhibits four peaks A, B, C, D at the following binding energies: 202.3, 203.7, 205.1, and 206.5 eV, respectively.
Variation of the binding energy of the Nb 3d5/2 level as a function of the valence of Nb atoms. Valence states of Nb atoms corresponding to peaks 2 and 3 are deduced.
- As oxygen atoms occupy interstitial sites in the bcc Nb lattice,23 we infer that the shifted Nb 3d levels in peak A could correspond to Nb6O and Nb4O compounds associated with the octahedral and tetrahedral sites, respectively ~Fig. 5!. Therefore, our analysis of photoemission spectra shows that oxygen dissolved in a Nb single crystal segregates during annealing in UHV and forms a NbOlike
overlayer covering a thin Nb metal layer enriched with interstitial oxygen atoms.

## Slide 7
Nb 3d
Nb
NbxO
Nb 3d
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
NbxO:
- extending to top surface Nb2O5
NbxCy:
- enhanced compared to NbO- so closer to surface
Nb 3d, 70°
UHV annealed Nb(100)– after 1hr in air
NbO
Nb-C
Nb2O5
NbO2
NbxO
Nb
XPS
Detector
Nb
Interstitial -rich
Nb
NbxCy / NbO2
NbO
Nb2O5
NbxO
Notes: - Figure 1 presents a typical photoemission spectrum of the Nb 3d levels of a Nb ~110! sample annealed at 1400 K for ;20 min with 260 eV photons. This spectrum exhibits four peaks A, B, C, D at the following binding energies: 202.3, 203.7, 205.1, and 206.5 eV, respectively.
Variation of the binding energy of the Nb 3d5/2 level as a function of the valence of Nb atoms. Valence states of Nb atoms corresponding to peaks 2 and 3 are deduced.
- As oxygen atoms occupy interstitial sites in the bcc Nb lattice,23 we infer that the shifted Nb 3d levels in peak A could correspond to Nb6O and Nb4O compounds associated with the octahedral and tetrahedral sites, respectively ~Fig. 5!. Therefore, our analysis of photoemission spectra shows that oxygen dissolved in a Nb single crystal segregates during annealing in UHV and forms a NbOlike
overlayer covering a thin Nb metal layer enriched with interstitial oxygen atoms.

## Slide 8
C 1s
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
O 1s
N 1s
N-infused Nb(100)– after 1hr in air
Nb2XyO5-y
-Besides already observed oxide and carbides phases: Hint for a different phase possibly Nb2XyO5-y
X : C/N/O ?
- Nitrogen: Very week broad peak in the energy range 397 - 399 eV
- Surface Carbon :
sp2 hybridization dominant
N-infusion: (800 °C -2 hrs, 120°C in 0.03 mbar N2 for 48 hrs)

## Slide 9
Normal-exit XPS
Nb
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb2XyO5-y
0°
70°
Nb
Interstitial -rich Nb
NbxO
NbxCy / Nb2XyO5-y/NbO2
NbO
Nb2O5
Nb-C : large amount
NbxO extending to top
N-infused Nb(100)– after 1hr in air
XPS
Detector

## Slide 10
UHV-annealed 600°C, in air for 1 hr
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
N-infused, in air for approx. 1 hr
N-infused vs UHV-annealed Nb (100)
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb2XyO5-y
Nb-C : very larger amount
- different chambers used
- C segregating from bulk?
  C-precipitates formed on this sample, but not on ultra-pure N-infused Nb
Less NbxO on diffused Nb
- NbxO extending to top
Slower Nb2O5 growth on N-infused Nb
higher NbO content

## Slide 11
N b 3d
N-infused Nb(100) after HPR
N 1s
Nb-C rich near-surface region
ads. N2
C 1s
O 1s
Nb-C
Nb-O
sp3 C

## Slide 12
C-rich precipitates on surface , C-rich layer just below the surface oxide
Negligible N level
N-infusion +HPR: Microscopic study
Pt layer

## Slide 13
(100)
(100)
C-rich precipitates:
Growth dependence of on the Nb grain orientation
Were not observed on :
    2000°C UHV-annealed SC Nb (100),
    EP LG Nb (100)
But observed on nano-polished LG Nb (100)
=> clean surface necessary to avoid the precipitates
Detrimental to cavity performance?
Nb Tri-crystal:
ADP_F2 : after EP and 800°C annealed with1DE3 FNAL in Jan 2018
(110)
(111)

## Slide 14
Systematic XPS studies on nanopolished Nb (100) can track the surfaces changes on N-infused compared to UHV-annealed Nb(100) sample after an hour of air-oxidation:
  - increased NbO and NbC but decreased NbxO content,
  Slower Nb2O5 growth on N-infused Nb sample
  Hint for new phase: NbXxO5-x ; X: O, C, N ?
  Nb-N bonding : very week but observable peak for Nb-N
Electron microscopy investigatons confirmed carbon-rich layer below the surface oxide.
Tricrystal Nb: (100), (110) and (111) microscopic investigations revealed dependence of growth of C-rich preipitates on grain-orientation. Moreover, cleaner surface (EP vs. nanopolishing) seems to suppress their formation.
Next steps: Pronounced intensity of Nb2O5 inhibits the detection of other phases in neighbouring BE range. To invstigate in detail NbxO and Nb2XyO5-y phase
- In-situ XPS experiments and infusion in XPS load-lock
- Sputter depth profiling: preferntial sputtering issues- how SIMS avoid this?
Summary:
Nb
Interstitial -rich Nb
NbxO
Nb2XyO5-y/NbO2/NbxCy
NbO
Nb2O5

## Slide 15: Acknowledgements
Detlef Reschke
Nicholas Walker
Joern Schaffran
Cooperation between:
DESY Nanolab – Prof. Andreas Stierle
DESY Linear Accelerator Technologies – Prof. Brian Foster
DESY Superconducting Accelerator Technologies – Dr. Hans Weise
Special thanks to: Dr. Waldemar Singer and Xenia Singer for providing the material.
- Anna Grassalino and her team for ongoing collaboration
between DESY and FNAL on N-infusion on cavities and samples
Marc Wenskat
Lea Steder
Christopher Bate
Heshmat Noei
Vedran Vonk
Thomas Keller
Andreas Stierle
Alena Prudnikava
Guilherme D. Semione
Satishkumar Kulkarni
Thank you very much for your attention!