## Slide 1: X-ray Cross-Correlation Analysis of Mesocrystals
Elizaveta Morozova
Summer Student
Supervised by Nastasia Mukharamova,
Ivan Vartaniants

## Slide 2: COINS: Coupled organic-inorganic nanostructures
Coupled organic-inorganic nanostructures (COIN) provide a new approach to applications of semiconductor nanocrystals (NC) for power conversion. A typical COIN consists of periodically alternating NCs and organic semiconductor molecules, promoting carrier transport across the lattice.
100
111
PbS
Cu4PAc
5 nm

## Slide 3: Experimental setup (P10 beamline, PETRA III)
Substrate: Si3N4-membrane, 0.5x0.5 mm2, 50 nm thick
X-ray beam: E = 13.8 keV Size = 400x400 nm2 (GINIX endstation) Flux = 1010-1011 ph/sec
Spatial scanning:
1) 21x21 points
2) 61x61 points
with 1 μm resolution.
Detector Eiger 4M Size = 2070x2167 pixels Pixel size = 75x75 μm Sample-detector distance = 38 cm

## Slide 4: Radial average

## Slide 5: Atomic Lattice (scan 1, scan 2)
a=5,9 Å
q (exp1) | q (exp2) | q(th) | (hkl) | h+k+l
1,855 | 1,855 | 1,8436 | {111} | 3
2,137 | 2,141 | 2,1288 | {002} | 2
3,033 | 3,028 | 3,01 | {022} | 4

## Slide 6: Superlattice (scan 1, scan 2)
q (exp1) | q (exp2) | q(th) | (hkl) | h+k+l
0,0939 | 0,0925 | 0,093 | {002} | 2
0,1284 | 0,1284 | 0,1263 | {112} | 4
0,1629 | 0,1615 | 0,1701 | {220} | 4
0,1864 | 0,1864 | 0,187 | {031} | 4
a=104 Å
c=135 Å
c/a=1,298
Unit cell parameters

## Slide 7: Average intensity of diffraction on the lattice
Atomic lattice
Superlattice
Scan 2
Scan 1
Scan 2
Scan 1
1
2
4
3
1
1
2
2
4
3
3
4
0,5
2,5
x107
x107
x107
0,8
1,25
0,85
1,2
2,15
1,65
x106
x107
x107
0,85
0,8
1,3
1,4
x107
x106
1,1
1,9
0,5
0,2
(111)
(002)/(020)/(200)
(200)
(220)

## Slide 8: WAXS spatial resolved map (scan 1)
(111)
(111)
(002)
Blue lines correspond to peaks with q in the range (2,0; 2,2) Å-1;
red – to (1,7;1,9) Å-1.

## Slide 9: SAXS spatial resolved map (scan 1)
Blue lines correspond to peaks with q in the range (0,9; 1,0) Å-1
(002)
(110)

## Slide 10: Cross-Correlation Analysis
CCF calculation
Averaging
Mask

## Slide 11: Cross-Correlation Analysis (qsaxs-waxs1, qsaxs-waxs2)
Scan 1 | 
-136° | 136°
-95° | 96°
-84° | 89°
-44° | 44°
Scan 2 | 
-135° | 136°
-92° | 89°
-44° | 45°

## Slide 12: Two typical structures forming the sample
φ=54°
ψ=41°
φ=161°
ψ=80°
-1 -1 0
-1 1 0
1 1 0
1 -1 0
0 -2 0
0 2 0
-2 0 0
2 0 0
2 -2 0
-2 2 0
-1 3 0
1 -3 0

## Slide 13: Peaks of diffraction patterns
(00)
(200)
(0)
(110)
(10)
(10)
(20)
(20)
(0)
(0)
()
(220)
(10)
()
(00)
(0)
(0)
()
()
(0)
()
(0)
(110)
(10)
(0)
(011)
(01)
(0)
(12)
(022)
(02)
()
()

## Slide 14: Model of CCF
φ
CCF(φ)

## Slide 15: Results
We analysed two scans: 21x21 µm, 61x61 µm;
Calculated unit cell parameters and tetragonal distortion;
(104 Å, 135 Å; c/a=1,3);
No domains were observed;
XCCA was performed and CCFs show some structure and look similar for both scans;
We created models of two structures the sample mostly consists of;
Model of CCF and real CCF look the same what means that conclusions about structure, atomic lattice and sizes of unit cells are truthful;
Despite we cannot see any structure, XCCA shows that there are two preferable orientations of the lattice in the sample and in general the orientation between AL and SL is conserved.

## Slide 16
Thank you for your attention!