## Slide 1
UHV-annealing vs N-infusion
a
b
c
Niobium surface investigation for RF cavity applications.
Arti Dangwal Pandey, Guilherme Dalla Lana Semione, Christopher Bate, Marc Wenskat, Jörn Schraffan, Thomas F. Keller, Vedran Vonk, Heshmat Noei, Detlef Reschke, Hans Weise, Andreas Stierle
Introduction
Thermal treatments of SRF cavities in vacuum and nitrogen partial pressures are known to increase the performance of niobium cavities. [1,2] However, the physical and chemical processes as well as the phenomena involved are not clearly understood [3-5];
Goal: In-situ tracking of the changes in surface layer during Nb thermal treatment by means of surface-sensitive techniques.
A much simpler system of single-crystal Nb were selected: heated in different vacuum conditions and nitrogen partial pressures.
Methods
X-ray reflectivity (XRR): to retrieve the layered structure of the surface based on electron density profile;
X-ray photoelectron spectroscopy (XPS) to identify the chemical entities present on the surface;
N, O and C interstitials occupy octahedral sites in the Nb bcc lattice; Give rise to diffuse scattering intensities;
Grazing Incidence X-Ray Diffraction (GIXRD) for tracking the changes in thermal diffuse scattering (TDS) and Interstitial induced diffuse scattering intensities during the treatment
Summary
In-situ investigation of the near-surface region during thermal treatments with and without N2;
XRR reveals dissolution of natural oxides, NbO remains at the surface after 800°C annealing step;
Thermal diffuse scattering and interstitial diffuse scattering under evaluation from HEGIXRD;
XPS: No Nb-N containing phase in Nb-infused Nb, significant changes in NbO and NbC phases.
Acknowledgments
For HR-EDX measurements and analysis: Thobias Krekeler, BEEM, TUHH.
This work was partially funded by the Bundesministerium für Bildung und Forschung (BMBF) project “Performance improvement of SRF cavities by surface treatment including mechanical polishing and nitrogen thermal treatment” and DSF.
surfaces changes on N-infused compared to UHV-annealed Nb(100):
slower Nb2O5 growth on N-infused Nb sample
Increased NbO and NbC phases
Hint for a new phase: NbXxO5-x ; X: O, C, N
Nb-N bond: signal too week to identify a Nb-N phase
Nitrogen infusion
  Nanopolished, cavity material (large-grain Nb)
  ΔT = 800°C (2 hours); Cooldown to 120°C
  ΔPN2 = 0.033 mbar (48 hours) while @120°C
800°C annealing partially consumes native oxides, NbO remains;
Addition of N2 doesn’t form new layers, effect also not time dependent within the proposed time scales;
Similar results obtained for single-crystal samples.
~2.7 nm
NbO
Nb
Nb2O5
NbO2
NbO
800°C/2 hours
During ‘N- infusion’
@ 120 °C
RT
~2.3 nm
Nb
Interstitial diffuse scattering
800°C UHV-annealed
NbO
Nb-C
Nb
NbxO
Nb 3d, 0°
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
UHV annealed + 1 hr. air-exposure
UHV annealed + 1 hr. air-exposure
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb2XyO5-y
N-infused + 1 hr. air-exposure
Chart: Eacc [MV/m]
| 1.96 | 1.64 | 2.1999999999999997 | 2.81 | 3.42 | 4.37 | 5.6499999999999995 | 7.26 | 9.17 | 11.6 | 13.1 | 15.1 | 17.3 | 19.899999999999999 | 23.7 | 27.799999999999997 | 31.599999999999998 | 32.6
1DE20: First test at DESY in 2007 | 31800000000 | 19900000000 | 23200000000 | 24100000000 | 21900000000 | 22600000000 | 23800000000 | 23400000000 | 22400000000 | 20900000000 | 20200000000 | 19900000000 | 19100000000 | 18100000000 | 18200000000 | 17500000000 | 15300000000 | 14300000000
1DE20: Tested at FNAL after Infusion | 24657704300 | 41607573200 | 40637791300 | 39867469400 | 168530008 | 42294642300 | 42158761500 | 41807821300 | 41816657000 | 41402377100 | 40823341600 | 40404776700 | 39763466400 | 39913322700 | 38419491000 | 35256632700 | 36166445900 | 36664991800 | 52124824700 | 48724596200 | 143288276000 | 35233885700 | 33877494600 | 32709221100 | 30913519900 | 30681465200 | 29959266700 | 29483788100 | 29359530200 | 29116039700 | 29029036400 | 28884369600 | 28901939600 | 28835204100 | 28845524100 | 28672516700 | 28922563900 | 28331031000 | 27837613900 | 27411666600 | 26380899900 | 26004022300 | 25921606700 | 7285548760 | 25380570300 | 26374555000 | 26483935700 | 26330605900 | 19422.2765 | 763287116 | 24717927200
Nb 3d, 70°
N1s
N1s, 70°
Samples infused with SRF cavity
[1] A. Grassellino et al, Supercond. Sci. Technol. 26 102001 (2013),
[2] A. Grassellino et al, Supercond. Sci. Technol. 30 094004 (2017),
[3] A. D. Pandey et al, Journ. of Mat. Sci. 53 10411 (2018),
[4] P. Dhakal et al, IEEE Tran. on App. Superc. 25 3500104 (2015),
[5] F. Barkov et al, Journ. Of App. Phys. 114 164904 (2013),
[6] M. Delheusy et al, Appl. Phys. Lett. 92 101911 (2008).
Electropolished Nb samples: N-infused with a SRF cavity
C-rich precipitates: Nb orientation dependent
XPS: difficult to detect phases below thick Nb penta-oxide
Ongoing: XPS depth-profiling
Nb(111)
Nb(100)
Nb 3d, 70°
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb 3d, 70°
NbO
Nb-C
Nb
NbxO
Nb2O5
NbO2
Nb2XyO5-y
Natural oxides dissolve upon annealing
N2 injection does not promote layer growth
Diffuse intensity as a tool to retrieve concentration profile
N, O atoms can occupy octahedral sites in the Nb bcc lattice; Give rise to diffuse scattering intensities ;
Simulation and experiments confirm such intensities for the (110) Nb surface [6];