## Slide 1
Low T Bake – Cool Down Studies
Daniel Bafia
TTC WG3
7 February 2019

## Slide 2: Push for Higher Accelerating Gradients: 75/120 Bake
Higher quench fields
Fewer cavities
Lower cost
f=1.3GHz
T=2K

## Slide 3: Push for Higher Accelerating Gradients: 75/120 Bake
Quench at 49MV/m!
Higher quench fields
Fewer cavities
Lower cost
f=1.3GHz
T=2K

## Slide 4: Push for Higher Accelerating Gradients: 75/120 Bake
Quench at 49MV/m!
Additional 2 hours at 75C
75/120 bake recipe:
75x4hrs/120Cx48hr in UHV
f=1.3GHz
T=2K

## Slide 5: Exploring 75/120C Bake Cavity Performance
Gradients of 49MV/m have been achieved at Fermilab
Notes: Sequence: 75/120 then EP then 120
-- Q matches at low

## Slide 6: Exploring 75/120C Bake Cavity Performance
Gradients of 49MV/m have been achieved at Fermilab
75/120 bake recipe yields higher Q0 and G (+4MV/m) than standard 120C bake
Curve shape changes – not due to trapped magnetic flux
Notes: Sequence: 75/120 then EP then 120
-- Q matches at low

## Slide 7: Further World Record Achieved: +50MV/m!
51MV/m=218mT
@ Low T!
50MV/m=213mT
@ 2K

## Slide 8: Quench Field Histogram
More than a dozen different cavities tested; multiple tests for several cavities
  Consistently achieve excellent cavity performance
Material : WC, TD, NX, Hareaus; cavities from AES, RI, DESY, KEK
KEK cavities (TD material): optical inspection indicates some potential surface flaws?
FNAL, DESY: TD, NX, WC, H
“Bunching up” of quench field observed: (45MV/m vs 48MV/m)
Chart: Quench Field (MV/m)
| 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50
 | 0 | 1 | 0 | 1 | 0 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 3 | 3 | 5 | 6 | 5 | 6 | 13 | 8 | 0

## Slide 9: Sensitivity of 75/120C vs 120C Baked Cavities
Compared to 120C bake, sensitivity to trapped magnetic flux is decreased post 75/120
Could be due to differences in the pinning of vortices due to introduction of vacancies at 75C
2/7/2019

## Slide 10: Bifurcation in Performance Post 75/120 Bake
f=1.3GHz
T=2K

## Slide 11: Bifurcation in Performance Post 75/120 Bake
Observed branching behavior in cavities retested without disassembly in between
f=1.3GHz
T=2K

## Slide 12: Bifurcation in Performance Post 75/120 Bake
Possible Causes for Branching | Likely Candidate?
Dewar | NO – observed in 2 separate dewars
Top Plate | NO
Cables | NO
Calibration | NO - Qext 2 does not explain branching in Q and G
Flux trapping | NO – MOST were cooled in zero compensated field
Observed branching behavior in cavities retested without disassembly in between
f=1.3GHz
T=2K

## Slide 13: Likelihood of Trapped Flux Causing Bifurcation
No transverse field compensation/fluxgates for these tests – but transverse fields measured to be <1mG in the past
Estimate of field necessary to cause bifurcation @ 40MV/m:
Rlower =270nΩ/1E10 = 27nΩ
Rupper =270/1.56E10 = 17.3nΩ
Btrapped =10nΩ /1.7nΩ /mG = 5.88mG

## Slide 14: Likelihood of Trapped Flux Causing Bifurcation
Tc
Tc
≤1mG before Tc
≤0.2mG before Tc
No transverse field compensation/fluxgates for these tests – but transverse fields measured to be <1mG in the past
Estimate of field necessary to cause bifurcation @ 40MV/m:
Rlower =270nΩ/1E10 = 27nΩ
Rupper =270/1.56E10 = 17.3nΩ
Btrapped =10nΩ /1.7nΩ /mG = 5.88mG

## Slide 15: Likelihood of Trapped Flux Causing Bifurcation
Tc
Tc
Tc
≤1mG before Tc
≤0.2mG before Tc
No transverse field compensation/fluxgates for these tests – but transverse fields measured to be <1mG in the past
Estimate of field necessary to cause bifurcation @ 40MV/m:
Rlower =270nΩ/1E10 = 27nΩ
Rupper =270/1.56E10 = 17.3nΩ
Btrapped =10nΩ /1.7nΩ /mG = 5.88mG
05/08 – no coils – 49MV/m
5/31 – coils – 41MV/m!

## Slide 16: Likelihood of Trapped Flux Causing Bifurcation
Tc
Tc
Tc
≤1mG before Tc
≤0.2mG before Tc
No transverse field compensation/fluxgates for these tests – but transverse fields measured to be <1mG in the past
Estimate of field necessary to cause bifurcation @ 40MV/m:
Rlower =270nΩ/1E10 = 27nΩ
Rupper =270/1.56E10 = 17.3nΩ
Btrapped =10nΩ /1.7nΩ /mG = 5.88mG
Trapped flux may not be responsible for bifurcation in performance
What about the effect of cavity cool down protocol?
05/08 – no coils – 49MV/m
5/31 – coils – 41MV/m!

## Slide 17: Motivation for Investigating Cavity Cool Down: Hydride Formation
Avg. No. of NbH Precipitates within 10 x 10 μm2 unit area during cooling
Plots courtesy of Zuhawn Sung
2/7/2019
Daniel Bafia | TTC at TRIUMF
Different recipes produce different amounts of hydrogen capture sites (vacancies, nitrogen, dislocations, etc)
Amount of captured hydrogen could vary the dangerous temperature region in which hydrides form
Dwelling in this “dangerous” temperature region could be detrimental to cavity performance – cool down rate could affect 75/120 bake cavity performance
Nb-H Phase Diagram

## Slide 18: Motivation for Investigating Cavity Cool Down: Hydride Formation
Avg. No. of NbH Precipitates within 10 x 10 μm2 unit area during cooling
Plots courtesy of Zuhawn Sung
2/7/2019
Daniel Bafia | TTC at TRIUMF
Different recipes produce different amounts of hydrogen capture sites (vacancies, nitrogen, dislocations, etc)
Amount of captured hydrogen could vary the dangerous temperature region in which hydrides form
Dwelling in this “dangerous” temperature region could be detrimental to cavity performance – cool down rate could affect 75/120 bake cavity performance
Nb-H Phase Diagram
No obvious relationship between cavity cool down rate and performance

## Slide 19: Motivation for Investigating Cavity Cool Down: Hydride Formation
Avg. No. of NbH Precipitates within 10 x 10 μm2 unit area during cooling
Plots courtesy of Zuhawn Sung
2/7/2019
Daniel Bafia | TTC at TRIUMF
Chart: Hydride Size Through Warm Up of 120C Baked Cavity Cutout
| -0.10565999999999999 | 0 | 0.10565999999999999 | 0.21132000000000006 | 0.31697999999999998 | 0.42264000000000002 | 0.5283000000000001 | 0.63396000000000008 | 0.73961999999999994 | 0.84528000000000003 | 0.95094000000000001
300K | 10.0272 | 12.1364 | 8.978 | 8.4522 | 18.869 | 45.913 | 59.8121 | 41.9346 | 16.5423 | 0 | 1.4022
320K | 6.7294 | 2.8077 | 4.4415 | 27.2424 | 38.8374 | 37.0574 | 0 | 0.8542
340K | 8.4002 | 6.8343 | 36.3309 | 45.221 | 50.4708 | 0 | 7.6039
360K | 10.6206 | 7.6734 | 23.9459 | 55.3222 | 51.6843 | 0 | 6.3301
380K | 7.3655 | 6.4319 | 37.371 | 48.8851 | 24.8587 | 0
For a 120C baked cavity cutout, hydrides appear to decrease in size when the sample is heated to 320K
Heating to 340K appears to INCREASE hydride size.
Elevated initial dewar temperatures may also affect the performance of 75/120 bake cavities
Nb-H Phase Diagram
Different recipes produce different amounts of hydrogen capture sites (vacancies, nitrogen, dislocations, etc)
Amount of captured hydrogen could vary the dangerous temperature region in which hydrides form
Dwelling in this “dangerous” temperature region could be detrimental to cavity performance – cool down rate could affect 75/120 bake cavity performance
No obvious relationship between cavity cool down rate and performance

## Slide 20: Effect of Elevated Initial Dewar Temperature on Cavity Performance

## Slide 21: Comparison of 75/120 Bake Cavities Cooled From 295K vs 320K
QvsE of Cavities Post 75/120 Bake
f=1.3GHz
T=2K

## Slide 22: Comparison of 75/120 Bake Cavities Cooled From 295K vs 320K
Cooling cavities from 320K shows consistently higher quench field and Q0 at high fields for cavities post 75/120 bake when compared to cooling from 295K.
QvsE of Cavities Post 75/120 Bake
f=1.3GHz
T=2K

## Slide 23: Decomposition of 75/120 Bake Cavities Cooled from 295K vs 320K
Branching in both BCS and residual components – not due to trapped flux
Cooling down from 320K gives a BCS similar to that of infusion

## Slide 24: Comparison of 75/120 Bake Cavities Cooled From 295K vs 320K
Cooling cavities from 320K shows consistently higher quench field and Q0 at high fields for cavities post 75/120 bake when compared to cooling from 295K.
In-situ 320K may be dissociating non-superconducting niobium hydrides
Chart: Hydride Size Through Warm Up of 120C Baked Cavity Cutout
| -0.10565999999999999 | 0 | 0.10565999999999999 | 0.21132000000000006 | 0.31697999999999998 | 0.42264000000000002 | 0.5283000000000001 | 0.63396000000000008 | 0.73961999999999994 | 0.84528000000000003 | 0.95094000000000001
300K | 10.0272 | 12.1364 | 8.978 | 8.4522 | 18.869 | 45.913 | 59.8121 | 41.9346 | 16.5423 | 0 | 1.4022
320K | 6.7294 | 2.8077 | 4.4415 | 27.2424 | 38.8374 | 37.0574 | 0 | 0.8542
Courtesy of Zuhawn Sung
QvsE of Cavities Post 75/120 Bake
AFM finds minimum Nb-H size @ 320K
f=1.3GHz
T=2K

## Slide 25: Comparison of Cavities Cooled From 295K vs 345K
f=1.3GHz
T=2K
QvsE of 120C and 75/120 Bake Cavities

## Slide 26: Comparison of Cavities Cooled From 295K vs 345K
QvsE of 120C and 75/120 Bake Cavities
In-situ 345K bake degrades 120C bake cavity performance, not 75/120 baked cavities!
f=1.3GHz
T=2K
120C baked cavity performs on lower branch post in-situ 345K!

## Slide 27: Comparison of Cavities Cooled From 295K vs 345K
Chart: Hydride Size Through Warm Up of 120C Baked Cavity Cutout
| -0.10565999999999999 | 0 | 0.10565999999999999 | 0.21132000000000006 | 0.31697999999999998 | 0.42264000000000002 | 0.5283000000000001 | 0.63396000000000008 | 0.73961999999999994 | 0.84528000000000003 | 0.95094000000000001
300K | 10.0272 | 12.1364 | 8.978 | 8.4522 | 18.869 | 45.913 | 59.8121 | 41.9346 | 16.5423 | 0 | 1.4022
320K | 6.7294 | 2.8077 | 4.4415 | 27.2424 | 38.8374 | 37.0574 | 0 | 0.8542
340K | 8.4002 | 6.8343 | 36.3309 | 45.221 | 50.4708 | 0 | 7.6039
QvsE of 120C and 75/120 Bake Cavities
In-situ 345K bake degrades 120C bake cavity performance, not 75/120 baked cavities!
In-situ 345K bake could be increasing hydride size for 120C bake but not for 75/120 bake
75/120 bake may introduce more vacancies – more robust to hydride formation at higher temps
120C baked cavity performs on lower branch post in-situ 345K!
f=1.3GHz
T=2K

## Slide 28: Decomposition of 120C Baked Cavity Cooled from 294K vs 345K
Branching observed in both residual and BCS resistances
Cooling from 345K causes BCS to resemble N-infused cavities
* Both curves have trapped flux
*
*

## Slide 29: Conclusions
Bifurcation in performance of cavities post 75/120 bake recipe is still not fully understood; branching behavior exists in both BCS and residual resistances
Branching behavior is likely not due to trapped magnetic flux
The decrease in the sensitivity to trapped magnetic flux could be due to a change in the pinning of vortices due to introduction of vacancies at 75C
Cavity cool down rates through “dangerous” nano-hydride formation regions may be responsible for observed bifurcation but has not yet been observed
Cooling cavities down from an initial dewar temperature of 320K consistently gives upper branch performance for 75/120 bake cavities whereas cooling from 345K causes degradation of 120C bake only.

## Slide 30: Backup Slides

## Slide 31: Flux Gates

## Slide 32: Flux Gates – AES010 + AES022
Cool From 345K
Cool From 294K
Upper performance for 120C
Lower performance branch for 120C

## Slide 33: Comparison of Cavities Cooled Down from 294K vs 345K
f=1.3GHz
T=2K
QvsE

## Slide 34: Effect of Cool Down on Performance: RI002
“Slow” Cool down
Upper branch obtained after cooling from 320K, could not recover lower branch

## Slide 35: AFM Warm up Study by Zuhawn Sung
300K
320K
360K
340K
380K

## Slide 36: Recovering Lower Performance Curve

## Slide 37: Recovering the Lower Performance Curve – AES022
Upper branch obtained by cooling from T=320K
Cooling from T0=295K again does not recover lower branch
Slow cooling from T0=320K also fails – cannot recover the lower curve
“Slow” Cool down