## Slide 1: Strong-field and attosecond science in nanoscale solids
Giulio Vampa
Stanford PULSE Institute

## Slide 2: Watching chemical and material processes on the atomic scale in space and time
Development of an XUV microscope with:
Superresolution (goal: atomic res.)
Chemical / elemental specificity
Time-resolved (atto-femto)
Non-contact
Non-vacuum
Giulio Vampa, Jelena Vuckovic, Shanhui Fan, Olav Solgaard, Phil Bucksbaum & David Reis (+ Tony Heinz)
Began Jan 2018

## Slide 3: Watching chemical and material processes on the atomic scale in space and time
Ghimire, Shambhu, et al. "Observation of high-order harmonic generation in a bulk crystal." Nature physics 7.2 (2011): 138.
Fundamentals and applications of high-harmonic generation from silicon

## Slide 4
Watching chemical and material processes on the atomic scale in space and time
Obvious connection: use DLA for e-/x-ray microscopy, as long as beams can be kept small (nanoscale)

## Slide 5: Watching chemical and material processes on the atomic scale in space and time
Ghimire, Shambhu, et al. "Observation of high-order harmonic generation in a bulk crystal." Nature physics 7.2 (2011): 138.
Fundamentals and applications of high-harmonic generation from silicon
… using coherent VUV/XUV high-harmonic sources
Ghimire et al, Nature Physics 7, 138 (2011)
G. Vampa et al., Optics Letters 44, 259 (2019)
Driver: 2.4 um, 70 MHz MOPA
108 ph/sec

## Slide 6
Watching chemical and material processes on the atomic scale in space and time
The lasers
Yb rod amplifier + OPCPA
Yb pump: Amplitude – 35 W, 230 fs, 350 kHz, 1030 nm
OPCPA: Class 5 Dual Quasar – 4 W, ~ 50 fs, CEP @ 1500 nm
2 W, ~ 100 fs, CEP @ 3200 nm
IPG Cr2+:ZnS MOPA
(80 MHz , 6W, 26 fs (3 cycles), 2.3 um, + 0.4 W of SH output!)
Now 27 W, 8 cycles. Future sub-2-cycles.
Generated ~ 11 eV harmonics from ZnO @ 80 MHz!

## Slide 7: Nanoscale bright coherent VUV sources One proposition with dielectric tips/cones
S. Buddhiraju, S. Fan collaboration
Size limitation is ~ 1 wavelength of XUV

## Slide 8: Nanoscale bright coherent VUV sources The goal
Phase matching absorption-limited VUV/XUV
Nanoscale VUV/XUV source
Size limitation is ~ 1 wavelength of XUV

## Slide 9: Nanoscale bright coherent VUV sources A first experiment

## Slide 10: Nanoscale bright coherent VUV sources Future plan
N. Sapra et al., ArXiv:1808.07630
Devise phase matching scheme for planar structures
Development of “attosecond nanophotonics” building blocks. Broadband nanophotonic couplers optimized for low GDD (w/ Fan & Vuckovic)
Notes: #3: ties to the general approach of merging strong-fields and light transients with nanophotonics (for example: on-chip sources and optical strong-field communication?)

## Slide 11: Going super-resolution
~ 10 nm
~ 1 nm
Isolated defects in a host lattice
Tips (dielectric & metallic)

## Slide 12
Joint opportunities
Coupling of short femtosecond laser pulses to planar nanophotonic devices
  Bandwidth (1 octave!)/ Spatio-temporal distortions
  Dispersion engineered waveguides
Tailored field distribution inside materials, not in vacuum
Nanopatterning skills
Nanotips as confined strong-field/XUV sources