## Slide 1: Tests on Chess 2 ASIC
Yubo HanIHEP , Dionisio Doering, Pietro Caragiulo, Larry Ruckman, Camillo Tamma, Su Dong

## Slide 2: Pixel description

## Slide 3: Outline
Checking basic characteristic of the 2(3 in total) chips:
  IV curve
  Tests Without/With Bias
    Sweeping Threshold with BL=0.7V (typical value)
    Similar Tests with varies BL

## Slide 4: IV curves
Similar IV curve to last 200 Ohm/cm ship:
  Both two chip could reach a plateau after ~ -7V
  High Plateau level: ~0.8mV
A 2nd step around -25V.

## Slide 5: Tests of Daughter board 1
Test:
Without bias voltage
BL=0.7V (868)
Threshold sweeping
Observations
Matrix 1 has “normal” performance
Matrix 2 has a very hot pixel (127,31)
Matrix 1
Matrix 2
Daughter board 1
200 Ohm/cm

## Slide 6: Tests of Daughter board 1
Daughter board 1
200 Ohm/cm
Matrix 1
Matrix 2
No bias
Bias -10V
No bias
Bias -10V
Test:
bias voltage: -10V
BL=0.7V (868)
Threshold sweeping
Observations
Matrix 1: “Tail” at higher threshold
Matrix 2: still has (127,31) problem but different threshold range to see it

## Slide 7: Tests of Daughter board 1
Daughter board 1
200 Ohm/cm
BL
Tests:
Bias voltage: -10v
BL= 0.4V, 0.6V, 0.8V, 1.0V, 1.2V
Threshold sweeping: BL±0.2V
Observations
The Threshold at which the chip starts to report hits has offset with the current BL
Still suggesting BL ~0.7V might be better
0.4V
0.6V
0.8V
1.0V
1.2V

## Slide 8: Tests of Daughter board 2
Daughter board 2
200 Ohm/cm
Matrix 1
Matrix 2
Test:
Without bias voltage
BL=0.7V (868)
Threshold sweeping
Observations
Both Matrix have normal TH vs Counts results
No more (127,31) pixel in Matrix 2

## Slide 9: Tests of Daughter board 2
Daughter board 2
200 Ohm/cm
BL
BL
Matrix 1
Matrix 2
Tests:
No Bias voltage
BL= 0.4V, 0.6V, 0.8V, 1.0V, 1.2V
Threshold sweeping: BL±0.2V
Observations
Still suggesting BL should be set to ~0.7V

## Slide 10: Tests of Daughter board 2
Daughter board 2
200 Ohm/cm
Matrix 1
Matrix 2
No bias
Bias -10V
No bias
Bias -10V
Test:
bias voltage: -10V
BL=0.7V (868)
Threshold sweeping
Observations
Tails at both Matrix
Threshold at which each matrix starting to see some hits moved to the left(but still has reasonable shape)

## Slide 11: Tests of Daughter board 2
Daughter board 2
200 Ohm/cm
Tests:
Bias voltage: -10V
BL= 0.4V, 0.6V, 0.8V, 1.0V, 1.2V
Threshold sweeping: BL±0.2V
Matrix 1 BL
Matrix 2 BL

## Slide 12: Summary and Next
Summary
Daughter board 1:
  Could be biased but large leakage current and has 2nd step
  Matrix 2 has hot pixel: (127,31)
    Cannot be disabled and will block other pixels from reporting hits
  Matrix 1 looks fine for now
Daughter board 2:
  Could be biased but large leakage current and has 2nd step
  Matrix 1 and 2 both have hits reported.
Next:
  One more board to test