## Slide 1: There and Back Again
LC from an European XFEL perspective
(With many stolen slides from N. Walker, O. Napoly, M. Omet, S. Michizono, A. Grassellino)
Marc Wenskat (UHH)
LC Forum @ 13th „Physics at the Terascale“ Meeting

## Slide 2: Why LC at all?
We could argue where the cross-over point is – but it is there
Future for e+e- is linear

## Slide 3: Evolution of Linearcollider Ideas
1994
Technology Review
Comittee (TRC) I
CLIC (CERN) 30GHz
TESLA (DESY) 1.3GHz
SBLC (DESY) 3.0GHz
JLC-S (KEK) 2.8GHz
JLC-C (KEK) 5.7GHz
JLC-X (KEK) 11.4GHz
NLC (SLAC) 11.4GHz
VLEP (IHEP) 14GHz
CLIC (CERN) 30GHz
TESLA (DESY) 1.3GHz
JLC-C (KEK) 5.7GHz
JLC-X (KEK) 11.4GHz
NLC (SLAC) 11.4GHz
2003
TRC II
CLIC (CERN) 12GHz
TESLA (DESY) 1.3GHz
JLC-X (KEK)
NLC (SLAC) 11.4GHz
2003
International Technology
Review Panel
2005
ILC (GDE) 1.3GHz
CLIC (CERN) 12GHz

## Slide 4: Tesla Technologie
R&D Goal in the 1990s: reduction $/MeV by a factor of 20!
  Factor 5 in Gradient 5 to 25 MV/m
  Factor 4 from cryomodule fabrication
Optimized for
  Low-Loss operation
  Emittance preservation
  RF power generation
And the Adventure for High Gradients and Low Losses

## Slide 5: Tesla Technologie

## Slide 6: Why SRF
“The construction of the superconducting XFEL free electron laser will provide prototypes and test many aspects of the linac.”
ITRP final report summary

## Slide 7: European XFEL
A „Sandbox-ILC“ ?

## Slide 8: EXFEL Fabrication Results

## Slide 9: EXFEL Fabrication Results

## Slide 10: EXFEL Fabrication Results

## Slide 11: EXFEL Fabrication Results

## Slide 12: Operation of EXFEL
Incl. Installation in module, impact of waveguide system
Avg. Gradient is 23 MV/m
If all cavities in the RF station operate at 29 MV/m

## Slide 13: From EXFEL to ILC
Cavity Specs
ILC TDR assumed ±20% gradient spread (28 ≤ G ≤ 42 MV/m)
How close are we?
 | ILC |  | XFEL | 
 | G [MV/m] | Q0 | G [MV/m] | Q0
Vertical Test | 35 | 5x109 | 26 | 1010
Installed | 31.5 | 1010 | 23.6 | 1010
 | Yield ≥28MV/m | ‹G›≥28MV/m
As received (1st Pass) | 75% | 35MV/m
After 25% retreated (2nd Pass) | 90% | 35MV/m
This is usable gradient!

## Slide 14: Test results per Vendor (max. G)

## Slide 15: Retreatment Model
Thanks to Nick Walker

## Slide 16: Extrapolation to ILC-VT

## Slide 17: SRF cost reduction R&D
How much can we safe?

## Slide 18: General R&D
[Reschke et al., Phys. Rev. Accel. Beams, 20, 042004 (2017)]
[Grassellino et al., SUST, 26, 102001 (2013) ]
[Grassellino et al., SUST, 30, 094004 (2017) ]
[Grassellino et al., arxiv 1806.09824]
Standard Cavity
Doped Cavity
Infused Cavity
Low-T Baked Cavity
Cavities limited by quench

## Slide 19: Cavity Fabrication Process
Only modifies recipe
Is industrialized (LCLSII)
No high gradients (LCLS-HE)
Changes recipe (less steps)
Not every lab succeeds
Recipe not fully understood
Only modifies recipe
Shows strong dependency
on cooldown procedure

## Slide 20: Summary
It’s been a long road…
  TESLA technology is now mature and industrialized
  almost ‘off the shelf’ (see LCLS-II)
Performance is very close to ILC requirements
  But not the cost!
  Larger scale industrialization will help if planned correctly
New SRF ‘breakthroughs’ may bring significant cost benefits
  higher gradients, higher quality factors
  but it’s industrial yield that matters

## Slide 21: Thanks for Listening!
Questions?

## Slide 22: Cavity & Cryomodule Fabrication
AMTF @ DESY
  Cavities
    Vertical Tests
    2 independen cryostats
    6 inserts, 4 cavities each
    3 days per Tests
    Plan: 8 cavities per week
  Modules
    3 parallel test benches
    Original plan 21 days
    Optimized down to 14 days
    1 module finished per week

## Slide 23: Comparison VT to module

## Slide 24: Comparison VT to module

## Slide 25: Degradation

## Slide 28: The Recipe
Time [h]
Temperature [°C]
Pressure [mbar]
N-Doping: Change of baking procedure
+ 5-10 μm removal of inner layer by chemical etching necessary
N2
800°C

## Slide 29: The Recipe
No chemistry needed
Time [h]
Temperature [°C]
Pressure [mbar]
N-Infusion
N2
800°C
120°C
Problem: No one cooks like Grandma

## Slide 30: How is the performance affected?
Model can explain Q0 increase but not difference between Doping & Infusion
Q0(E) dependency change
Effect has not been seen in low mfp cavities
Difference in Quenchfield
+
Quench field does not increase/reset with more inner surface removal!

## Slide 31: Cavity-Tests
10.4 tests per week
Peak: 15 tests per week
1.48 tests per cavity
  (1.2 assumed)

## Slide 32: Tesla Technologie
Control of niobium material (high purity)
Mechanical construction in a clean environment
  electron-beam welding (EBW)
Preparing RF (inner) surface ultra-clean mirror surface
  electro-polishing (EP)
Removing hydrogen from the surface layer
  800° C bake
Removing surface contamination
  alcohol and/or detergent rinsing
  100-150 bar high-pressure rinsing (HPR)
And the Adventure for High Gradients and Low Losses

## Slide 33: Module Assembly Rate

## Slide 34: Why SRF?
Low-Loss cavities
  High RF → Beam-power efficiency
  Lower operational costs
„Simple“ RF power generation
  1.3 GHz relative low f – standard components
  Long pulses / fill time (1ms/0.6ms)
  Low peak power
Emittance preservation
  Large cavity iris (low f)
  Low transverse / longitudinal wakefields
  Loose alignment tolerances