## Slide 1
The Next Generation
Material Structures
for
SRF Technologies
M. Eng. A. Özdem Sezgin, Dr. –Ing. Michael Vogel
Prof. Dr. rer. nat. habil. Xin Jiang
LOT
Fak. IV, Department Maschinenbau
University of Siegen
14.02.2020
Hamburg
SIS Multilayer Structures for Applications in SRF Technology (SMART)

## Slide 2
Project
KEY CHALLENGES | 
Materials: | Stoichiometric films with low defect density for high crystalline quality.
Coating Processes: | Up-scaling capacity.
Optimization studies to determine feasible deposition parameters: Cathode Power, Gas pressure, Target/substrate materials, Substrate temperature, Substrate bias, Process gas.
Systematic investigations of surface properties of novel materials – formed by coating of mono- or multi-layers of varying: Composition (e.g., Nb, Nb(Ti)N, Nb3Sn, AlN, etc.) Thickness (multilayer S-I-S).

## Slide 3
Initial Objectives
Witness samples (Si – Nb, NbN ) for initial studies of Stoichiometry, Crystallography, ((Morphology)).
Obtaining high-quality thin films (TFs) by controling the TF structures through: * TF Thickness, * TF Composition, * TF Uniformity.

## Slide 4
CC800 - DCMS
Materials & Infrastructures
Al2O3
Goodfellow
(60*60*1mm3)
Purity: 99.6%
Al2O3
Goodfellow
(25*25*0.1mm3)
Purity: 96%
ALD –Al2O3
(44nm) / Si<100>
Wf ~ Hamburg
Cleaved
Wf
Coated
substrates
Nb
NbN
Target: Nb (RRR300)
(100*88*10mm3)

## Slide 5
Experiments
Process | Substrate Temperature T [oC] | Process Gas Pressure p[mPa] | Process Gas | Process Gas Mass Flow Rate [sccm] | Cathode Power [W] | Substrate Bias [V] | Coating Time tc [min]
1. 964 | 650 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
2. 970 | 200 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
3. 973 | 200 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
4. 975 | 400 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
5. 977 | 200 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
6. 980 | 650 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
7. 990 | 715 | 1200 | Ar / N2 | 500 / 43 | 400 | 0 | 30
8. 994 | 715 | 1200 | Ar / N2 | 500 / 43 | 60 | 0 | 240
9. 1012 | 200 | 1200 | Ar / N2 | 500 / 42 | 60 | 0 | 240
10. 1010 | 400 | 1200 | Ar / N2 | 500 / 43 | 60 | 0 | 240
11. 1013 | 200 | 1200 | Ar / N2 | 500 / 43 | 60 | 50 | 240
12. 1014 | 400 | 1200 | Ar / N2 | 500 / 43 | 60 | 50 | 240

## Slide 6
Material Characterizations
XRD | Phase analysis
SEM / EDX | Thickness Composition

## Slide 7
Results
Cross section (CS) - ALD-Al2O3-Si
Thickness (Th)=44.67nm

## Slide 8
DC-NbN
T200-400W-0V
977
NbN
Al2O3
Si
Al2O3
NbN
SEM – CS Images

## Slide 9
975
EDX – CS Analysis

## Slide 10
977 – T200
980 – T650
975 – T400
SEM – Surface (S)

## Slide 11
DC-NbN-T650-400W-0V
A. Özdem Sezgin, 12.02.2020
980
SEM / EDX

## Slide 12
T  Thickness
T=200 [oC]
T=400 [oC]
T=650 [oC]
Th=1.315 μm
Th=1.226 μm
Th=1.170 μm
977
975
980
SEM – Thickness Analysis

## Slide 13
Si (100)
XRD
  NbN
  Superconducting NbN Phases:
  phase ()
  ( =12 – 15 K )
  phase ()
  ( = 15 – 17.3 K)
  phase ~ 11.6 K)
Nb4N3(111)

## Slide 14
Future Work
Further elaboration of the thin films with various materials characterization techniques (e.g.,TEM, AFM, STM, SIMS, etc.), Working on Nb substrates - provided by Hamburg team, Target geometry and composition screening (e.g., NbxSny, Nb target with Sn plugs, Nb and Sn individual targets), Utilizing different PVD methods (DCMS, RFMS, HiPIMS), Multilayered TF studies - incorporating insulating layer (e.g., AlN) (to pave the way to SIS structures).

## Slide 15
Acknowledgements
Apart from the invaluable guidance and on point constant feedback from my supervisors, I do appreciate each and every member of LOT for their extensive support. I also would like to acknowledge my colleague Stewart Leith for fruitful discussions and the exchange of information along with Thorsten Staedler, Petra auf dem Brinke from LOT and Markus Hartmann from LWF for AFM, SEM / EDX and XRD measurement introductions, respectively.

## Slide 16
THANK YOU
FOR
YOUR ATTENTION !