## Slide 1: Grain boundary segregation and precipitation of carbides in heat treated Nb cavity cutouts and samples
MML
From Matter to
Materials and Life
Arti Dangwal Pandey - on behalf of SRF R&D team and Nano lab at DESY
TTC 2021, TESLA Technology Collaboration

## Slide 2
800 °C /3 hrs + EP + 120 ° C /48 hrs
+ 800 °C /3 hrs + 120 ° C /48 hrs
+ 800 °C /3 hrs + 120 ° C /48 hrs
M. Wenskat et al, SUST 33, 115017 (2020)
T-maps @ 1.5 K
Reasons behind Q-degradation?
Infusion attempts with/ without nitrogen on fine grain Nb cavities
800 °C /3 hrs + 120 ° C /48 hrs
1DE16
Schmitz et al, Review of Scientific Instruments 89, 54706 (2018)

## Slide 3
Quench spot
Cold spot
Nb2C
Cavity cutouts: Carbide Precipitates overall
SEM, X-ray photo electron Spectroscopy (XPS): Nb2C additional phase
XPS: Nb3d
Cold spot
Quench spot
Hot spot
Increased agglomeration of precipitates at grain boundaries

## Slide 4
Nb Nb2C
Grain boundary segregation: Nb grain decoupling
SEM, electron backscatter diffraction (EBSD), and Focused ion beam (FIB) milled cross sections
Nb Nb2C
Bonin & Safa (1991) Supercond. Sci. Technol. 4 257
cold spots
Quench-spot
FIB Cross-section view
Depth of carbides into Nb >> RF penetration depth
Decouples the Nb grains within RF layer
Enormous Q-degradation as seen in granular thin films on cavities/ Ti contaminated Nb cavities
Pt layer
ANTOINE C, et al., Proceedings of the 1997 Workshop on RF Superconductivity,
Abano Terme (Padova), Italy
A. Grassellino et al., arXiv (2013), arXiv:1305.2182

## Slide 5: Comparison to a successful N-infusion treatment
SEM + Electron backscatter diffraction (EBSD)
(111)
(111)
(001)
- much less ‚C‘ segregation at few grain boundaries
~100 nm
Carbides were also reported by FNAL already
[A. Grassellino etal. In “Unprecedented quality factors at accelerating gradients up to 45 MVm^-1 in niobium superconducting resonators via low temperature N infusion”]
GB Segregated carbides width
>200 nm @ cold spot; 500 nm @ quench spot
of 1DE16
Nb sample N- infused with 1DE20 at FNAL
Notes: I quote: " Further studies will be performed on the origin of these precipitates, but preliminary XRD results indicate they are niobium carbides. The origin of these carbides is currently under investigation, but it is expected to affect negatively cavity performance."

## Slide 6: Carbide growth dependence on Nb orientation
SEM + Electron backscatter diffraction (EBSD)
α-Nb2C (orthorhombic)
Precipitates
Nb(111)
Nb (bcc)
More segregation at higher index plane side
Grain boundary segregation
Size and shape changes with Nb grain orientation

## Slide 7
Grain-size distribution
electron back scattered diffraction (EBSD)
High Q , high Eacc after : 800 °C /3 hrs + 40 µm EP + 120 ° C /48 hrs
Quench spot
Av. size < 30 µm
Av. size ~ 40 µm
Cold spot

## Slide 8: Misorientation angle (θ) distribution
Low-angle grain boundaries with high dislocation density
bcc Fe – C system
In quench spots: Excess of low-angle grain boundaries at higher θ (up to 14̊)
Low angle grain boundaries
Dislocation density increases with θ for low-angle grain boundaries

## Slide 9
Nb2C precipitates and grain boundary segregation observed on cavity cut-outs as well as Nb samples heated up to 800 C (incl. successful N-inf)
- Dimensions decided by C content in furnace ambient and cavity surface
Q-degradations due to
  - For high ‘C’ contamination: enormous GB segregation and precipitation of carbides of large dimensions (~0.5 µm) occur. Carbides penetrating into the GBs result in to Nb grains decoupling, and hence, lead to anamolous Q-losses starting at low Eacc
  - Nb2C as surface defects might result ohmic losses and hence, a quench at a reduced Eacc
  - Excess of low angle grain boundaries in high theta regime, with abundance of very small grains facilitates early flux penetration and hence a quench at a reduced Eacc
Summary:

## Slide 10: C-segregation, low angle grain boundaries => Q-degradation
C excess, Q-loss, and misorientation angles distribution
Cold spot Hot spot Quench spot
Excess of carbides at grain boundaries/ precipitates : higher losses in cavities
Excess of low-angle grain boundaries

## Slide 11: Acknowledgements
Colleagues at FNALfor N-infusion of samples and cavity
HZB
BEEM (electron microscopy) group at TUHH
DESY Nanolab team and MSL/MPL group at DESY
Thank you very much for your attention!