## Slide 1
Reducing the impact of radioactivity on quantum circuits in a deep-underground facility
Francesco Valenti, Laura Cardani et al.
arXiv:2005.02286 (submitted to Nature Communications)
500 mt

## Slide 2: Superconducting quantum circuits
• Supercurrent carriers: Cooper pairs (CP), e- bound by phonons with binding energy Δ
e- --- e- + 2Δ = 2 QP (quasiparticles)

## Slide 3: Superconducting quantum circuits
• Supercurrent carriers: Cooper pairs (CP), e- bound by phonons with binding energy Δ
• Simplest circuit: LC resonator
C
L
This work:
Inductive loss ≫ capacitive loss
e- --- e- + 2Δ = 2 QP (quasiparticles)
RQP

## Slide 4: Superconducting quantum circuits
• Supercurrent carriers: Cooper pairs (CP), e- bound by phonons with binding energy Δ
• Simplest circuit: LC resonator
C
L
Qi-1 = ω0RQPC
This work:
Inductive loss ≫ capacitive loss
e- --- e- + 2Δ = 2 QP (quasiparticles)
RQP

## Slide 5: Superconducting quantum circuits
• Supercurrent carriers: Cooper pairs (CP), e- bound by phonons with binding energy Δ
• Simplest circuit: LC resonator
C
L
Qi-1 = ω0RQPC
L≈Lkinetic (NQP)
⇒ ω0-2 = L(NQP)C
RQP
This work:
Inductive loss ≫ capacitive loss
e- --- e- + 2Δ = 2 QP (quasiparticles)

## Slide 6: Quasiparticles in SC circuits
• Static effect: Qi decreases (f0 shifts)
Lévy-Bertrand et al., arXiv:2010.03845
Higher blackbody T: more broken CPs
 more QPs
Fingerprint: Qi

## Slide 7: Quasiparticles in SC circuits
• Static effect: Qi decreases (f0 shifts)
• Dynamic effect: f0 jitters, or even drops
Lévy-Bertrand et al., arXiv:2010.03845
Higher blackbody T: more broken CPs
 more QPs
Fingerprint: Qi
Fingerprints:
Drop count
(coarse)
Jitter spectrum
(fine)
Grünhaupt et al., PRL 121, 117001 (2018)

## Slide 8: QPs: where from?
• Tc~1 K, T of operation ~10 mK  NOT thermal!

## Slide 9: QPs: where from?
• Tc~1 K, T of operation ~10 mK  NOT thermal!
• Possible source:
radiation generating phonons in the substrate
hν ≫ 2Δ
substrate
C
L
«QP burst»

## Slide 10: QPs: where from?
• Tc~1 K, T of operation ~10 mK  NOT thermal!
• Possible source:
radiation generating phonons in the substrate
Adapted from:
Karatsu et al., APL 114,032601 (2019)
• Implies time-correlated drops for same-chip resonators
hν ≫ 2Δ
Resonator #
substrate
C
L
«QP burst»

## Slide 11: QP abatement
hν ≫ 2Δ
substrate
C
L
«QP burst»

## Slide 12: QP abatement
Reducing phonons:
-Karatsu et al., APL 114,032601 (2019)
-Valenti et al.,
PRApp 11,054087 (2019).
-Valenti, Henriques et al.,
APL 115,212601 (2019).
hν ≫ 2Δ
substrate
C
L
«QP burst»

## Slide 13: QP abatement
Reducing radiation:
This work!
Reducing phonons:
-Karatsu et al., APL 114,032601 (2019)
-Valenti et al.,
PRApp 11,054087 (2019).
-Valenti, Henriques et al.,
APL 115,212601 (2019).
substrate
C
L
«QP burst»
hν ≫ 2Δ

## Slide 14: Radiation: where from?
• What I thought «radioactive contamination» looks like:

## Slide 15: Radiation: where from?
• What I thought «radioactive contamination» looks like:
• What it also looks like:
Solder
Unetched
copper
Unshielded
cryostat
(In an above ground lab)
«Near sources»
«Far sources»
Silver paste

## Slide 16: Radiation: where from?
• What I thought «radioactive contamination» looks like:
• What it also looks like:
Solder
Unetched
copper
Unshielded
cryostat
(In an above ground lab)
«Near sources»
«Far sources»
Silver paste

## Slide 17: How to protect from…
Laboratori Nazionali del Gran Sasso, Italy
Near sources:
Acid cleaning
Far sources:
Deep-undeground facility

## Slide 18: Radiation abatement: setups
Far sources
abatement

## Slide 19: Radiation abatement: setups
Near sources
abatement
Far sources
abatement

## Slide 20: Radiation abatement: setups
Near sources
abatement
Near and far sources
abatement

## Slide 21: Radiation abatement: results
QP burst rate (mHz)
Internal quality factor at single photon
K : control
R : cleaned
G : cleaned and shielded
Arrows: chronology

## Slide 22: Radiation abatement: results
QP burst rate (mHz)
Internal quality factor at single photon
K : control
R : cleaned
G : cleaned and shielded
Arrows: chronology

## Slide 23: Radiation abatement: results
QP burst rate (mHz)
Internal quality factor at single photon

## Slide 24: Summary
Superconducting circuits degraded by quasiparticles
Radioactivity is a source of quasiparticles
Radioactivity abatement improves the performance of superconducting circuits

## Slide 25
Thank you for your attention!