## Slide 1: RRR measurements of niobium samples after vacuum heat treatments with and without nitrogen
8. Annual MT Meeting
Christopher Bate
DESY MSL
Universität Hamburg - Institut für Experimentalphysik
Hamburg, 26.09.2022

## Slide 2: RF superconductivity
Niobium as material of choice for SRF cavities
EuCARD-BOO-2012-001 Editorial Series on.” (2012).
Type II superconductor with
Used worldwide from colliders to light sources
Affordable continuous wave and long pulse at high gradients
  Field(acceleration) can be ON all the time
Steady progress in advancement of this technology
  Lately with some important breakthroughs
EU-XFEL

## Slide 3: RF superconductivity
Standard cavity
N doped cavity
N infused cavity
Mid-T baked cavity
cavities limited by quench
TESLA shaped cavity figure of merit
Nitrogen Infusion as the main focus for my research
Increase less required power
Increase decrease accelerator length
EuCARD-BOO-2012-001 Editorial Series on.” (2012).
Critical magnetic field for Nb

## Slide 4: RF superconductivity is a surface phenomenon
RF fields
Niobium
~3 mm
Helium cooling
RF only probes the penetration depth (λL = 47 nm) of the material
→Final surface treatment is crucial to performance!
Oxide layers
RF fields
RF currents <100 nm
<1% thickness

## Slide 5: Nitrogen surface treatments
Cavities are processed in ultra-high-vacuum furnaces
https://td.fnal.gov/srf-capabilities/

## Slide 6: Nitrogen Infusion
A recipe developed at Fermilab
Supercond. Sci. Technol. 30 094004 (2017)
800°C – 3 hours in vacuum
(base pressure ~ mbar)
mbar N2
at 120°C for 48 hours
No further steps needed!
@800°C
HFQS
x2
Low reproducibility at other labs
Underlying mechanism?
  Nitrogen?
  O, H, C Interstitials?
Nitrogen
?
N,O,H,C

## Slide 7: RRR measurements on samples
Residual Resistivity Ratio (RRR) - Resistive measurement
Proportional to thermal conductivity
  or better established in SRF community
Sensitive to changes in impurities (e.g. diffusion during cavity treatments)
  Scales linearly with impurity concentration
The is a function of the electron mean free path
  minimum can be found at
Is the Nitrogen Infusion influencing the at the surface?
  investigations on nitrogen infused samples
DC measurement selected to investigate the influence of Nitrogen Infusion on fine-grain samples
Pramana 93 (2019) 3, 51 DOI: 10.1007/s12043-019-1813-4
Nb sample
Heater

## Slide 8: RRR measurements on samples
Total of 10 samples measured
All samples received a 800°C baking and a BCP before the baseline measurement
  800°C for 3h had no significant influence on
5 samples were subjected to a temperature treatment, but without nitrogen, i.e. under vacuum conditions
  800°C 3h 120°C-400°C 48h in vacuum
  Treatment without nitrogen can only change the RRR value via contamination or purification
5 sample were subjected to a Nitrogen Infusion in a temperature range between 120°C and 400°C
  400°C close to the temperature beyond which no nitrides are formed
  800°C 3h 120°C-400°C 48h with nitrogen
  Same processes as without nitrogen also take place in the presence of nitrogen
  In addition to the penetration of nitrogen into the surface
difference between initial and after gives information about
N,O,H,C
Impurities
800°C 3h
120°C-400°C 48h
in N
Nitrogen
Clean surface no visible preicipitates on fine-grain sample after 400°C N-Infusion

## Slide 9: RRR measurements on samples
Infusion T | 
400°C | 
330°C | 
260°C | 
160°C | 
120°C | 
Infusion T | 
400°C | 
330°C | 
260°C | 
160°C | 
120°C | 
Shown is
Deterioration in RRR for all temperatures was found irrespective of whether nitrogen was used or not
For temperatures above 260°C,
At 160°C and 120°C, no significant changes are observed
Tendency for to decrease with T above 260°C data insufficiently precise to establish this

## Slide 10: Thank you

## Slide 11: Backup

## Slide 12: RRR measurements on samples
Resistive measurement
Residual Resistivity Ratio − 𝑅𝑅𝑅 → Level of purity
DC measurement selected to investigate the influence of nitrogen Infusion on fine-grain samples
Nb sample
Heater

## Slide 13: Sample furnace
Residual gas analysis (RGA)
Final pressure: mbar