## Slide 1
200 channel sensors
21.09.2022
INFN Padova
Sergii Vasiukov
The sensor has been bonded in Pisa and arrived in Padova on 19 September 2022

## Slide 2
The results of a visual test of the condition of
the strips and contacts/bondings using an optical microscope
The all bindings look well.
A short circuit has been observed between strips number 33 and 34 (from the top of the board label)!
There is a lot of dust and lint on the detector surface.
The backside metallization has irregular thickness.

## Slide 3
Front view
Back side

## Slide 4
Front view (back illumination)
Back side (back illumination)

## Slide 5
Sapphire - Front view
Output wires and strips bonding

## Slide 6
Front view (back illumination)

## Slide 7
Plugs and electric elements