## Slide 1: The 192Ch-GBP-W under X-ray
25.10.2022
INFN Padova
Sergii Vasiukov

## Slide 2
X-ray tube (tungsten): U=40kV; I=50mA (continuous mode)
X-ray | Channels output (mean value) | std
OFF | 200uV | ~ 100 uV
ON | 1 – 10 mV | ~ 500 uV
Feature of the measurements:
Inertia
Humidity sensitivity
Inertia:
The monitor current gradually decreases after turning on the X-ray radiation from 0.5 to 0.41 µA at a bias voltage of 500V.
Humidity influence (No X-ray):
Humidity | Current monitor
< 60% (No rain) | 1.1 – 2.1 nA
> 80% (Rain) | 5 – 10 nA
Testing in progress now…