## Slide 1: Status SCARPIA
[Wenskat et al., Physical Review B 106.9 (2022): 094516]
Discussion ongoing with U Mainz – first tests planned Q1’23
Studies ongoing @ U Rostock – good collaboration in “QPR community”
Swapped Method – Study ongoing, preliminary results published
QPR:
Talking about it since 2018.
First cooldown on Monday!

## Slide 2
Effect of cavity treatments on niobium oxide layers
Rezvan Ghanbari, on behalf of SRF R&D Team
02.12.2022

## Slide 3
~5 nm
+ O,N,H,C
Interstitials
Nb oxides, nitrides, hydrides
Vacancies
Grain boundaries
N-doping
N-Infusion
120C-baking
Mid-T
Rezvan Ghanbari
TOSCA meeting 02.12.2022
~200 nm
What is the role of oxide layers on the performance of cavities?
Surface analysis of several samples which is treated at DESY
include first set of Mid-T treated samples which is done with cavities at Zanon Research & Innovation Srl
Mid-T studies should achieve:
RBCS ≤ 6 nΩ
Anti-Q slope below 16MeV : dQ0/dEacc > 0
Rres ≤ 2 nΩ
which is defined by Mid-T studies at FNAL (In-situ) and IHEP and KEK (modified recipes in furnaces & with caps)
[Ito, H., et al. Prog. Theor. Exp. Phys. 2015 (2021).]
[Zhou, Q., et al. Radiat. Detect. Technol. Methods 4.4 (2020): 507-512.]
[Posen, S., et al. Phys. Rev. Appl. 13.1 (2020): 014024.]
L. Steder, et al., Medium Temperature treatments of superconductingradio frequency cavities at DESY, THPOGE 22

## Slide 4
Anti-Q-slope seen but improvement “masked” by increased Rres
1DE9 has lowest Rres
Cavity 1DE9
Cavity 1DE7
Cavity 1DE5
Cavity 1AC2
120°C
Sample Niob 1
300°C
Caps
Sample Niob 2
Sample Niob 4
Caps
is very different ()
1AC2 has significant increase in Rres
Sample Niob 3
RBCS ≤ 6 nΩ
Rres ≤ 2 nΩ
Anti-Q slope
dRs/dEacc < 0
Rezvan Ghanbari
TOSCA meeting 02.12.2022

## Slide 5
Pentoxide layer thickness reduces due to Mid-T treatment
Pentoxide layer thicknesses:
Niob 2 << Niob 4 ≈ Niob 5
NbxO layer thicknesses:
Niob 2 > Niob 4 > Niob 5
baking before Mid-T mitigates pentoxide layer reduction
1DE9 performed better than 1DE5
less pentoxide means lower Rres ?
X-Ray Photoelectron Spectroscopy
Etching depth
Nb2O5
NbxO
NbO
Nb0
Cavity 1DE9
Niob 2
Niob 4
Niob 5
Cavity 1DE5
Reference
Rezvan Ghanbari
TOSCA meeting 02.12.2022

## Slide 6
Oxide layer shows surface magnetism
sensitive to magnetic fields within first 15nm
Different treatments, different Remanence magnetization
Kerr microscopy & MOKE magnetometry
Magneto-orbital Kerr effect
Faraday Effect Magnetic Cyrcular Dichroism
Imaging
Remanence Curves
[Technische Universität Chemnitz, Physik, OHL, vl_sc/VL10.pdf]
Niob 1
Niob 6
Niob 7
Niob 8
Niob 9
100
Magnetic field: 201,73 mT
Niob 1
Cavity 1AC2
Magnetic domains form in oxide layers
Rezvan Ghanbari
TOSCA meeting 02.12.2022

## Slide 7
Oxide layer shows surface magnetism
6
1
8
7
9
Niob 6: baking (Reference)
1st assumption: A thin N-monolayer is formed as a substrate for pentoxide regrowth
[Zhussupbekov, K., et al. SciRep 10 (2020): 3794]
[Esquinazi, P., et al. IEEE Trans. Mag. 49.8 (2013): 4668-4674]
2nd assumption: N-infusion reduce H-concentration near the surface -> weaker coupled magnetic impurities
Niob 1: Mid-T treatment (baked with cavity 1AC2 at )
Higher remanence seen – fits to increase in of 1AC2 after anneal
Niob 8: Accidental baking at 10-4 mbar and
Known from literature: pentoxide grows instead of dissolving
Niob 7 & 9: N-Infusion treatment -> Significant decrease of magnetization. Why?
Rezvan Ghanbari
TOSCA meeting 02.12.2022

## Slide 8
Extensive high pressure rinsing (HPR) grows thicker Nb2O5
Thickness of pentoxide layer:
Niob 10 < Niob 11 << Niob 12
depends on amount of HPR cycles
Course EP
Baking, 800C, 3h
Fine EP
XPS measurements
Store under high pure ethanol
Reference
0 time HPR
Niob 10
Standard recipe
6 times HPR
Niob 11
18 times HPR Niob 12
Store under high pure ethanol
Mid-T treatments
SIMS measurement
Store in air
Interstitial oxygen concentration after Mid-T annealing could depend on amount of HPR cycles
Penetrate up to 5nm
207.6 eV
Pentoxide binding energy
[Dangwal Pandey, Arti, et al. Journal of materials science 53.14 (2018): 10411-10422]
Niob 10
Niob 11
Niob 12
X-Ray Photoelectron Spectroscopy
Rezvan Ghanbari
TOSCA meeting 02.12.2022

## Slide 9
Key insights
Pentoxide layer thicknesses reduce with Mid-T treatment
Magnetic domains observed in oxide layers
Increase amount of high pressure rinsing cycles -> increase the thickness of pentoxide layer
The higher remanence magnetization correlates to higher and not optimal residual resistance
Rezvan Ghanbari
TOSCA meeting 02.12.2022

## Slide 10
Thank you for your attention !
Dr. Marc Wenskat
marc.wenskat@desy.de
Rezvan Ghanbari
rezvan.ghanbari@desy.de
Contacts at the meeting
M. Aeschlimann (TUKL), C. Backes (TUKL), C. Bate, G. Deyu, A. Ermakov, M. Kohantorabi, N. Krupka, H. Noei, A. Dangwal Pandey, D. Reschke, N. Schäfer (TUDA), M. Stahl (TUKL), L. Steder, M. Wiencek, …
We would like to thank
Prof. Wolfgang Hillert
Wolfgang.hillert@desy.de
Rezvan Ghanbari
TOSCA meeting 02.12.2022