## Slide 1: Radiation tolerance of MIMOSIS-1
M. Deveaux on behalf of the
IPHC-IKF-GSI (CBM-MVD) Collaboration
(05P19RFFC1)
Supported by

## Slide 2: The CBM Micro Vertex Detector (MVD)
CBM
CBM-MVD
The CBM – MVD will operate at:
100 kHz Au+Au collisions (10 MHz beam)
Beam hole: 11mm
3rd High-D consortium meeting, 9-10 Feb. 2023
M. Deveaux

## Slide 3
CBM-MVD Sensor requirements
How to arrive there (starting from ALPIDE) based on 180 nm technology?
 | Requirement
Time resolution | ~5 µs
Spatial resolution | ~5 µm
Sensor thickness | ~50 µm
Power dissipation | 200 mW/cm²
Radiation doses (non-ionizing) | > 7x1013 neq/cm²
Radiation doses (ionizing) | > 5 Mrad
Radiation gradient on chip | 100%
HI-tolerance | 10 Hz/mm²
Rate (average/peak) | 150/700 kHz/mm²
 | Requirement
Time resolution | ~5 µs
Spatial resolution | ~5 µm
Sensor thickness | ~50 µm
Power dissipation | 
Radiation doses (non-ionizing) | > 7x1013 neq/cm²
Radiation doses (ionizing) | > 5 Mrad
Radiation gradient on chip | 100%
HI-tolerance | 10 Hz/mm²
Rate (average/peak) | 150/700 kHz/mm²
3rd High-D consortium meeting, 9-10 Feb. 2023
Mostly established by ALPIDE
(Sensor of ALICE ITS2 upgrade)
Incompatible with ALPIDE
> 20x internal bandwidth needed
per year
no safety factor
10 x ALPIDE

## Slide 4: MIMOSIS R&D plan
MIMOSIS-0 (2018)
Demonstrate pixel concept.
Demonstrate zero suppression.
Demonstrate readout concept.
MIMOSIS-1 (2020)
Full dimension sensor
Add buffer structure.
SEE hardening 1/2
MIMOSIS-2 (Q2/2023)
On-chip pixel grouping.
Final pixels.
SEE hardening 2/2
All submissions:
Additional CE18 test structures to study specific design questions.
MIMOSIS-1, 60µm thick
We are here
MIMOSIS-1
Commisioning during 2020 lock-down
MIMOSIS-3
Final sensor for mass production
In synergy with:
3rd High-D consortium meeting, 9-10 Feb. 2023

## Slide 5: MIMOSIS-1
Size: 504 x 1024 pixels (3 cm x 13mm active)
Full set of data concentration buffers.
Pixels types: 2x DC, 2x AC (>20V depletion voltage)
MIMOSIS-1, 60µm thick
p-stop
n-gap
standard
Standard
Rad. hard, candidate 1
Rad. hard, candidate 2
First proposed by W. Snoeys et al.
H. Pernegger et al., 2017 JINST 12 P06008
A
B
C
D
AC-pixel
>20V HV top bias
Decoupling capacitor
Back bias possible.
P-Well bias (ALPIDE) possible
Most likely Fully Depleted
3rd High-D consortium meeting, 9-10 Feb. 2023

## Slide 6: Beam tests (MIMOSIS-1)
Date | Location | Beam | Goal
13. – 14. Mar 2021 | GSI / mCBM | 1 AGeV Pb | Single-Event-Effects (SEE)
23. – 24. May 2021 | GSI / mCBM | 1 AGeV Xe | SEE
07. – 13. Jun 2021 | DESY | 5 GeV e- | Performance
19. – 26. Sep 2021 | DESY | 5 GeV e- | Performance (X-ray irradiated)
05. – 12. Oct 2021 | CERN | ~100 GeV | Performance (neutron irradiated)
14. – 20. Feb 2022 | DESY | 5 GeV e- | Performance (mixed irradiated) ++
21. – 28. Mar 2022 | COSY | 0.3 – 3 GeV p | Performance, dE/dx?
23. – 29. May 2022 | GSI/UNILAC | ~4 MeV Ca | SEE, slow fragments
01. – 07. Sep 2022 | CERN | ~100 GeV | Response to inclined tracks,…
Date | Location | Beam | Goal
13. – 14. Mar 2021 | GSI / mCBM | 1 AGeV Pb | Single-Event-Effects (SEE)
23. – 24. May 2021 | GSI / mCBM | 1 AGeV Xe | SEE
07. – 13. Jun 2021 | DESY | 5 GeV e- | Performance
19. – 26. Sep 2021 | DESY | 5 GeV e- | Performance (X-ray irradiated)
05. – 12. Oct 2021 | CERN |  | Performance (neutron irradiated)
14. – 20. Feb 2022 | DESY | 5 GeV e- | Performance (mixed irradiated) ++
21. – 28. Mar 2022 | COSY | 0.3 – 3 GeV p | Performance, dE/dx?
23. – 29. May 2022 | GSI/UNILAC | ~4 MeV Ca | SEE, slow fragments
01. – 07. Sep 2022 | CERN |  | Response to inclined tracks,…
Date | Location | Radiation
Jul – Aug 2021 | Ljubjana (TRIGA) | ~1 MeV reactor neutrons
Sep 2021 | Karlsruhe (KIT) | ~10 keV X-rays
Aug 2022 | Karlsruhe (KIT) | ~10 keV X-rays
Special thanks to IPHC for massive support in beam time preparation.
Meanwhile: 14 IPHC people (9-10 FTE) involved in MIMOSIS.
Irradiation campaigns:
Shielding for PCB-ICs
(X-rays @ KIT)

## Slide 7
MIMOSIS-1 beam test setup
MIMOSIS-1 beam telescope:
6 MIMOSIS-1 sensors
4 reference sensors (standard epi-layer)
2 device under test
Reference Track Uncertainty:
  2.5 µm + 1.5 µm Mult. Scattering (DESY only)
Irradiation:
1 MeV reactor neutrons (TRIGA, Ljubjana).
Storage at room temperature.
Beam test:
5 GeV e- Beam @ DESY
120 GeV Pion Beam @SPS-CERN
Stabilized room temperature
Scan over wide phase space:
  4 pixel flavours (only 2 shown)
  3 epi – flavours
  Various Vbb, VHV
preliminary
3rd High-D consortium meeting, 9-10 Feb. 2023

## Slide 8
Mimosis-1: Tolerance to non-ionizing radiation
Vbb=-3V
HV=10V
DC-pixels:
Standard epi-layer reaches limits.
Good performance for p-stop, n-gap.
AC-pixels:
Standard epi-layer reaches limits.
Excellent performance for p-stop.
n-gap worse than DC version
  Unexpected, to be followed up.
Preliminary
3rd High-D consortium meeting, 9-10 Feb. 2023
Vbb=-3V
Preliminary

## Slide 9
MIMOSIS-1: Tolerance to non-ionizing radiation
Vbb=-3V
HV=10V
1 hit/frame
<0.05% of all pixels masked
Observation:
Det eff. >> 99% for 1014 neq/cm².
Resonable performance after 3x 1014 neq/cm².
AC-pixel shows better efficiency (as expected).
Dark rate < 10-6 for all pixels tested.
  => Holds for DC-pixels (not shown).
  => Matches requirements.
Preliminary
Preliminary
3rd High-D consortium meeting, 9-10 Feb. 2023
Vbb=-3V
Preliminary

## Slide 10
MIMOSIS-1 spatial resolution
?
?
Preliminary
Preliminary
Observation:
Best resolution for standard epi.
  Larger charge sharing (measured, not shown).
Resolution mildly worse after irradiation.
  Bulk damage reduces cluster size.
Plots hold for small dimensions of pixel
  ~10 % worse resolution for long dimension (not shown).
Results for all pixels match CBM requirements at default 120 – 150 e threshold.
Note: Preliminary results
Still preliminary alignment.
  Fixing this may or may not eliminate outlayers
  (work in progress).
3rd High-D consortium meeting, 9-10 Feb. 2023
Approx. alignment
uncertainty.

## Slide 11
MIMOSIS-1: Tolerance to ionizing radiation
Observation:
Good detection efficiency also after ionizing doses.
Radiation seems to improve performance sometimes
  Radiation may modify pixel tuning (7 parameters)
  Probably room for improvement.
Dark rate stays below 10-7
No impact on spatial resolution within uncertainties
3rd High-D consortium meeting, 9-10 Feb. 2023
standard
p-stop
standard
p-stop

## Slide 12
Response to combined irradiation (5 MRad + 1014neq/cm²)
Mixed irradiation:
Efficiency (and dark rate) in CBM specs.
Spatial resolution is slightly deteriorated
(acceptable for CBM)
3rd High-D consortium meeting, 9-10 Feb. 2023

## Slide 13
Summary and conclusion
3rd High-D consortium meeting, 9-10 Feb. 2023
MIMOSIS-1 forms the first full size prototype of the MIMOSIS sensor for the CBM-MVD.
    5 µs / 5 µm time/spatial resolution.
    80 MHz/cm² peak rate.
MIMOSIS-1 irradiated with up to 3x1014 neq/cm² were tested in laboratory and in beam.
    >> 99% detection efficiency after 1014 neq/cm², 5 MRad and a combination of both
    ~99% detection efficiency after 3x1014 neq/cm² (p-stop, AC-pixel)
    <10-6 fake hit rate (after 1014 neq/cm², <0.05% of all pixels masked)
    ~5 µm spatial resolution before and after irradiation => Matches requirement.
    Results are preliminary: Few sensors tested, preliminary alignment.
MIMOSIS-1 matches the requirements of the CBM-MVD…
… and forms a mile-stone toward a sensor for higgs-factories.

## Slide 14: CBM-MVD collaboration members
Julio Andary1, Benedict Arnoldi-Meadows1, Ole Artz1, Jérôme Baudot2, Grégory Bertolone2, Auguste Besson2, Norbert Bialas1, Roma Bugiel2, Gilles Claus2, Claude Colledani2, Hasan Darwish1,2,3, Michael Deveaux1,3,6, Andrei Dorokhov2, Guy Dozière2, Ziad El Bitar2, Ingo Fröhlich1,3, Mathieu Goffe2, Benedict Gutsche1, Fabian Hebermehl1, Abdelkader Himmi2, Christine Hu-Guo2, Kimmo Jaaskelainen2, Oliver Michael Keller6, Michal Koziel1, Franz Matejcek1, Jan Michel1, Frédéric Morel2, Christian Müntz1, Hung Pham2, Christian Joachim Schmidt3, Stefan Schreiber1, Matthieu Specht2, Dennis Spicker1, Joachim Stroth1,3,4, Isabelle Valin2, Yue Zhao2, Roland Weirich1 and Marc Winter5 1Goethe-Universität Frankfurt, Germany 2Université de Strasbourg, CNRS, IPHC UMR 7178, Strasbourg, France 3GSI Helmholtzzentrum für Schwerionenforschung GmbH, Germany 4Helmholtz Forschungsakademie Hessen für FAIR, Germany 5IJCLab, UMR9012 – CNRS / Université Paris-Saclay / Université de Paris, France 6Facility for Antiproton and Ion Research in Europe GmbH,Germany
Supported by:
(05P21RFFC2)
3rd High-D consortium meeting, 9-10 Feb. 2023