## Slide 1: HTS Developments at KIT and GSI
Tiemo Winkler, GSI
on behalf of colleagues from KIT and GSI
10.10.2023
9th MT Days, KIT / Karlsruhe

## Slide 2: HTS compact undulator
λ = 13 mm
Vertical racetrack
Two different prototype coils
Vertical racetrack (VR)
Helical undulator (Hel.)
4 mm, non-insulated ReBCO tape
iron core
VR
Hel.
Up to ≈ 300% Ic at LN2
Up to ≈ 110% Ic at LHe
    Successfully powered
Goal:
High-field (B ≥ 2 T)
Small-period undulator λu = 13 mm
Courtesy of S. C. Richter
Helical undulator
S. C. Richter et al. (2023) IEEE Trans. Appl. Supercond. 33(5) 4100207
S. C. Richter, PhD. thesis, KIT (2023)
Notes:     Main challenges:
  Bending radii < 5 mm,
  Quench protection

## Slide 3: HTS compact undulator
LN2
Two different prototype coils
Vertical racetrack (VR)
Helical undulator (Hel.)
Up to ≈ 300% Ic at LN2
Up to ≈ 110% Ic at LHe
    Successfully powered
Goal:
High-field (B ≥ 2 T)
Small-period undulator λu = 13 mm
S. C. Richter et al. (2023) IEEE Trans. Appl. Supercond. 33(5) 4100207
S. C. Richter, PhD. thesis, KIT (2023)
Courtesy of S. C. Richter
LHe
4 mm, non-insulated ReBCO tape
iron core
VR
Hel.
Notes:     Main challenges:
  Bending radii < 5 mm,
  Quench protection

## Slide 4: HTS laser-structured undulator
12 periods per tape, λu = 8 mm
Jointless design
Stacked design
T. Holubek et al., Supercond. Sci. Technol. 30, 115002 (2017)
D. Astapovych et al., FEL2022 Proceedings, WEP45 (2022)
B. Krasch et al., MT-28 (2023), to be published in IEEE (TAS)
Courtesy of D. Saez de Jauregui & A. Grau
30 layers of laser-scribed REBCO tapes, width of 12 mm and thickness of 55 μm
Two different prototype coils
Jointless winding
Stacked design (reduces HTS usage by 75%)
Notes: The grooves in each layer force the current in a defined path, creating a sinusoidal field
HTS tape is bent over the droplet-shape-block, inserted inside the yoke brings a jointless winding
In stacked design, individually structured tapes are stacked and soldered alternating at the tape ends. This novel design reduces the need for HTS material by 75% (sustainability).

## Slide 5: HTS laser-structured undulator
Courtesy of D. Saez de Jauregui & A. Grau
Successfully tested in LHe @ 4.2 K
30 layers of laser-scribed REBCO tapes, width of 12 mm and thickness of 55 μm
Two different prototype coils
Jointless winding
Stacked design (reduces HTS usage by 75%)
T. Holubek et al., Supercond. Sci. Technol. 30, 115002 (2017)
D. Astapovych et al., FEL2022 Proceedings, WEP45 (2022)
B. Krasch et al., MT-28 (2023), to be published in IEEE (TAS)
Notes: The grooves in each layer force the current in a defined path, creating a sinusoidal field
HTS tape is bent over the droplet-shape-block, inserted inside the yoke brings a jointless winding
In stacked design, individually structured tapes are stacked and soldered alternating at the tape ends. This novel design reduces the need for HTS material by 75% (sustainability).

## Slide 6: HTS transport line
400 MeV
Goal:
Lab-scaled transport line for LPAs
High strength miniture magnets Simple coils
Lm = 39 cm
λ = 11.9 cm
Novel iron–core periodic magnets:
Using pancake coils were designed
Half a period was demonstrated
Courtesy of S. Fatehi
S. Fatehi et al. IPAC23, WEODC1 (2023)
S. Fatehi, PhD. thesis, KIT (2023)
Notes:     LPA: Laser Plasma Accelerators
    LWFA: Laser wake field accelerator
    TGU: Transverse Gradient Undulator

## Slide 7: HTS transport line
12 mm, non-insulated ReBCO tape
In LN2 and LHe up to 1 kA Showing no degradation
    Successfully powered & tested:
Goal:
Lab-scaled transport line for LPAs
High strength miniture magnets Simple coils
Novel iron–core periodic magnets:
Using pancake coils were designed
Half a period was demonstrated
Courtesy of S. Fatehi
S. Fatehi et al. IPAC23, WEODC1 (2023)
S. Fatehi, PhD. thesis, KIT (2023)

## Slide 8: HTS cable development
I.FAST development
Goal:
Round HTS cable for fast ramped applications: 30 kA @ 7 T
Magnetization loss
dependent on superconductor dimensions:
Multiple steps to deal with high losses:
  Striation of tapes
  Higher operating temperature
  Longer cycle duration
  Adapt Magnet design
This project has received funding from the European Union’s Horizon 2020 Research and Innovation programme under GA No 101004730.

## Slide 9: HTS beam transfer magnet
Goal:
Upgrade superferric magnets with HTS coils. Minimal changes in infrastructure
Affected component
18 Tm infrastructure at GSI is H-windowframe magnet using pancake coils
Activities:
Ongoing study for AC loss per cycle
  AC loss in order of 1 kJ/cycle
  AC loss highly affected by position of coil in yoke
Ongoing study for conceptual design including mechanics, cooling and basic coil design
S-FRS Dipole FoS

## Slide 10
GSI
18 - 20 October 2023
https://indico.gsi.de/event/17548/
Topics:
- Research Infrastructures and Facilities
- Low Loss and Energy Efficient Accelerator R&D
- Industry
- Technology Transfer and Cooperation

## Slide 11
Questions?
Thank you to my colleagues from KIT for the slide preparation