## Slide 1: SIS Activities at Universität Hamburg
Marc Wenskat - on behalf of the SRF R&D team
3.5.2024 | Universität Siegen

## Slide 2: What did we achieve so far?
@CERN, next with HZB
@BUW & UHH
@HZDR, data from the past
Delay +1y
Fabrication ongoing

## Slide 3: Single-Cell PEALD System
Last parts getting fabricated
Bottle neck: Control
  Many I/O with various properties
  PLC?
Focus on this system now 100%

## Slide 4: Optimizing the process
Simulating the Al2O3 coating process using ANSYS
  Want to do the same for PEALD system
Simulation and experimental data agree well
  p vs. t in chamber
  Calculated & measured GPC → extraordinary, as it contains complex chemical reactions on the surfaces!
Cycle time down but GPC as well → overall t reduction by 33%
  Saves time
  Less parasitic annealing
[G. Deyu et al., Chem. Mater. 2024, 36, 2846−2856]
Simulation

## Slide 5: FE and SEY Studies
Cavities coated at CEA Saclay with Al2O3 were limited around 18 MV/m
  Argument: FE due to higher SEY
Why did we achieve 42 MV/m then?
SEY measurements of our Al2O3 layer
  Lower then CEA (4.5) – why?
  Higher deposition temperature at CEA ?
on SIS
Frederic Braun

## Slide 6: Pancake effect
Original argument for Multilayer: thin films enhance Hc1
We measured Hc1 using a VSM
  75nm of NbTiN on Si
As-deposited is not good
  We know that from Tc as well
Best explanation for Hc1 enhancement is pancake effect
[G. Stejic et al., PRB 49.2 (1994)]
Co-Autor: Alex Gurevich
[A. Gurevich, APL 88 (2006)]
PhD Thesis Isabel Gonzalez

## Slide 7: The QPR is ready
Commissioning done
Transition to regular operation next
5 QPR samples currently fabricated at RI
Looking for PhD student & funding
PhD Thesis Ricardo Monroy-Villa

## Slide 8: Thermal resistance of thin films
x
10 Nb sample pairs, multiple tests:
  as fabricated (2)
  + coarse BCP (4)
  + 800°C (10) → Baseline
  repetitive cooldowns (4)
  SIS (1) + anneal (1)
  Nb3Sn (2)
  Mid-T next
MSc Thesis Cem Saribal
BSc Theses Anton Lorf / Leon King
Based on old work from C. Antoine (CEA) and Jay Amrit (U Paris-Saclay)

## Slide 9: Flux trapping effciency
A. Ivanov, T. Koettig, and A. Macpherson. "Partial Meissner effect measurement by a superconducting magnetic flux lens." arXiv preprint arXiv:2103.06697 (2021).
A. MacPherson
D. Turner
MSc Thesis Lea Preece
90 mm
Argument from Cornell:
Multilayers have to many defects → enhancement
is nullified
Study trapping efficiency as a first measure

## Slide 10: Results are consistent and exciting…
A. MacPherson
D. Turner
MSc Thesis Lea Preece
Observed behaviour fits experience:
  Higher T higher expulsion
What about S-S and S-I-S?

## Slide 11: Vacancy studies important for flux trapping
First studies on S-I-S samples „back then“
New post-processing recipe since then
Now (flux trapping!) also S-S relevant
Application for beamtime submitted
TEM studies in parallel
25nm
15nm
25nm
15nm

## Slide 12: Summary & next steps
Busy 15 months – many studies about SIS and its various aspects
PEALD single-cell system delayed
Our two pillars for SESAM would be:
  Coat a cavity + accompanying studies
  Flux expulsion studies + accompanying studies
  Request 2x PhDs – no significant invest