## Slide 1
Dynamic Analysis of
Normal-Conducting Magnets
D. Moll1, P. Viarouge2, H. De Gersem1,
M. Breschi3, A. Macchiagodena3, P. L. Ribani3,
F. Boattini4, L. Bottura4 , E. Simoni5
1Technical University Darmstadt, Germany,
2Université Laval, Canada,
3University of Bologna, Italy, 4CERN, Switzerland, 5HEIA-FR, Switzerland
IMCC and MuCol Annual Meeting
May 2025

## Slide 2: Outline
Time-domain analysis of normal-conducting magnets
  Field quality evaluation
  Excitations with higher duty cycles
Frequency-Domain Analysis & Equivalent Circuit Modeling
  Frequency- Domain Loss Evaluation Method
  Equivalent Circuit & Nonlinear Dynamic Modeling
  Cross-Validation :Simplified Time-Harmonic & High-Fidelity Transient FEA Model

## Slide 3: Outline
Time-domain analysis of normal-conducting magnets
  Field quality evaluation
  Excitations with higher duty cycles
Frequency-Domain Analysis & Equivalent Circuit Modeling
  Frequency- Domain Loss Evaluation Method
  Equivalent Circuit & Nonlinear Dynamic Modeling
  Cross-Validation :Simplified Time-Harmonic & High-Fidelity Transient FEA Model

## Slide 4: Fast ramping magnets
Main components:
  Laminated iron core: nonlinear, hysteretic
  Conductors: skin- & proximity effects
    Cooling system?
  Beam pipe: induced currents
Different operation modes:
  RCS 2,3,4: zero mean operation
  RCS 1 with DC offset
  Duty cycle ~ 1%
IMCC Interim report, 2024

## Slide 5: Numerical modeling - Maxwell
Maxwell‘s equations:
  Magnetic Gauss:
  Faraday-Lenz:
  Ampère:
Ohm‘s law:
Ampère‘s law:
  Constitutive relationship (or ) needed
    Linear:
    Nonlinear, anhysteretic, isotropic:
    Hysteretic models: Energy-based, Preisach, …
Voltages of every conductor
Distribution functions

## Slide 6: Hysteretic magnetic material model
Magnetization :
, requires:
  Weights =1
  Anhysteretic magnetization operator
  Distinct history operators
straightforward, inversion cumbersome
  Fixed-point iteration needed
A. Bergqvist, ”Magnetic vector hysteresis model with dry friction-like
pinning”, Physica B, 233:342–347, 1997
F. Henrotte et al., ”An energy-based vector hysteresis model for ferro-
magnetic materials”, COMPEL, 25:71–80, 2006.

## Slide 7: Ferromagnetic material model – Eddy currents
Dipole magnet length: 5 m gap height: 30mm 2D analysis
Laminates feature eddy currents in x-y plane
  Not explicitly included in 2D simulations
  Homogenization approach:
Loss calculation:
  Resistive:
  Eddy currents:
  Hysteresis:
P. Dular et al., “A 3-D magnetic vector potential formulation taking
eddy-currents in lamination stacks into account”, IEEE Trans. Magn.,
vol. 39, no. 3, pp. 1424–1427, 2003

## Slide 8: Insights of FEM analysis
Peak excitation current: 50kAt (12.5kA per bar)
Loss density of single pulse (J/m³)
First cycle differs due to
wrong initial state

## Slide 9
Two laminated FeCo permeameter ring samples with/without interleaved Kapton rings
Material Properties for Accelerator Magnets
50 µm Kapton rings
300 µm steel rings
ring stack
excitation/detection windings
NI USB6451
AE Techron 2120 current amplifier
Keysight 33500B Waveform Generator
Keithley multimeter
DCCT power supply
DCCT Zero-Flux MACC
First results: 54 different current pulses up to 1.2 T, 28 kT/s Example: 100 A, 16 ms current pulse, FeCo rings only
Low-field eddy current time constant 

 ≈ 0.40.7 ms
Courtesy Nicholas Sammut, Marco Buzio

## Slide 10: Outline
Time-domain analysis of normal-conducting magnets
  Field quality evaluation
  Excitations with higher duty cycles
Frequency-Domain Analysis & Equivalent Circuit Modeling
  Frequency- Domain Loss Evaluation Method
  Equivalent Circuit & Nonlinear Dynamic Modeling
  Cross-Validation :Simplified Time-Harmonic & High-Fidelity Transient FEA Model

## Slide 11: Field quality analysis
Field quality evaluated on several 5 mm reference circles. (All in vacuum chamber)
Multipole coefficients [T] as function of time and position
Air gap and beam pipe with
10µm Titanium coating
20mm
50mm
30mm

## Slide 12: Beam pipe affecting field quality
Without beam pipe:
With beam pipe:
Unwanted
multipole coefficients
are larger on average.
Similar peak values.

## Slide 13: Relative multipole coefficients
Relative multipole coefficients:
Requirement: 10 Units on 10 mm reference circle
  Green region
Strong quadrupole and sextupole coefficients: Shim design recommended / ongoing
Without beam pipe:
With beam pipe:

## Slide 14: Outline
Time-domain analysis of normal-conducting magnets
  Field quality evaluation
  Excitations with higher duty cycles
Frequency-Domain Analysis & Equivalent Circuit Modeling
  Frequency- Domain Loss Evaluation Method
  Equivalent Circuit & Nonlinear Dynamic Modeling
  Cross-Validation :Simplified Time-Harmonic & High-Fidelity Transient FEA Model

## Slide 15: Excitations with higher duty cycles
Time domain analysis:
+ Captures all details
- Too slow for optimization routines
Frequency domain analysis:
+ Fast heuristic
- Assumes finite number of significant
frequencies
  Requires larger duty cycles
Duty cycle: 0.9ms/200ms <0.5%
Duty cycle: 0.9ms/1.8ms =50%
Duty cycle: 100%
How much does magnet behavior differ for these excitations?

## Slide 16: Losses per period
Copper loss: 75.93 J/m
Titanium loss: 16.46 J/m
Iron loss: 25.11 J/m
  Hysteresis: 8.76 J/m
Copper loss: 69.21 J/m
Titanium loss: 16.43 J/m
Iron loss: 22.89 J/m
  Hysteresis: 7.48 J/m
Copper loss: 48.24 J/m
Titanium loss: 16.31 J/m
Iron loss: 22.69 J/m
  Hysteresis: 7.41 J/m

## Slide 17: Outline
Time-domain analysis of normal-conducting magnets
  Field quality evaluation
  Excitations with higher duty cycles
Frequency-Domain Analysis & Equivalent Circuit Modeling
  Frequency- Domain Loss Evaluation Method
  Equivalent Circuit & Nonlinear Dynamic Modeling
  Cross-Validation :Simplified Time-Harmonic & High-Fidelity Transient FEA Model

## Slide 18: Problem Statement
Pulsed operation of Normal Conducting magnets leads to additional losses such as :
  Magnetic losses in the ferromagnetic yokes
  Joule losses in windings (skin & proximity effects)
Accurate loss evaluation is critical for:
  Global efficiency & Magnet Thermal design
A dynamic magnet model or equivalent circuit is essential for:
  Power converter sizing
  Current pulse control strategy development

## Slide 19: Frequency- Domain Loss Evaluation Method
Objective: Balance accuracy& computational speed for loss estimation in pulsed steady-state regimes with Time-harmonic FEA for efficient iterative optimal design
Fourier decomposition of periodic current pulse on
Time-harmonic FEA for each harmonic 𝑛=0 - 7
Sum harmonic contributions to compute steady-state losses on
Sum Compute average steady-state losses on
Real & Reconstructed Signal
(𝑛=0 - 7 ) on
Steady-state obtained on on with Transient FEA

## Slide 20: Equivalent Circuit & Nonlinear Dynamic Modeling
Time-Harmonic FEA results allow identification of an equivalent circuit with the same frequency response, usable in time-domain simulation
  3 R-L cells fitted by least-squares to match impedance frequency response obtained by Time-harmonic FEA & to model induced eddy current in bars
Nonlinear extension of the dynamic model:
  obtained via saturated magnetostatic FEA using magnetic material B(H)
  Analytical fit → nonlinear inductance inserted into equivalent circuit
Nonlinear hybrid equivalent circuit:

## Slide 21: Cross-Validation Between Simplified Time-Harmonic and High-Fidelity Transient FEA Model
Benchmark: Transient FEA with magnetic saturation & dynamic hysteresis
Simplified Time-Harmonic FEA (linear, frequency-domain) faster to compute steady-state Joule & magnetic losses
Loss evaluation with both methods
  for steady-state operation on
  Valid despite simplified assumptions (steady-state, linear)
[Insert comparison graph and performance summary table]

## Slide 22: Cross-Validation Between Simplified Time-Harmonic and High-Fidelity Transient FEA Model
Dynamic Validation of the Equivalent Circuit Using Transient FEA
Validation scenario:
  Nonlinear hybrid equivalent circuit model driven by pulsed power converter in Simulink
  Simulated input magnet voltage applied to Voltage supplied full Transient FEA model
Agreement on Current waveform reproduction
Transient FEA
Voltage
Current Pulse
Simulink
Transient FEA
SPS-Simulink

## Slide 23: Conclusion & Perspectives
High-Fidelity Transient FEA Magnet Model with saturation for:
  accurate dynamic loss estimation under pulsed regime
  spatial field quality analysis
Simplified Time Harmonic FEA Methodology :
  for loss computation under steady-state pulsed regime
  for identification of nonlinear hybrid equivalent circuit model usable in circuit simulations & Magnet-converter-control co-design
  suitable for implementation in iterative design optimization with computational efficiency
Cross-validation with acceptable accuracy
High-fidelity &simplified FEA models are complementary tools used at different levels of modeling complexity within an integrated CAD & simulation environment.