## Slide 1: mERLin: materials enhanced ERL for increased sustainability
Márton Major, Amir Farhood, Alexey Arzumanov and Lambert Alff
Technical University of Darmstadt, Darmstadt, Germany
SuperSurfer kick-off meeting
DESY, Hamburg
2. December 2024

## Slide 2: BMBF project plan / funding
Novel dual target sputtering process for energy-efficient SRF technology
Sustainable operation of electron accelerators
Combined electromagnetic-thermal numerical simulations considering layered surface structures

## Slide 3: BMBF project plan / funding
Novel dual target sputtering process for energy-efficient SRF technology (not funded)
Sustainable operation of electron accelerators (not funded)
Combined electromagnetic-thermal numerical simulations considering layered surface structures (funded)

## Slide 4: Novel dual target sputtering process for energy-efficient SRF technology
Coating of RF samples for the Quadrupole Resonator (QPR)
Realization of novel in-cavity dual target sputtering process
Inner coating of copper cavities
Performance tests on QPR samples and cavities
Coating of structures for the consortium partners (HOM antennae, QPR cups, samples)

## Slide 5: Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 6: Nb-Sn phase diagram
Charlesworth JP, Macphail I, Madsen PE., Journal of Materials Science. 1970 Jul 1;5(7):580-603.

## Slide 7: Challenge: Vapor-pressure of Sn
Literature results for the critical temperature as
functions of Nb–Sn composition.
A Godeke 2006 Supercond. Sci. Technol. 19 R68

## Slide 8: TU Darmstadt approach: Nb3Sn co-sputtering
Nb
Nb3Sn
Sn Target
Nb Target
Argon
Heater
MFC
Butterfly valve
Substrate
Exhaust
Nils Schäfer

## Slide 9: Nb3Sn cavity roadmap
Optimization of the sputtering parameters (sputter power, substrate temperature, etc.) on fused silica substrate
Adaptation of the growth parameters (further optimization of growth temperature etc.) for copper substrate
Upscaling of the sputtering process to the cavity geometry:
  Optimizing the sputtering parameters for the new (larger) sputtering chamber
  Design and production of the mini double ring magnetron for cavity sputtering
  Inner coating of Cu cavities
N. Schäfer, N. Karabas, J. P. Palakkal, S. Petzold, M. Major, N. Pietralla, and L. Alff, Kinetically induced low-temperature synthesis of Nb3Sn thin films, J. Appl. Phys. 128, 133902 (2020)
E. Barzi, B. C. Barish, R. A. Rimmer, A. Valente-Feliciano, C. M. Rey, W.A. Barletta, E. Nanni, M. Nasr, M. Ross, M. Schneider, S. Tantawi, P. B. Welander, E. I. Simakov, I. O. Usov, L. Alff, N. Karabas, M. Major, J. P. Palakkal, S. Petzold, N. Pietralla, N. Schäfer, A. Kikuchi, H. Hayano, H. Ito, S. Kashiwaji, H. Monjushiro, H. Hama, F. Hona, K. Umemori, K. Takahashi, T. Takahashi, Y. Kondo, K. Yamakawa, K. Kon, T. Kubo, An Impartial Perspective for Superconducting Nb3Sn coated Copper RF Cavities for Future Accelerators, arXiv:2203.09718 [physics.acc-ph] (2022)
N. Schäfer, D. Günzing, T. Jiang, N. Karabas; A. Arzumanov, D. Motta-Meira, K. Ollefs, P. Komissinskiy, M. Major, M. Arnold, N. Pietralla, H. Wende, L. Molina-Luna, D. Lützenkirchen-Hecht, L. Alff, Role of kinetic energy on Nb3Sn thin films by low-temperature co-sputtering, J. Appl. Phys. 134, 043903 (2023)

## Slide 10: Physical properties of Nb3Sn films grown on Cu – conclusions
N. Schäfer et al. to be published
The thin film synthesis results in Nb3Sn layers with overall highly beneficial properties for their application as coatings in copper based SRF cavities.
At processing temperatures where copper diffusion is negligible, around 480 °C, a critical temperature of 16.8K can be achieved. At the same time, 𝐻𝑐1 is enhanced which enhances the applicable acceleration gradients. Low surface roughness and high mechanical stability further makes these coatings excellent candidates for cavity applications.

## Slide 11: Upscaling to copper cavities

## Slide 12: Upscaling to copper cavities
Nb
Sn
Alexey Arzumanov

## Slide 13: Upscaling to copper cavities
300 nm Nb3Sn films grown at different substrate temperature on fused silica substrate
X-ray diffraction patterns
Resistivity normalized to the resistivity at 20 K
Ts (°C) | 400 | 500 | 600
Nb (at%) | 74.9±1.6 | 74.6±0.4 | 74.0±0.4
Sputtering parameters: DC sputtering INb = 450 mA ISn = 80 mA
Amir Farhood

## Slide 14: Nb3Sn sputtered on substrates of fused silica, sapphire and copper at 500 ◦C to investigate the impact of substrate
(a)
(b)
a) XRD patterns of Nb3Sn thin films grown on different substrates
b) Voltage normalized to the voltage at 20 K of thin films measured by coil amplitude method (Meissner effect)
Amir Farhood

## Slide 15: From the TOSCA collaboration
Disc coating (for Hamburg) – still ongoing
Antenna coating with Nb3Sn (for Mainz) – still ongoing
New top cover with Z-shift for the antenna coating
Alexey Arzumanov

## Slide 16
Sputtering spot
Cavity sputtering
In cooperation with Fraunhofer FEP, Dresden

## Slide 17: Acknowledgement
Thank you for your attention!
Funded by BMBF Project 05H21RDRB1 and the German Research Foundation (DFG) through grant GRK2128 (AccelencE)
Nils Schäfer
Matthias Mahr
Philipp Komissinskiy
Jürgen Schreeck
Gabi Haindl
Norbert Pietralla Michaela Arnold
Christian Dietz
Sebastian Bruns