## Slide 1: Recent developments in superconducting RF.
To be honest: Just cavities – no modules, couplers, LLRF, clean rooms …
Marc Wenskat
MSL
12.7.2025
Slides stolen from: TTC2025 if not mentioned otherwise

## Slide 2: Rough overview: Who and what
  US
Busy with PIP-II, LCLS-II HE & SQMS
  DE(SY)
Indirect contributions to ESS, Planned to contribute to PIP-II
Focus on HDC EXFEL Upgrade
  JP
ITN (medium grain)
  PRC
SHINE, DALIA
Significant ramp up
  EU
All in the wake of FCC – hence it is mostly (thin) film R&D
Also ESS and PIPI-II

## Slide 3: What do we need to achieve?
Two remarks:
  Yield is important
  This is operational gradient
Recent developments in superconducting RF.
[The Linear Collider Facility (LCF) at CERN arXiv:2503.24049]

## Slide 4: What performances do exist?
A variety of treatments – an old slide
Recent developments in superconducting RF.
EXFEL Spec
[Reschke et al., Phys. Rev. Accel. Beams, 20, 042004 (2017)]
[Grassellino et al., SUST, 26, 102001 (2013) ]
[Grassellino et al., SUST, 30, 094004 (2017) ]
[Posen et al., Phys. Rev. Applied 13, 014024 (2020)]
[Gurevich, APL, 88, 012511 (2006)]
Standard Cavity
Doped Cavity
Infused Cavity
Mid-T Bake
SIS Coating
LCLS-II CW
@2K
?
HDC Spec
LC Spec

## Slide 5: A controversial take
Recent developments in superconducting RF.

## Slide 6: Quo vadis 2-step?
Cornell & Jlab dropped the R&D
KEK recently reported on their efforts „it is complicated“
China is interested in other recipes
Although we did not see a significant improvement as FNAL, we simply do a 2-step bake now instead of the „standard European XFEL“ 120°C bake. Why? Because why not – and to increase statistics.
Cornell, Jlab, KEK, DESY
Recent developments in superconducting RF.

## Slide 7: Reminder: EXFEL Fabrication VT results

## Slide 8: Operation of EXFEL
Incl. Installation in module, impact of waveguide system
<Eop> = 23.6 MV/m
<Eusable>VT = 29.8 MV/m
Recent developments in superconducting RF.
Some important details:
Administrative limit @ EXFEL for CM of 30 MV/m
@EXFEL 4 modules (32 cavs) driven by 1 Klystron
Future installations will have „finer granularity“
Will allow to operate individual cavities closer to their maximum
- 20%
Do we need to achieve 38MV/m in VT?

## Slide 9: EXFEL vs. LCLS-II vs. LCLS-II HE (N-Doping)
Recent developments in superconducting RF.
4+4 GeV – CW – 464x 1.3 GHz cavities
EXFEL
Modules: administrative limit @ 26 MV/m
284 Cavities
+ 180 Cavities

## Slide 10: EXFEL vs. LCLS-II vs. LCLS-II HE (N-Doping)
EXFEL
Suitable recipe for CW but operational gradients are not sufficient for LC

## Slide 11: SHINE / Shanghai tested two recipes
8 GeV – CW – 600x 1.3 GHz cavites
Recent developments in superconducting RF.

## Slide 12: SHINE will go for Mid-T
Simpler recipe than N doping – same outcome & purely domestic fabrication!
Recent developments in superconducting RF.

## Slide 13: “SHINE cryomodule design adopts the TESLA technology and refers to E-XFEL and LCLS-II”
„FE and MP issues are still challenging for the rest of CMs”
Recent developments in superconducting RF.

## Slide 14: Something old & something new
Recent developments in superconducting RF.
A thorough parameter scan of T-t space
350°C midT shows HFQS again
  diffusion of oxygen
We know how to cure that
Do a simple lowT bake
  Either 48h@120°C (EXFEL)
  Or 2-step bake
  Significant improvent in Eacc and Q0
  3/3 – but single cell
  5/5 – but single cell
Pushing for 9-cell now
Go-to recipe for HDC upgrade
        10x 9cells next year(s)
        He-Tank, then cryomodule
LC Spec
LC Spec

## Slide 15: CERNs SRF R&D for FCC
The main direction is to push performance of thin films on copper cavities (Nb and Nb3Sn)
Recent developments in superconducting RF.
SA18 facility will undergo severe upgrade & changes
Total of ~370 cryomodules and 1500 cavities
Actual distribution (time/spatial) depends operation

## Slide 16: ITN - who
Recent developments in superconducting RF.

## Slide 17: ITN – what (Europe)
Besides recipes:
  Material studies (MG)
  PED
Recent developments in superconducting RF.

## Slide 18: Medium grain cavity fabrication
It‘s all about the flow…
Recent developments in superconducting RF.

## Slide 19: Performance is comparable
Recent developments in superconducting RF.

## Slide 20: Let me be pessimistic
Other „Nb“: Medium grain (ITN)
  Same output for less cost
Nb3Sn?
  Not for high gradients…
Travelling Wave?
  The waveguide will kill us
SIS Multilayer?
  Completely theoretical so far
Recent developments in superconducting RF.

## Slide 21: How can we pull this off?
Significant expertise & capacities in the world
On a 5y scale: optimize new midT/lowT recipe on FG (coldEP) and bring it into the modules (EXFEL HDC upgrade)
Transfer it to industry & partners
On a 10y + X scale: proof-of-concept for TW and/or SIS – then do the industrialization

## Slide 22
Contact
  Dr. Marc Wenskat / MSL
   +49 (0)40 8998-2032  marc.wenskat@desy.de
Deutsches Elektronen-Synchrotron DESY
  Notkestraße 85 22607 Hamburg www.desy.de

## Slide 23
LC Spec