## Slide 1: Precision timing with silicon detector
N. Cartiglia
INFN Torino
New trends in silicon sensors design
How an idea that did not work revolutionized a very mature detector technology

## Slide 2
Silicon life in 2010
Very mature silicon systems, very large silicon trackers
Millions of channels, very reliable, very radiation hard
A true statement:
Silicon sensors are not suitable timing detectors
A nagging problem:
Radiation damage causes charge trapping, reducing the signal in heavily irradiated sensors.

## Slide 3
Solution to the nagging problem
Add moderate gain, “to control and optimize the charge multiplication effect, in order to fully recover the collection efficiency of heavily irradiated silicon detectors” [1]
[1] G.Pellegrini,et al., Technology developments and first measurements of Low Gain Avalanche Detectors (LGAD) for high energy physics applications, Nucl. Inst. Meth. A 765 (2014) 12.

## Slide 4: First design innovation: low gain avalanche diode (LGAD)
In LGAD, a moderately p-doped implant creates a volume of high field, where charge multiplication happens.
The gain layer:
a parallel plate capacitor with high field
zoom
Drift area with gain
0.5 – 2 mm long
Traditional Silicon Detector
Low-gain avalanche diode
p+ gain implant
~1 mm

## Slide 5: First design innovation: low gain avalanche diode (LGAD)
In LGAD, a moderately p-doped implant creates a volume of high field, where charge multiplication happens.
The gain layer:
a parallel plate capacitor with high field
zoom
Drift area with gain
0.5 – 2 mm long
Traditional Silicon Detector
Low-gain avalanche diode
p+ gain implant
~1 mm
It turned out that the LGAD design does not solve the charge-trapping problem as the LGAD mechanism does not work well in high radiation environments (above 2-3E15 1-MeV neq/cm2)

## Slide 6: 2012: Silicon sensors as timing detectors
RD50 June 2012, Bari

## Slide 7: Why internal signal multiplication improves timing?
“Low gain” needs to be understood in connection with the noise of the electronics: it is the range of gain with an improved signal-to-noise ratio.
Signal
Best S/N ratio
Total Noise
Noise floor, gain independent
Signal (gain)
Amplitude
10 100
Noise floor
The electronics has a noise floor
The signal increases with gain
The signal noise increases with gain with steeper characteristics
The total noise is flat at low gain, and then it increases fast
Low gain
The success of LGADs rests on the fact that the sensor noise is hidden by the electronic noise
Noise

## Slide 8
Temporal resolution vs sensor thickness
Resolution without gain
Both CMS and ATLAS have opted for 50 mm thick UFSD,
(intrinsic time resolution of about 30 ps)
Silicon sensors have an intrinsic resolution that depends on the thickness
LGAD
LGAD
Intrinsic LGAD
LGAD
LGAD
Intrinsic LGAD
LGADs are now a commercial commodity, many foundries are producing them.
The combined CMS+ATLAS order exceeds 20 m2 for a cost in excess of 5-6 million CHF

## Slide 9: LGAD temporal resolution for thin sensors
LGAD intrinsic temporal resolution improves in thinner sensors:
==> reasonable to expect 10-20 ps for 10-20 mm thick sensors.
10 fC (gain = 20)
4 fC (gain = 20)

## Slide 10
Timing layers and 4D tracking
Timing
By “4D tracking” we mean the process of assigning a spatial and a temporal coordinate to a hit.
Timing can be available at different levels of the event reconstruction:
Timing in a single point (timing layer ATLAS,CMS): 3+1 tracking

## Slide 11
Timing layers and 4D tracking
Timing
By “4D tracking” we mean the process of assigning a spatial and a temporal coordinate to a hit.
Timing can be available at different levels of the event reconstruction:
Timing in a single point (timing layer ATLAS,CMS): 3+1 tracking
Timing at some points along the track

## Slide 12
Timing layers and 4D tracking
Timing
By “4D tracking” we mean the process of assigning a spatial and a temporal coordinate to a hit.
Timing can be available at different levels of the event reconstruction:
Timing in a single point (timing layer ATLAS,CMS): 3+1 tracking
Timing at some points along the track
Timing at each point along the track: 4D tracking

## Slide 13
Timing layers and 4D tracking
Timing
By “4D tracking” we mean the process of assigning a spatial and a temporal coordinate to a hit.
Timing can be available at different levels of the event reconstruction:
Timing in a single point (timing layer ATLAS,CMS): 3+1 tracking
Timing at some points along the track
Timing at each point along the track: 4D tracking
Many timing coordinates per track yield better-performing detectors but require more complex read-out systems.
Some projects will be perfectly fine with having a limited set of timing points

## Slide 14
Why is timing needed at HL-LHC?
protons
protons
No temporal information:

## Slide 15
Why is timing needed at HL-LHC?
protons
protons
No temporal information:
protons
protons
With temporal information:

## Slide 16
Why is timing needed at HL-LHC?
protons
protons
No temporal information:
protons
protons
With temporal information:
HL-LHC situation:
the collisions are so dense that overlap in space
Timing allows to separate them

## Slide 17
Combining spatial and temporal resolutions
In silicon sensors, the position resolution depends on the pixel size
Very good position resolution requires very small pixels
The pixel size determines the space available for the electronics
Sensor
ASIC
Good temporal resolution requires a sizable amount of power per electrode.
“Simply” adding timing capabilities to a pixel detector will not work in large systems, the cooling requirements are too high

## Slide 18: Second design innovation: resistive silicon detector
-------------
+++++++++
-------------
+++++++++
In resistive silicon detectors, instead of many p-n diodes, there is a single diode.
The n-doped implant is resistive and acts as a signal divider
Very uniform electric and weighing fields, perfect geometry for timing
p-bulk
n++
p++
n+
Signal sharing is the key ingredient to excellent spatial resolution using large pixels
Standard silicon detector
Resistive silicon detector
(AC-LGAD, RSD, DC-RSD)

## Slide 19
3
4
1
2
Signal sharing in resistive silicon detectors
The signal sees several impedances in parallel, and it is split according to Ohm’s law.
Each pad gets a share of the total signal, exactly as in a current divider

## Slide 20
RSD principle of operation in motion

## Slide 21
Example: square pixel, 500-micron pitch
DC-RSD pixel sensor
A particle hits the detector
The signal is shared among the 4 electrodes

## Slide 22
Signal shape: square pixel, 500-micron pitch
The picture shows the amplitude recorded by 6 electrodes,
  4 in the hit pixel
  2 in the adjacent pixel.
The signal is fast, same shape of a standard LGAD.
Perfect isolation: the signal is seen only in the electrodes belonging to the hit pixel.

## Slide 23
Spatial and temporal resolution, 500-micron pitch
RSDs achieve a spatial resolution of about 5% of the pitch,
and 30-40 ps temporal resolution

## Slide 24
Standard vs RSD tracker
Standard Tracker
RSD-based tracker
Resistive implant
~ 50 mm
Pixel size
~ 250 x 250 mm2
Silicon bulk
Contacts
Electronics
~ 150 mm
Gain implant
--
---
- --
+
++
+++
Pixel size
~ 25 x 25 mm2
An RSD-based tracker has a factor of 100 less electrodes, provides the same spatial resolution and in addition has excellent temporal resolution

## Slide 25
Standard vs RSD tracker
Several experiments are presently considering building an RSD-based tracker
Standard Tracker
RSD-based tracker
Resistive implant
~ 50 mm
Pixel size
~ 250 x 250 mm2
Silicon bulk
Contacts
Electronics
~ 150 mm
Gain implant
--
---
- --
+
++
+++
Pixel size
~ 25 x 25 mm2
An RSD-based tracker has a factor of 100 less electrodes, provides the same spatial resolution and in addition has excellent temporal resolution

## Slide 26
Silicon sensors: a very intense R&D
No gain
Hybrid
Monolithic
BiCMOS
(SiGe)
3D
Si/Diamond
Low-gain (LGADs)
Resistive
BiCMOS
(SiGe)
Standard
No gain
Low-gain (LGADs)
CMOS
Planar
Sensor
ASIC
Sensor
ASIC

## Slide 27
Silicon sensors: a very intense R&D
No gain
Hybrid
Monolithic
BiCMOS
(SiGe)
3D
Si/Diamond
Low-gain (LGADs)
Resistive
BiCMOS
(SiGe)
Standard
No gain
Low-gain (LGADs)
CMOS
Planar
Sensors for 4D tracking
Sensor
ASIC
Sensor
ASIC

## Slide 28
Tracking in 4-dimensions: a very rich field
Hybrid
Low-gain (LGADs)
The present R&Ds in position-sensitive timing detectors is very diverse
Sensor
ASIC
Presented so far
Resistive
Standard

## Slide 29
Tracking in 4-dimensions: a very rich field
No gain
Hybrid
The present R&Ds in position-sensitive timing detectors is very diverse
Sensor
ASIC
3D
Si/Diamond

## Slide 30
4D tracking at extreme fluence
No gain
Hybrid
Two possible options:
Column
Trenches
The amount of charge is
controlled by the sensor
thickness (~1-2 fC)
Both requires small pixels to achieve good temporal precision
==> very good position resolution
Sensor
ASIC
3D sensors use vertical electrodes to achive very high radiation resistance
3D
Si/Diamond

## Slide 31
4D tracking using monolithic sensors
Monolithic
No gain
Low-gain (LGADs)
CMOS
Sensor
ASIC
BiCMOS
(SiGe)
BiCMOS
(SiGe)

## Slide 32
4D tracking using monolithic sensors
Monolithic
No gain
Low-gain (LGADs)
CMOS
Sensor
ASIC
In this research path the best resolution has been obtained by using a SiGe front end and small exhagonal pixels (65 microns).
.
BiCMOS
(SiGe)
BiCMOS
(SiGe)

## Slide 33
4D tracking using monolithic sensors
Monolithic
No gain
Low-gain (LGADs)
CMOS
Sensor
ASIC
In this research path the best resolution has been obtained by using a SiGe front end and small exhagonal pixels (65 microns).
.
Studies have shown excellent results for prototypes with and without gains
BiCMOS
(SiGe)
BiCMOS
(SiGe)

## Slide 34: Electronics: What is the best pre-amp choice?
Current Amplifier
Charge Sensitive Amplifier
Current signal in a 50 mm sensor
Energy deposition in a 50 mm sensor
Fast slew rate
Higher noise
Sensitive to Landau bumps
Slower slew rate
Quieter
Integration helps the signal smoothing

## Slide 35
Read-out chips for LGADs
In the past 3-4 years, the ATLAS and CMS collaborations poured a considerable amount of resources into designing the read-out chips for their respective timing layers.
A timing layer with large pixels needs less power than a layer of small traditional pixels
As a comparison, the RD53 readout chip for pixel detectors for tracking (i.e. no timing) at the HL-LHC with 50 x 50 um2 and 25 x 100 um2 feature sizes is estimated to have a power density of about 1 W / cm2
ATLAS: ALTIROC, TSMC 130 nm, 15x15 pads,
CMS: ETROC, CMOS 65 nm, 16x16 pads
For both: input load about 4 pF, jitter ~ 20ps at 10fC of input charge
Power:
ALTIROC ~ 3.5 mW/ch, 2-300 mW/cm2
ETROC~ 3 mW/ch

## Slide 36
Present status of ATLAS-CMS timing layer
LGADs are available from many vendors: HPK, FBK, CNM, BNL
and several more are coming on line: Micron, NDL (China), IHEP (China)
ATLAS and CMS are planning to use ~ 20-30 m2
 Mature technology
Installation: 2026-2027
CMS: 2 layers, covering the full endcap 1.6 < eta < 3
ATLAS: 2 ½ - 3 layers, covering high rapidity 2.5 < eta < 4
CMS: 7 m2 of sensors on each side
HPK2
16x16 array
2.1 cm

## Slide 37
Wrap-up
4D tracking is a very young booming field, hybrid and monolithic approaches are yielding very good results
The paste of innovation is very fast (especially considering that silicon sensors is a very mature field)
Several demonstrators with temporal precision of about 30 ps are available. Not unreasonable to expect 10-15 ps in the next few years.
In my view, the most difficult part is in the design of the electronics.
Temporal resolution degrades very quickly if the whole system is not “perfect”
It is very difficult to combine very good position precision, <5 mm, with good temporal resolution using the “single-pixel design”. Charge sharing might be the key to solve this problem.

## Slide 38
Wrap-up
4D tracking is a very young booming field, hybrid and monolithic approaches are yielding very good results
The paste of innovation is very fast (especially considering that silicon sensors is a very mature field)
Several demonstrators with temporal precision of about 30 ps are available. Not unreasonable to expect 10-15 ps in the next few years.
In my view, the most difficult part is in the design of the electronics.
Temporal resolution degrades very quickly if the whole system is not “perfect”
It is very difficult to combine very good position precision, <5 mm, with good temporal resolution using the “single-pixel design”. Charge sharing might be the key to solve this problem.
Thank you for your attention

## Slide 39
Backup

## Slide 40: Intrinsic LGAD time resolution
The temporal resolution is degraded if one energy deposit is much larger than the average.
Thick sensors have worse temporal resolution because it is more likely that at least one energy deposit is much larger (local Landau fluctuation in the energy deposition)
WF2 Simulated energy deposits
15-micron thick sensor
80-micron thick sensor
Large energy deposits are more likely in thicker sensors
Because the signal changes shape on an event-to-event basis
due to non-uniform energy deposition along the particle path
Why do LGADs have an “intrinsic” time resolution?

## Slide 41: Resistive Silicon Detector (RSD, AC-LGAD, DC-RSD)
Resistive Silicon Detectors
combine low-gain and resistive read-out
p-bulk
n+
p++
Gain implant
30-50 mm

## Slide 42: Tracking in 4 Dimension
The introduction of timing allows separating collisions that happen in the same location

## Slide 43
Why gain improves the temporal resolution?
The timing capabilities are determined by the characteristics of the signal at the output of the pre-Amplifier:
Larger Signal/noise ==> better timing
Time is set when the signal crosses the comparator threshold

## Slide 44
Irradiation effects
Irradiation causes 3 main effects:
Decrease of charge collection efficiency due to trapping
Doping creation/removal
Increased leakage current, shot noise
The main effect in LGAD is “acceptor removal”, i.e., the reduction of the gain implant doping
The electric field due to the gain implant decreases  Compensated with higher bias
Main technique to decrease acceptor removal: carbon implantation in the gain layer
Carbon spoils the properties of silicon sensors.
However, in the right amount and only on the gain implant, it increases the sensor rad. resistance by a factor of 3
carbon implantation

## Slide 45
Acceptor removal
Unfortunate fact: irradiation de-activate p-doping removing Boron from the reticle
Boron
Radiation creates Si interstitial that inactivate the Boron:
Si_i + B_s  Si_s + B_i
Gallium is substitutional
From literature, Gallium has a lower possibility to become interstitial
Carbon is substitutional
Interstitial Si interact with Carbon instead of with Boron and Gallium
Two possible solutions: 1) use Gallium, 2) Add Carbon

## Slide 46: Effect of acceptor removal
To some extent, the gain layer disappearance might be compensated by increasing the bias voltage
Acceptor removal,
Gain layer deactivation

## Slide 47
Impurity engineering of radiation resistance
Carbon addition works really well, increasing by a factor of 2-3 the radiation hardness
Gallium is actually is not more rad-hard than Boron
less radiation resistance
more radiation resistance: B+C

## Slide 48: UFSD temporal resolution in thinner sensors
Non uniform ionization:
Physical limit of UFSD sensors
UFSD temporal resolution improves in thinner sensors:
==> reasonable to expect 10-20 ps for 10-20 mm thick sensors.
Be aware: very difficult to do timing with small signals… power consumption increases
FBK UFSD32 production

## Slide 49: RSD spatial resolution
RSDs at gain = 30 achieve a spatial resolution of about 2-3% of the pitch size:
RSD:
1300 x 1300 mm2: sx ~ 40 mm
450 x 450 mm2: sx ~ 15 mm
Traditional standard pixel
1300 x 1300 mm2: sx ~ 920 mm
450 x 450 mm2: sx ~ 320 mm
Chart: RSD2 crosses: spatial resolution when the total AC amplitude = 60 mV
| 1300 | 450 | 340 | 200
1300 um | 40 | 15 | 13 | 10
 | 9.6519


Chart: RSD2 crosses: spatial resolution for 4 different pitch sizes
| 29 | 53 | 69 | 154
1300 um | 95 | 50 | 33 | 15.4
450 um | 34 | 25.3 | 19.9 | 15.5 | 10.6 | 10.1 | 8.4 | 7.9 | 10.6
340 um | 44.8 | 34.1 | 21.87 | 19.9 | 13.85 | 12.8 | 10.6 | 7.4 | 6.33
200 um | 45.9 | 26 | 24.13 | 18.5 | 15.9 | 10.5 | 8.5 | 7.8 | 5.2 | 4.4
gain = 30

## Slide 50: RSD temporal resolution
Chart: RSD2 Crosses: time jitter for 3 different pixel sizes
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185
Calculated Jitter | 240 | 120 | 80 | 60 | 48 | 40 | 34.2857 | 30 | 26.6667 | 24 | 21.8182 | 20 | 18.4615 | 16 | 14.1176 | 12.6316 | 11.4286 | 10.4348 | 9.6 | 8.8889 | 8.2759 | 7.7419 | 7.2727 | 6.8571 | 6.4865
1300 x 1300 um^2 | 56.745 | 32.8786 | 23.4028
450 x 450 um^2 | 36.3716 | 28.9083 | 22.7264 | 17.598 | 16.4973 | 15.3704 | 14.2113
200 x 340 um^2 | 54.8016 | 56.5406 | 39.4137 | 30.3111 | 18.6773 | 15.7493 | 12.0416 | 8.6626 | 7.7775
gain = 30
The resolution depends mostly upon the signal size and weakly on the pixel size
RSDs at gain = 30 achieve a temporal jitter of about 20 ps

## Slide 51: Why low gain? Shot noise in LGAD - APD
Idg
Ids
+
-
+
-
+
-
+
-
IL
Bulk Leakage current
Signal current
Surface current
k = e/h ionization rate
x = excess noise index
M = gain
gain layer p+
n++ electrode
p++ electrode
Correction factor to the standard Shot noise,
due to the noise of the multiplication mechanism