## Slide 1: Polarized electron source R&D @IHEP
A photocathode DC gun @IHEP
Scheme of PES R&D based on DC gun
Wien filter
Mott polarimeter
Polarized electron source R&D for CEPC at IHEP
Research goals: Generation of electron beams with high bunch charge (≥1nC) and high polarization (≥85%)
Based on a photocathode DC gun already developed by IHEP with an extremely high vacuum (10-10Pa)
Beam line setup and design of key components such as Wien filter and Mott polarimeter has been carried out
Expect beam commissioning scheduled in 2027

## Slide 2: Polarized electron source R&D @IHEP
Domestic R&D on the superlattice GaAs cathode
Since the beginning of this year, we have been starting the R&D of the most important part for PES: Photocathodes
In collaboration with a domestic company Acken Optoelectronics Ltd. @ Suzhou
Superlattice GaAs photocathode will be produced by MBE: Polarization > 85%, QE > 1%
Build a platform for photocathode performance test (both pol & QE), this platform has been designed and is currently under development
The first photocathodes have been produced and will be tested soon
Platform for cathode test: ESP & QE
GaAs | 5 nm | p=5×1019 cm-3
GaAs/GaAsP SL | (4/3 nm) ×14 | p=5×1017 cm-3
GaAsP0.35 | 2750 nm | p=5×1018 cm-3
Graded GaAsPx (x = 0~0.35) | 5000 nm | p=5×1018 cm-3
GaAs buffer | 200 nm | p=2×1018 cm-3
p-GaAs substrate (p>1018 cm-3) |  | 
Structure of Superlattice layers
Samples of superlattice GaAs/GaAsP