## Slide 1
Overview of the HPK-campaign
20 December 2011
Joachim Erfle
University of Hamburg
Notes: 1

## Slide 2: Overview
Introduction to the HPK-campaign
    Devices
    Materials
    Measurements and irradiations
Results of first irradiations
    Dark current
    Effective doping concentration
    Signal collection
Conclusions
courtesy of A. Dierlamm, KIT
17 institutes involved
Notes: 2

## Slide 3: Goals of the HKP-campaign
The main challenges for the tracker at the HL-LHC will be:
    Higher radiation dose
    Higher occupancy
The current tracker would not withstand the radiation and also develop occupancy problems
→ Find best best suitable silicon material and layout for a future tracking detector
To achieve that we investigate a large variety of materials:
    Different oxygen, carbon,… content
    Different bulk doping (n and p)
Test sensor geometries and layouts
Irradiations with neutrons or/and protons to simulate HL-LHC radiation dose

## Slide 4: Wafer overview: HPK-campaign
structure | to study
pad diodes | material
baby strip sensor | reference design / material
baby strip sensor with integrated pitch adapter | design
pixel sensor | reference Design / material
multigeometry pixel | layout parameters
multigeometry strips | layout parameters
baby strixel | design
test-structures | process parameters
Notes: 4

## Slide 5: Silicon material
material | thinning method | active thickness | physical thickness
FZ | deep diffusion | 120,200,300 μm | 320 μm
FZ | --- | 200 μm | 200 μm
FZ | handling wafer | 120 μm | 320 μm
MCz | --- | 200 μm | 200 μm
Epi | handling wafer | 50,100 μm | 320 μm
Of each material there are 3 different types:
  n-type (N)
  Two different strip isolation technologies for p-bulk:
  p-type with p-stop (P)
  p-type with p-spray (Y)

## Slide 6: Wafer-Processing (deep diffusion)
Standard method for thinning: wafer bonding of Si to Si-substrate (low ohmic)
  Well known process
  Relatively expensive
New method: deep diffusion
  Active volume of a 320μm wafer reduced by diffusing high doping from the back.
At high irradiation thick sensors not fully depletable
Mean free path of charge carriers severely reduced due to trapping for highly irradiated sensors
→ In thin sensors less charge is trapped and
voltage needed for full depletion is lower.
pn-junction
active thickness
active volume
inactive volume
physical thickness
Notes: 6

## Slide 7: Sequence of Measurements and irradiations
Pre qualification
First irradiation
Single irradiation qualification
Second irradiation
Measurements and time development
of defect (annealing) studies
courtesy of A. Dierlamm, KIT
courtesy of S. Müller, KIT
HL-LHC: Lint=3000 fb-1

## Slide 8: Irradations
Neutrons: 1 MeV (TRIGA Reactor Ljubljana)
Protons: 23 MeV (Karlsruhe cyclotron)
radius | protons Φeq [cm-2] | neutrons Φeq [cm-2] | total Φeq [cm-2] | active thickness
40 cm | 3 ∙ 1014 | 4 ∙ 1014 | 7 ∙ 1014 | ≥ 200 μm
20 cm | 1 ∙ 1015 | 5 ∙ 1014 | 1.5 ∙ 1015 | ≥ 200 μm
15 cm | 1.5 ∙ 1015 | 6 ∙ 1014 | 2.1 ∙ 1015 | ≥ 200 μm
10 cm | 3 ∙ 1015 | 7 ∙ 1014 | 3.7 ∙ 1015 | ≤ 200 μm
5 cm | 1.3 ∙ 1016 | 1 ∙ 1015 | 1.4 ∙ 1016 | < 200 μm
courtesy of S. Müller, KIT
HL-LHC: Lint=3000 fb-1

## Slide 9: Involvement of DESY and UHH
Doris Eckstein, DESY | Coordination of diode measurements
Georg Steinbrück, UHH | Central European Consortium Project leader
Joachim Erfle, UHH | IV/CV diode measurements Setting up ALiBaVa station for CCE measurement of strip sensors Initiating transfers, tracking parts and checking DB consistency
Thomas Pöhlsen, UHH | TCT/CCE diode measurements
Alexandra Junkes, UHH | Microscopic defect measurements IV/CV diode measurements
Peter Buhmann, UHH | Technical support
Coralie Neubüser, UHH | IV/CV diode measurements
Christian Scharf, UHH | IV/CV diode measurements
Henning Wenck, UHH | IV/CV diode measurements
Evangelos Nagel, UHH | TCT/CCE diode measurements

## Slide 10: Volume current versus fluence
Currents match expected value from M.Moll‘s thesis within the uncertainties.
-> dose measurements are ok.
currents are measured after annealing of 10 min@ 60°C at 0°C and scaled to 20°C
J. Erfle, UHH
neutrons
neutrons
protons
protons

## Slide 11: Volume current versus fluence: Baby sensors
courtesy of A. Nürnberg, KIT
First Baby sensors show higher currents than expected from volume current (M. Moll)
-> maybe a surface effect or internal gain?
currents are measured after annealing of 10 min@ 60°C at -20°C and scaled to 20°C
neutron irradiated Baby sensors
Expected volume current (M. Moll)

## Slide 12: Material characteristics of thin FZ: deep diffusion before irradiation
Concentration profile from CV-curve:
front
320µm N
120µm P
120µm P
Diodes behave like parallel-plate capacitors
→ measure capacitance vs voltage to determine depletion depth and charge carrier concentration
Deep diffusion influences effective doping
J. Erfle, UHH
J. Erfle, UHH

## Slide 13: Neff for different materials / irradiations
protons
neutrons
All measured n-type materials (FZ and MCz) are type-inverted after neutron or proton irradiation.
n-type
capacitances are measured at 0°C, 1kHz after annealing of 10min@60°C
J. Erfle, UHH
J. Erfle, UHH

## Slide 14: Neff for different materials / irradiations
n-type
p-type
protons
neutrons
capacitances are measured at 0°C, 1kHz after annealing of 10min@60°C
J. Erfle, UHH
J. Erfle, UHH
J. Erfle, UHH
J. Erfle, UHH
All n-type materials undergo type inversion
No p-type material undergoes type inversion
All p-type materials show a steep increase in Neff and therefor depletion voltage

## Slide 15: Comparison to non-HPK materials
Type inversion for 100 mm FZ ✔
No type inversion for 100 mm MCz ✔
No type inversion for 50 mm FZ ✗
Radiation damage is always the same,
oxygen high for MCz and 50 µm FZ!
We need to know:
Differences for n- and p-type material
Influence of Neff,0, [O] (and [C], [H], [N])
courtesy of A. Junkes, UHH
N-type materials, 23 GeV proton irradiated

## Slide 16: Time resolved charge collection measurement with TCT shows type inversion
FZ320P
FZ320N
not type inverted
type inverted
unirradiated
p@3E14
courtesy of T. Pöhlsen, UHH
courtesy of T. Pöhlsen, UHH
- holes
- electrons
U=300V
U=600V
courtesy of J. Lange
Laser: 672 nm, red
3µm penetration depth
type inversion of FZ and MCz n-type materials is confirmed by TCT.
Signals are measured at 0°C, after annealing of 10min@60°C
E
depth
Rear
Front
red

## Slide 17: CCE of diodes, after p@3E14
p-type:
hole
collection
n-type:
electron
collection
infrared laser
red laser, front injection
p-type
n-type
measurements are performed at 0°C and 600V, with 20ns integration time
unirradiated
courtesy of T. Pöhlsen, UHH
courtesy of T. Pöhlsen, UHH
courtesy of J. Lange
infrared laser: CCE is about 90%
Electrons only: CCE ~ 85%, holes collection only: CCE ~ 67%
Electron readout performs better
infrared

## Slide 18: Signal of FZ320P baby sensor, after p@3E14
Signal induced by a 90Sr source, readout by ALiBaVa
Vdepl
courtesy of K. Hoffman, KIT
CCE of FZ320 p-type is about 87% at p@3E14, compared to non-irradiated
measurements are performed at -20°C

## Slide 19: Some experimental structures
Idea to reduce occupancy and increase resolution
To be able to read out from the sides, inner strips are routed out in the first metal layer
Strip-sensor with integrated Pitchadapter in the first metal layer
Strixel-sensor
Pitchadapter needed for readout-chip connection
Is it possible to integrate it on the sensor without loosing active area?
courtesy of A. Kornmayer, KIT

## Slide 20: First results for integrated pitch adapter
Silicon Sensor Developments for the CMS Tracker Upgrade
Electron from a Sr90-source
at different positions
Flat S/N in standard region of about 17
Reduced S/N in PA-region, noise stays constant
courtesy of A. Kornmayer, KIT
courtesy of A. Kornmayer, KIT
Notes: 20

## Slide 21: First results for strixel sensors
Silicon Sensor Developments for the CMS Tracker Upgrade
Seed strip (far)
1. far neighbour
1. near neighbour
Seed strip (near)
1. near neighbour
1. far neighbour
Electron from a Sr90-source at near area
Electron from a Sr90-source at far area
Seed strip (far)
1. far neighbour
1. near neighbour
Signal in the far area only measured on strips in the far area.
Signals in near area appear also on far strips
courtesy of A. Kornmayer, KIT
Notes: 21

## Slide 22: Conclusions and outlook
HPK-campaign is making progress
Diode currents at low fluencies as expected
Baby sensors at high fluencies have additional current
Neff develops not as expected: - type inversion for all n-type
                - no type inversion for p-type
                - steep increase for p-type
CCE with baby sensors and diodes reduced to ~90% after 3E14 proton irradiation
More irradiations to come (irradiations with 20cm equivalent fluence finished, radiation clearance measurements have to be done)
Trying to understand material properties in detail
Full annealing studies to be done
Notes: 22

## Slide 23: Backup

## Slide 24: CCE of FZ320 after proton irradiation
measurements are performed at 0°C
courtesy of T. Pöhlsen

## Slide 25: TCT pulses – p-type
FZ200P
FZ320P
MCZ200P
not type inverted
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
300V
600V
250V
measurements are performed at 0°C, using a red laser

## Slide 26: TCT pulses – n-type
FZ200N
FZ320N
MCZ200N
type inverted
measurements are performed at 0°C, using a red laser
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
courtesy of T. Pöhlsen
200V
300V
300V

## Slide 27: oxygen content
material | bulk resistivity | oxide concentration
FZ320P | 3-8 | 3,50E+016
FZ200P | 3-8 | 3,00E+017
FZ120P | 3-8 | 5,00E+017
FZ320N | 1.2-2.4 | 1,80E+016
FZ200P | 1.2-2.4 | 3,00E+017
FZ120P | 1.2-2.4 | 5,00E+017
MCZ200P | >2 | 3,75E+017
MCZ200N | >0.5 | 3,00E+017