Bump bonding studies
Jan Hampe, DESY FEC
Daniel Pitzl, DESY CMS
PSI visit, 25.1.2012
Bump bonding at IZM would be the most expensive task in the pixel upgrade project.
Search for alternative:
  - Bump placement without wet chemistry and lithography: solder ball technique from PacTech!
  - Flip chip bonding at DESY: which bonder to buy?
First results on pixel test structures.

---
CMS Pixel Sensors
- 60 wafers under production at CIS (Erfurt)
  - standard CMS pixel sensor design (double sided, n-in-n, p-spray insulation).
  - for Karlsruhe, INFN, CERN/Taiwan, MRI, Purdue, DESY.
  - 5 wafers with increased bump pad passivation opening: 30 µm, for DESY.
  - Delivery in Feb 2012.
- Full sensors for first bump bondings.
- Single chip sensors for tests with new ROCs.
design: Tilman Rohe, PSI

---
CMS Pixel bump bonding
Deposit bump material
in a planar process:
sputtering,
photo lithography,
etching:
Form bumps by melting
in a re-flow oven:
PSI process uses Indium: low melting point at 156.6oC.
Not favored by industry: brittle, long term stability?

---
Bump deposition and flip chip bonding
Ch. Broennimann et al.: Development of an Indium bump bond process for silicon pixel detectors at PSI NIM A565(2006)303-8

---
Alternative
- Still need under-bump metal UBM
- Deposit bump ball directly
- Flip chip bond as before

---
PacTech solder ball laser jet
- Start with high-precision balls.
- 40 µm balls at 80 µm pitch possible now.
  - 30 µm balls being certified.
- Drop through capillary towards pad.
- Melt by laser pulse during fall.
- Solidify on pad.
- Step-motor controlled.
- 5 balls / second.
 http://www.pactech.de/index.php?option=com_content&view=article&id=154&Itemid=21 pub 68

---
PacTech test structures
Pac 2.7 Wafer from Pac Tech GmbH
Two 200-mm Wafers with 275 Chips each
5-µm electroless Ni/Au UBM on both
40-µm SAC305 Solder Jetting with SB2 on one
Wafer Sawing & Chip Singulation
w/o
Solder
Balls
180
Solder
Balls
SiO2
Au
~29 µm
40-µm round
Passivation Opening
~48 µm
Available since Dec 2010.
Used with 4 machines/vendors.
Only 180 bumps / chip.
Diagnostics difficult.
Karsten Hansen, DESY FEC

---
Bump bonding tests with Kadett at SET
Tacking-Cycle Parameters:
automatic Alignment:	diagonal B2B
Chip & Substrate Heating: 25 ... 200°C, 0 ... 20 s
Force Adjustment: 1 ... 6 kg,	5 ... 20 s
Flip-Chip Bonder Kadett from S.E.T.
High-Accuracy Placement
&
Semi-Automatic
Device Bonder
example: 1 kg in 5 s @ 163°C in 10 s
sheering test:
UBM
Bond Head with 22-mm ceramic heating chuck
Substrate 50-mm ceramic heating chuck
Compression: appr. 8 µm
Shear Force: 1.8 kgf → 55 mN / Bump
Karsten Hansen, DESY FEC

---
Laser flip-chip bonding
Neodym-dotierter Yttrium-Aluminium-Granat-Laser
1064 nm
units
per
hour
PacTech
publication 66
Nov 2009

---
Solder Ball Placer:
pre-formed balls are placed sequentially at 6-7 Hz
fused by laser heating
30 µm balls being certified, 40 µm ordered for test.
Pac Tech: SB2 Jet
Industry standard, expensive, slow.
For placing and re-flow heating. Used at IZM.
SET: FC 150
Flip-chip bonder
PSI design: cheapest, slow.
no > 50 mm heating chuck available.
SET: Kadett K1
Unitemp:
RS-350-110
Tacking Tests completed on small samples:
> 0.6 g/ball @ 155°C for chip & substrate.
Re-flow tests completed: OK.
Novel Industry Standard: medium price
laser-assisted, fast.
Pac Tech: Laplace
RFA 300M
Tacking Tests completed:
low force with chip at 195°C for 1s.
Reflow Tests completed: OK.
Finetech: FINEPLACER femto
Novel FC 150 competitor: medium price.
Placing and re-flow heating, low-force, fast.
Tacking / re-flow tests under way.
Karsten Hansen, DESY FEC

---
Probe station at DESY FEC
Süss Microtech PA 300 Probe Station
Probe-Card Holder
auctioned
from
Qimonda
in Dec 2009
will order 42 needle probe card for testing ROCs after bump bonding.
up to 300 mm wafers
Semi-Automatic
Shielded
Thermo chuck -40 .. +125oC

---
Test structures for bump bonding
- Designed by I. Diehl, DESY FEC:
  - Contact chains with 160 bumps, sensor and ROC geometries.
- Idea:
  - Measure electrical continuity on external pads,
  - Get statistics in the ‰ range.
- Ordered at CIS Erfurt:
  - 100 mm silicon substrate, 400 µm thick, 20 wafers.
  - 2 masks: one metal layer, one passivation layer
  - pad metalization AlSiCu, under bump metal Ti-Ni-Au.
  - delivery now promised for end of May.
- At PacTech:
  - Thin some wafers to 175 µm or less.
  - Deposit 40 µm bumps on the sensors, dice wafers.
  - Flip chip bonding.

---
Timeline from April 2011 and reality
May 2011: Test structures being produced by CIS Erfurt
  - required 3 iterations: passivation residue on pads
Jun-Jul 2011: thinning, bump bonding and dicing at PacTech, 40 µm balls. Design and build formic acid chamber for laser re-flow.
  - done by Nov 2011
- Aug-Sep 2011: evaluation at DESY: bump yield. Still to be done.
- Sep/Oct 2011: decide whether to order machines: solder ball placer, flip chip bonder. EU-wide tender and 5 months delivery time.
  - Early Spring 2012 ?
- Winter 2011/12: produce test structures for 30 um balls.
  - Needed? can we do with 40 um balls?
- Spring/Summer 2012: bump bonding tests at DESY, first on test structures, then on pixel sensors and ROCs. Still to be done.
- end 2012: bump bonding established at DESY? Slip into 2013 OK?

---
Test structures for bump bond tests
Dummy structures for bump bond yield characterization:
Sensor
ROC
Fabricate at CiS
Bond at PacTech
measure at DESY
Schliffbilder at DESY:
Embedding
Cutting
Polishing
microscope photos
ROC dummy
Sensor dummy

---
New test structures for bump bonding
100 mm wafer
2 masks: metal and passivation
2 CMS pixel 'sensor' structures
40 'ROC' structures
Produced at CIS Erfurt
Inge Diehl, DESY FEC

---
New test structures for bump bonding
pixel sensor structures
these will receive the bumps
Inge Diehl, DESY FEC

---
New test structures for bump bonding
double-column chain
pixel chip structures
metal pad 50 µm Ø
window in passivation 30 µm
for 40 µm Ø bumps
Inge Diehl, DESY FEC

---
New test structures for bump bonding
pixel chip structures
alignment
marks
test pads for 4-point
I-V measurement
Inge Diehl, DESY FEC

---
'Sensor' test structure from CIS
geometry of the barrel pixel sensors
one half of the contact chain
is on the sensor:

---
'ROC' test structure from CIS
after bump bonding the
contact chain is closed
on the ROC.
on the same wafer, before dicing:
Pad pitch = 100 µm / 200 µm
Pad metal = 50 µm diameter
Passivation opening = 30 µm

---
4-point conductivity measurement
inject current,
measure
voltage drop
probe pads
in the 'ROC'
periphery
Probe card delivered from Wentworth: 104 needles.
Programmable switching box is ready.

---
Under bump metal from PacTech
Dummy-ROC with UBM:
Probe pads
with UBM:
main problem:
residual passivation layer
on the pads from CIS.
1st batch: 15 of 18 wafers bad
2nd batch: ~5% bad
3rd batch: delivered last week
are pin holes a problem?
ENIG UBM:
Electroless Nickel-Gold
5 µm Nickel
50 nm Gold
40 µm diameter

---
Solder balls placed with PacTech SB2
Pad bumped with
40 µm solder ball,
after re-flow:
'sensor' with solder balls:
Side view of bumped
daisy chain structure

---
Laster re-flow with PacTech LaPlace
After solder placement
After laser reflow
microscope
focus
at top of
ball:
Laser re-flow
(10 sec. in formic acid atmosphere)
Spherical top
Crater on top
microscope
focus
at pad:
Slightly off-centered
Self-aligned

---
Formic acid chamber for PacTech LaPlace
Formic acid chamber for LaPlace laser bonder
designed and built by PacTech on our request:
Groove for gas inlet and exhaust
Bumped sensor
Tacked ROC
Special glass for high infrared transmission
Sealed automatic cover (open)

---
Flip chip bonding at PacTech
Schliffbilder:
'ROC' side: single reflow
Nickel
Tin
Nickel
'sensor' side: three reflows

---
CIS problem: residual passivation on pads
Schliffbild:
UBM missing on 'ROC' side
Tin
Nickel

---
Bare module production at DESY FEC
Solder Ball Jetting
ENIG UBM at Pac Tech
Jetting 40 µm Solder Balls
SB2 Jet
Flip-Chip Placement and Re-flow:
Schliffbilder:
bumped
After re-flow
LaPlace
PacTech Test Chip
After tacking
Bare module test on probe station:
+
+
Suess PA300
Probe Card (PSI Design)
Test Board from PSI / ETHZ

---
Pixel module assembly tools at Uni HH
Tool rebuilt according to
PSI CAD drawings.
Gluing tests on dummy
modules underway.