## Slide 1: Measurements on MPIX sensors
DESY Zeuthen

## Slide 2: Overview of measured sensors
  19 Float Zone silicon
    320, 200 mm thickness (each type twice); 120mm (each type at least once)
  9 Magnetic Czocharlski silicon
    200 mm thick (each type at least twice)
  6 Epitaxial silicon
    100, 50 mm thickness (each type once)

## Slide 3: Overview of measurements
I/V and C/V of the bias ring
For each region 3 measurements of
  I/V and C/V curves of the pixels
  Inter pixel resistance and capacitance
  Bias resistor for poly silicon
  Some measurement of punch through resistor

## Slide 4: Bias

## Slide 5: Bias resistor: Poly silicon
Very homogeneous
For N-bulk higher than for P-bulk
Values are for long pixels are
  6.4MW for N-type and 5 MW for p-bulk
Values are for short pixels are
  3.2 MW for N-type and 2.5 MW for p-bulk

## Slide 6: Bias resistor: Punch through
Second plot!

## Slide 7: Rint
Higher than for M
  PS ~ 1013 Ohm
  PT ~ 1014 Ohm
  Some to high to measure

## Slide 8: Inter pixel capacitance (Cint)

## Slide 9: Ctotal

## Slide 10: Itotal
Curves for N type have “normal” shape but positive offset of poly silicon
Curves for P-bulk have normal shape and positive offset for PS (negated in plot!) and peaks for PT biasing

## Slide 11: More Itotal
Comparison of different sensor thicknesses
Some of the tests…

## Slide 12: Conclusions
Talk have to be finalized: Wednesday 10 o’clock???
Measurements are on going
  Now have from each type measurements
  Making a lot afford to understood the current offset
    NO Explinations up to now
Wait for irradiated sensors

## Slide 13: Appendix
Measurement setup and all results

## Slide 14
12
11
10
9
8
7
6
5
4
1
2
3
12
1
Pixel 32…1
8
Line
1
N
S
E
W

## Slide 15: I/V & C/V - Bias ring
A
VDC
Sample
Chuck
BP
Bias Ring
Guard Ring
Bias
Adapter
LCR Meter
BP
Bias Ring
Guard Ring
H
L

## Slide 16: C/V Bias Ring
Notes: 16

## Slide 17: I/V Bias Ring

## Slide 18: Cint & Rint
LCR Meter
BP
Bias Ring
H
L
Guard Ring
BP
A
Bias Ring
VDC
Guard Ring
DC-PADs
H

## Slide 19: Cint

## Slide 20: Rint

## Slide 21: Ctotal & Itotal
30/01/2012
DESY Zeuthen
21
Bias Ring
A
DC-PADs
BP
Guard Ring
Bias
Adapter
LCR Meter
BP
Guard Ring
L
H
Bias Ring

## Slide 22: Ctotal

## Slide 23: Itotal

## Slide 24: Rbias & RPunch through
VDC
Sample
Chuck
BP
Bias Ring
A
DC-PAD
Guard Ring
H
Lin
Hout
RPT
U
VDC
Sample
Chuck
BP
Bias Ring
PAD
Guard Ring
I