## Slide 1
Thinner passivation may lead to unwanted UBM growth
WAFER 4, SENSOR 3, N-SIDE
Max. 4 pixels
No pad affected
May work anyway
If it‘s the only defect on the wafer I wouldn‘t complain

## Slide 2
P-side defects look more serious but are not necessarily problematic
WAFER 4, SENSOR 1, P-SIDE
P-side not affected by PacTech process and involved in further processing
Looks bad
Stress induced?
Maybe not problematic.

## Slide 3
P-side defects look more serious but are not necessarily problematic
WAFER 4, SENSOR 2, P-SIDE
Not serious?
CiS handling ? because metal affected, which is later under passivation layer

## Slide 4
P-side defects look more serious but are not necessarily problematic
WAFER 5, SENSOR 1 + 3, N-SIDE
Sensor 1
Not good but is it problematic?
Probably not for Pac Tech
One or two Pixel affected only
Sensor 3
Could end as a defective pad after UBM process

## Slide 5
P-side defects look more serious but are not necessarily problematic
WAFER 5, SENSOR 1 + 3, P-SIDE
Sensor 1
Looks removable through Pac Tech rinsing process
Sensor 3
CiS related failure but maybe unproblematic for P-side
Just one pixel in sensor

## Slide 6
Wafer 6 has few lost pixels due to debris
WAFER 6, ALL SENSORS , N-SIDE
Pixel lost
Chipped silicon?
Problematic?
Most probably pixel lost

## Slide 7
Wafer 6 presents interesting defect. First real problem?
WAFER 6, ALL SENSORS , N-SIDE
Probably not aliasing
Pairs of pixels present (colored) defects along punch through line:
Pads seem not affected
UBM problematic?

## Slide 8
Wafer 6 has scratch on P-side. CiS handling?
WAFER 6, SENSOR 1, P-SIDE
Probably not aliasing
Seems to be below passivation

## Slide 9
Wafer 6 P-side has area of thickness variation in passivation layer
WAFER 6, SENSOR 2 , P-SIDE
Dust was within the deposition process
Not a problem for functionality?

## Slide 10
Wafer 6 P-side not very much affected
WAFER 6, SENSOR 2 , P-SIDE
Probe mark?
removable

## Slide 11
Wafer 6 P-side again presents non-uniform metal
WAFER 6, SENSOR 3 , P-SIDE
I think, there is no problem

## Slide 12
Color change, i.e. thickness variation, is not a good sign
WAFER 7, SENSOR 1 , N-SIDE
May not be a problem but it is a sign for non uniform processing
 Not good, should be avoided

## Slide 13
Dirty wafer. Handling problem
WAFER 7, ALL SENSORS, P-SIDE
A lot of debris
Scratchlike dirt depositions
CiS or Uni-HH handling?
Perhaps Pac Tech rinsing cleans away most of it, but it should be avoided
P-Side doesn‘t matter as much as N-side

## Slide 14
Wafer 8 is dirty with minor fabrication issues
WAFER 8, ALL SENSORS
N-side
Nothing serious
Usual kind and number of defects
P-side
Nothing serious
Very dirty
Few pixels have defective passivation
Sensor 3

## Slide 15
Interesting scratchy structure can perhaps cleaned away by Pac Tech
WAFER 9, SENSOR 2, N-SIDE
P-side
Nothing serious
Very dirty
Few pixels have defective passivation
Is it deposit or passivation layer related?

## Slide 16
Interesting scratchy structure can perhaps cleaned away by Pac Tech
WAFER 9, SENSOR 2, N-SIDE
Two to six pixel affected
No pad directly affected
If this occurs every 6 wafers (18 sensors) there is no big problem