## Slide 1: Diode Measurements – Macroscopic Effects
Preliminary Results from the Diodes Group
Brown University, CERN, DESY, Hamburg University, Santander (IFCA), KIT, Vilnius
Doris Eckstein
HPK Workshop

## Slide 2: Diodes (Pad sensors) in the HPK Campaign
n bulk
n+ implant
p+ implant
Al contact
Al contact
simple structures
  non-segmented pads on both sides
allow to study material properties:
  volume current
  depletion voltage/ effective doping concentration
  trapping (charge collection)
  temperature dependence
  fluence dependence
  dependence on irradiating particle type

## Slide 3: Irradiations and Measurements
Neutrons: 1 MeV (TRIGA Reaktor Ljubljana) annealing not an issue
Protons: 23 MeV (Karlsruhe cyclotron) irradiation in cooled environment
800 MeV (Los Alamos) air cooling to ~RT
23 GeV (CERN PS) sensors get warm during irradiation
-> fluence dependent annealing
https://twiki.cern.ch/twiki/pub/CMS/SLHCSensorDevelopment/HPK_measurement_specs_V2.7.pdf
Measurements according to:
radius | proton Φeq [cm-2] | neutron Φeq [cm-2] | total Φeq [cm-2] | Active thickn.
40 cm | 3 ∙ 1014 | 4 ∙ 1014 | 7 ∙ 1014 | ≥ 200 μm
20 cm | 1 ∙ 1015 | 5 ∙ 1014 | 1.5 ∙ 1015 | ≥ 200 μm
15 cm | 1.5 ∙ 1015 | 6 ∙ 1014 | 2.1 ∙ 1015 | ≥ 200 μm
10 cm | 3 ∙ 1015 | 7 ∙ 1014 | 3.7 ∙ 1015 | ≤ 200 μm
5 cm | 1.3 ∙ 1016 | 1 ∙ 1015 | 1.4 ∙ 1016 | < 200 μm

## Slide 4: Materials and oxygen content
material | thinning | active thickness | thickness | O[1017]
Float Zone (FZ) | deep diffusion | 320μm 200 μm | 320 μm | 0.8-1 3-4
Float Zone (FTH) | thinned | 200 μm | 200 μm | ?
MCz | --- | 200 μm | 200 μm | 5
p-on-n (n-type):
FZ320N
FZ200N
MCz200N
n-on-p (p-type)
with p-stop(1) with p-spray
FZ320P FZ320Y
FZ200P FZ200Y
MCz200P MCz200Y
(1) no isolation of pad and guard ring
not an issue after irradiation anymore
no difference as concerns the diodes
important to keep in mind:
this FZ material is different
concentrate on 200µm

## Slide 5
Current above full depletion
𝛼𝑀𝑜𝑙𝑙 = 5.3∙10−17𝐴/𝑐𝑚
𝐼/𝑉= 𝛼∙Φ𝑒𝑞
independent of material
and irradiation type
current at Vfd + 20%

## Slide 6
Capacitance measurements
Capacitance measurement:
0OC (at 1kHz ), -20OC (at 1kHz, 455Hz)
extract full depletion voltage Vfd
calculate
fluence dependence of Neff after p irradiation (for n we have only two points)
  fix an annealing step (ideally 8 min @ 80OC corr. to 80 min @ 60OC )
annealing of Neff for a given fluence

## Slide 7
Neff – fluence dependence
23 MeV protons
n-type material
material comparison
 MCz200N and FZ200N behave similar

## Slide 8
Neff – fluence dependence
23 MeV protons
p-type material
material comparison
 p-type rise from start

## Slide 9
Neff – fluence dependence
n-and p-type material
23 MeV protons
material comparison
 p-type depletion voltage higher

## Slide 10
Neff – fluence dependence
n-type material
23 GeV protons
material comparison

## Slide 11
Neff – fluence dependence
23 GeV protons
p-type material
material comparison

## Slide 12
Neff – fluence dependence
23 GeV protons
n-type material
thinned 200 um FZ
material comparison
 FTH200N has smaller depletion Voltage

## Slide 13
Neff – fluence dependence
p-type material
23 GeV protons
thinned 200 um FZ
material comparison

## Slide 14
Neff – fluence dependence
n- and p-type material
23 GeV protons
material comparison
 p- and n-type similar, thinned more flat

## Slide 15: Neff – fluence dependence after 23GeV and 23 MeV protons
n-type material
dependence on particle energy
steeper rise of depletion
voltage after 23MeV protons
which material does invert and
which not?

## Slide 16: Neff – fluence dependence after 23GeV and 23 MeV protons
p-type material
dependence on particle energy
steeper rise of depletion
voltage after 23MeV protons

## Slide 17: Annealing of Neff
Irradiation with protons 23MeV
Fluence: 3e14 neq
all materials are p-type
after this fluence

## Slide 18: Annealing of Neff
Irradiation with neutrons
Fluence: 4e14 neq
all materials are p-type
after this fluence

## Slide 19: MCz200N after 23MeV and 23 GeV Protons
p-type
n-type
annealing behaviour
annealing behaviour:
3.5x1013
5.8x1013
9.5x1013
2.4x1014
1.8x1011
9.6x1012
3.8x1014
With increasing fluence the annealing behaviour:
Changes to p-type after 2.4x1014 23MeV p
Stays n-type up to 3.8x1014 23GeV p

## Slide 20: MCz200N after 23MeV and 23 GeV Protons
high field
 p-type
small field
 n-type
red laser TCT illumination from the front
charge injected close to p+ electrode
electrons drift through bulk to backplane
1 min @ 80OC
1 min @ 80OC
MCz inverts after 23 MeV protons
does not invert after 23 GeV protons

## Slide 21: Charge Collection Efficiency with TCT

## Slide 22
CCE measured with radioactive source (Sr-90) and infrared laser
Advantage source: Absolute energy scale
Advantage laser: much larger signal, less influenced by noise
Result: CCE relative to non-irradiated sensor.
Shape between laser and source agrees very well!
Details on CCE measurement
Charge Collection Efficiency with TCT and Source
 now show laser

## Slide 23
Charge Collection Efficiency – Fluence Dependence

## Slide 24: CCE GeV vs. MeV Protons
-20o C at 1e15
CCE after GeV proton irradiation smaller above depletion than after MeV protons
Could be attributed to trapping
 Have to bring all sensors to same level of annealing

## Slide 25: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 800V bias (above depletion) after 23MeV proton irradiation
* FZ320 looses faster
* n-type and p-type rather similar

## Slide 26: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 800V bias (above depletion) after 23GeV proton irradiation
All fairly similar

## Slide 27: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 800V bias (above depletion) after 23 MeV and 23GeV proton irradiation
Charge collection equivalent for all materials
Thicker sensors loose faster

## Slide 28: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 800V bias (above depletion) after neutron irradiation
n-type and p-type similar

## Slide 29: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 800V bias (above depletion) after neutron and 23 MeV proton irradiation
need more neutron data

## Slide 30: Charge Collection on Strips vs. Diodes
n bulk
n+ implant
p+ implant
Al contact
Al contact
p bulk
p+ implant
n+ implant
Al contact
Al contact
a pad diode has a symmetric structure
strips (weighting field) , electron vs. hole
collection play a role
 Can not base decision about material solely on diodes

## Slide 31: Mixed Irradiations
Pixels
Strips
Lint=3000 fb-1 @14 TeV
Pion/Neutron mixture
Note:
Particle Fluences
are shown!
[ G. Kramberger et al., NIM A609 (2009), 142-148
leakage current increases in accordance with received Φeq
FZ: damage accumulated
MCz-n: damage compensated
 donors introduced in p irradiation compensated by acceptors introduced in n irradiation

## Slide 32: Mixed irradiations: 23 MeV Protons

## Slide 33: Mixed irradiations: 23 MeV Protons + Neutrons
fluences add
no compensation effect
n+p mixed

## Slide 34: Current status

## Slide 35: Conclusions
Huge amount of information already available
MCz200N and FZ200N behave similarly due to the similar level in oxygen concentration.
  This FZ deep deffused is not what we have known as FZ so far.
We need to know more about the oxygen content of the FTH
  ITME SIMS measurements (send diode)
Charge collection with diodes shows similar behaviour of all material types.
Propose to cut down on CCE measurements on pad diodes
  Measure at 80min@60oC only
We need to get all diodes to at least 80min@60oC annealing
Feed-back meeting with Hamamatsu

## Slide 36: Thanks
To all involved in the measurements
To Joachim and Thomas for the plots

## Slide 37: More Material
BACKUP

## Slide 38: Is it the MCz?

## Slide 39: MCz TCT illumination from back

## Slide 40: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 500V bias (above depletion) after 23 MeV and 23GeV proton irradiation

## Slide 41: Charge Collection in Diodes
signal calculated from CCE as CCE * 22000e * d/300µm
at 500V bias (above depletion) after 23 MeV p and n irradiation

## Slide 42: FZ200N compared to MCz200N
remember high oxygen content, similar level
diodes behave quite similar

## Slide 43: FZ200N - Red laser Illuminations
different fluences of 23 MeV protons
as irradiated (no annealing) at 0oC
2.5 e14 for 23 MeV and 23 GeV protons
30 min @ 80oC
different energies for ~same fluence
FZ200 inverts after 23 MeV protons
does not invert after 23 GeV protons