## Slide 1
ATLAS Silicon Strip Tracker Upgrade Activities with Focus on German Groups
Ulrich Parzefall
University of Freiburg
ATLAS Si Strip Tracker Upgrade

## Slide 2: Outline
Overview
Layout
German Participation
Summary & Outlook

## Slide 3: Silicon Tracker Layout
LoI ITK Layout
  All silicon detector (TRT replaced by strips)
Robustness under challenging conditions
  Reduced material budget
  Balance high performance with ease of build
Forward strips
Pixel Disks
Barrel strips
Stub layer
Barrel Pixels
Beam pipe
r
z


Layers | Pixels | Strips
Barrel | 4 2 small, 2 large | 5 2 short, 3 long
End-cap | 2x6 | 2x7
Phase-2, 3000 fb-1

## Slide 4: Barrel Stave Concept
Stave Modules
  Hybrid: ASICS glued to kapton-flex, then wirebonded
  Populated hybrid directly glued to silicon sensor, strips connected via wire bonds
  Prototyping with Hamamatsu 6” sensor and ABCn ASIC (now 250nm, moving to 130nm)
Stave Core
Module
10cm
Stave Support
Structure
~1.2 m
Double-sided Stave
  48 modules glued to core structure
  Carbon fibre laminated to foam filler
  Embedded cooling pipes (CO2)
  Co-cured bus tape for data and power
Attached to global support structure
  Carbon fibre support structure with brackets for attachment
  End insertion for easy assembly and access
Bus cable
Hybrids
Coolant tube structure
Carbon honeycomb
or foam
Carbon fiber
facing
Readout IC’s
1280 strips
Phase-2, 3000 fb-1

## Slide 5: Stave Module Production
Stavelet Program
  Three single-sided 4-module “Stavelets”
  Allow testing of construction and powering options
  Two full-length staves nearing completion, doubled-side stavelets planned
Next steps
  256 channel ASIC in 130nm submitted
  Halve number of chips  lower power
Focus on mass-production
  Testing & population on panel
  Simple vacuum pickup tooling
8 production sites
  ≈70 Modules produced
  ≈10 Modules “made in Germany”
Phase-2, 3000 fb-1

## Slide 6: Stave End-cap = Petal
German groups involved in end-caps
ECs follow stave concept closely (module & hybrid design, assembly)
EC has 6 rings of sensors with radial strips, glued onto bus tape, glued onto carbon core
Phase-2, 3000 fb-1

## Slide 7: Stave End-cap = Petal
7 disks per end-cap
  Many different sensor sizes
  Strip length 8 mm to 58 mm
32 petals per disk
  6 rings of sensors with radial strips
Petalet programme underway
  Double-sided, six-sensor prototype
  Explore many options
  Prototypes sensors & hybrids available
  All module types produced successfully
~60cm
~30cm
Phase-2, 3000 fb-1

## Slide 8: German Participation in Si Strips
Germany responsible for one End-Cap
  224 Petals with 4072 modules
Berlin (Humboldt)
  Module prototyping & production
DESY
  Module prototyping & production (Z)
  R&D, Prototyping & production of Cores (HH)
  Module-to-core mounting
  Macro-Assembly
Freiburg
  Hybrid procurement
  Module prototyping & production
  Module-to-core mounting
And the other Endcap…

## Slide 9: Sensors
Tests on ATLAS12 minis (HPK) confirm radiation hardness to 1015 Neq
Full 6” ATLAS12EC design progressing (mostly by Valencia, production with HPK very likely)
Negotiating 8” p-type run with “a large European vendor”
EC: Current module building with 4” CNM sensors

## Slide 10: Hybrids
4-Layer Kapton-flex PCB
Design principles from barrel
Made at Würth Electronics (D)
Populated either in-house or in industry
ASICs placed in-house
Reasonably smooth production so far
Power
LV
HV
Data Readout
Bias connections (4x per sensor)

## Slide 11: Cores
First petalet cores made and tested successfully
Tested for planarity, thermal performance etc
Stress and pressure tests of Ti-tubes and joints
Titanium Tube bonded into Petalet

## Slide 12: Assembly
Manual assembly with precision tooling
  Tools made in our workshops
  Adjustable to achieve desired dimensions (glue thickness)
More complex and delicate than it might look, yet easier than double-sided ATLAS SCT modules
All petalet module types produced successfully
Next step: module-to-core assembly
Trial upper module for Petalet
Lower module for Petalet

## Slide 13: Module Performance
Assembled modules show good performance
Noise, thermal behaviour
module noise ~560e
long-term stability of noise
bias-dependence of noise
strip number
Noise (e-)

## Slide 14: Summary & Outlook
Phase-2 ATLAS Silicon Strip Tracker design defined in LoI
3 German groups closely cooperating in End Caps
HU Berlin, DESY, Uni Freiburg
  Each group takes over particular responsibilities
Plan to build one End Cap in Germany
ATLAS Si Strip (Endcaps) in general appear short of manpower/groups

## Slide 15: Credits
Based on material from and/or discussions with a large number of colleagues
Tony Affolder, Phil Allport, Dario Ariza, Ingo Bloch, Ingrid Gregor, Marc Hauser, Susanne Kühn, Carlos Lacasta, Riccardo Mori, Richard Nickerson, Volker Prahl, et al

## Slide 16: BACKUP only after this slide

## Slide 17: Design Parameters and Layout
Effect of
stub layer
Total of 14 hits with full coverage to η<2.5
  Pixels to η<2.7 (forward muon ID)
Minimize gaps in coverage
  Last strip disk at z=3m
  Small “stub” layer in barrel
  Last pixel layer at 25-30cm
    Improve double track resolution
Good momentum resolution across whole pseudorapidity range
=1.0
=2.0
=3.0
Phase-2, 3000 fb-1