## Slide 1: DCD Irradiation and temperature tests
Florian Lütticke, Carlos Marinas
University of Bonn
DESY BelleII PXD/SVD meeting, 22.10.2013 , luetticke@physik.uni-bonn.de

## Slide 2: Outline
Measurement Setup
Irradiation Results
Temperature Measurements
luetticke@physik.uni-bonn.de

## Slide 3: DCDB Irradiation setup
Irradiation at KIT with 60keV X-rays
Hybrid 4 .1 without Matrix
Homogeneous irradiation
After each step:
  Annealing, 80°C, 100 min
  Measure transfer curves for different bias voltages and for different DAC settings
  External measurement of DAC current
  Done with 4 ADCs
  Extract INL, Gain, Offset from data
luetticke@physik.uni-bonn.de

## Slide 4: Irradiation INL: Pre Irradiation
luetticke@physik.uni-bonn.de

## Slide 5: Irradiation INL: 5kGy
luetticke@physik.uni-bonn.de

## Slide 6: Irradiation INL: 10kGy

## Slide 7: Irradiation INL: 20kGy

## Slide 8: Irradiation INL: 35kGy
luetticke@physik.uni-bonn.de

## Slide 9: Irradiation INL: 60kGy
luetticke@physik.uni-bonn.de

## Slide 10: Irradiation INL: 100kGy
luetticke@physik.uni-bonn.de

## Slide 11: Irradiation INL: 200kGy
luetticke@physik.uni-bonn.de

## Slide 12: Irradiation Voltage Log
Irradiation
Annealing
80 °C, 100 min
Characterization
5kGy
+5kGy
+15kGy
+25kGy
+100kGy
+40kGy
+10kGy
= 200kGy TID
0
1
2
3
4
Time [days]
VTT
VDD
luetticke@physik.uni-bonn.de

## Slide 13: Irradiation Current Log
Higher current consumption after irradiation in VDDD
Current decrease during operation - additional annealing?
DCD gets quite warm in the measurement setup
After irradiation VDDD changes if bias voltages change – not observed before irradiation
0
1
2
3
4
Time [days]
VTT
VDD
luetticke@physik.uni-bonn.de

## Slide 14: Temperature INL: -30°C
luetticke@physik.uni-bonn.de

## Slide 15: Temperature INL: -20°C
luetticke@physik.uni-bonn.de

## Slide 16: Temperature INL: -10°C
luetticke@physik.uni-bonn.de

## Slide 17: Temperature INL: 0°C
Bad timing setting in FPGA – Bit was stuck
luetticke@physik.uni-bonn.de

## Slide 18: Temperature INL: 10°C
luetticke@physik.uni-bonn.de

## Slide 19: Temperature INL: 20°C
luetticke@physik.uni-bonn.de

## Slide 20: Temperature INL: 30°C
luetticke@physik.uni-bonn.de

## Slide 21: Temperature Scan Voltage Log
8
10
12
16
18
Time [days]
14
VTT
VDD
luetticke@physik.uni-bonn.de

## Slide 22: Temperature Scan Current Log
+10°C
0°C
-10°C
run crashed
-10°C
-20°C
-30°C
+20°C
+30°C
One power supply
lost connection
Power supply
software
maintenance
climate chamber needed by different project
8
10
12
16
18
Time [days]
14
VTT
VDD
luetticke@physik.uni-bonn.de

## Slide 23: Current consumption changes with temperature
-10°C
-20°C
-30°C
250mA
300mA
VTT
VDD
luetticke@physik.uni-bonn.de

## Slide 24: Difference of Irradiation
Pre irradiation
Post irradiation @ 10°C
luetticke@physik.uni-bonn.de

## Slide 25: Irradiation Results
After 20kGy DCD starts to show strange behavior.
  Unable to switch off analogue part
  High VDDD current consumption
  VDDD current depends on Bias voltages.
  Gets worse at 35kGy then starts to improve again
  At 100kGy analogue part could partly switched off (half current consumption)
  Power consumption decreases over time – additional annealing?
After the weekend behavior changed
  DCD was stored under room temperature during the weekend
  On Monday, DCD was installed in climber chamber, switched on and run for a few hours
  Measurements show performance similar to the initial performance
    Irradiated DCD seems to have a wider area of acceptable bias voltages
    DCD shows higher gain / less dynamic range .
DCD irradiated with 60keV X-rays up to TID of 200kGy could be operated in a temperature range between +30 to -30°C
To be confirmed with new DCDB versions

## Slide 26: Thank you very much!