## Slide 1: Depleted Monolithic ACTIVE PIXELS FOR future HEP experiments
Y. Fu, M. Havranek, T. Hemperek, T. Kisisita, H. Kruger, T. Oberman
5th March 2014
7th Detector Workshop of the Helmholtz Alliance "Physics at the Terascale"

## Slide 2
Hybrid Pixel Detectors
fine pitch flip-chip assembly of:
  CMOS R/O chips (CSA + DSP per pixel)
  Si (planar or 3D) or Diamond detectors
+ high density electronics
+ moderate - good SNR
- high material budget
- high cost (chip + sensor + hybridization)
Properties
Monolithic Pixels
+ cheap
+ low material
+ good resolution
not very radiation hard
small signal (little depletion)
usually no CMOS in active area
Promises
Properties

## Slide 3
Hybrid Pixel Detectors
fine pitch flip-chip assembly of:
  CMOS R/O chips (CSA + DSP per pixel)
  Si (planar or 3D) or Diamond detectors
+ high density electronics
+ moderate - good SNR
- high material budget
- high cost (chip + sensor + hybridization)
Depleted MAPS
large depletion depth d ~(ρV)1/2
AND rad. hardness > 1014-15 /cm2
AND full CMOS
AND low power
AND low cost
for HL-LHC need
Properties

## Slide 4
High Luminosity LHC - Cost
„Combining the two 3Ds” R. Lipton et al 2012 JINST 7 C12010
ATLAS
90 EUR/cm2
70* EUR/cm2
Monolithic Sensors < 10 EUR/cm2
* - including thinning -> HL-LHC ~25 EUR/cm2

## Slide 5
High Luminosity LHC Environment - Requirements
ATLAS Phase II Letter of Intent
outer
Inner
Occupancy [%]
Inner layer
Outer layer
Low power
Low material
Occupancy
Resolution
Low cost
Low power
Low material
Resolution
hybrid pixels (65nm)
low cost hybrid pixels or monolithic

## Slide 6
Charge Collection in Depletion Layer
Depletion width d
  QMIP
  Cparallel plate
  High voltage on the r/o node  HV CMOS process
  High resistive substrate material  CMOS on high resistive substrate (“HR CMOS”)
  Something in-between
Chart: Depletion Width in Silicon
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150 | 155 | 160 | 165 | 170 | 175 | 180 | 185 | 190 | 195 | 200
1 | 0 | 0.30411 | 0.43008 | 0.52673 | 0.60822 | 0.68001 | 0.74491 | 0.8046 | 0.86015 | 0.91233 | 0.96168 | 1.1778 | 1.36 | 1.5205 | 1.6657 | 1.7991 | 1.9234 | 2.04 | 2.1504 | 2.2553 | 2.3556 | 2.4518 | 2.5444 | 2.6337 | 2.72 | 2.8037 | 2.885 | 2.9641 | 3.0411 | 3.1162 | 3.1895 | 3.2612 | 3.3314 | 3.4 | 3.4674 | 3.5334 | 3.5983 | 3.662 | 3.7246 | 3.7861 | 3.8467 | 3.9064 | 3.9651 | 4.023 | 4.0801 | 4.1363 | 4.1919 | 4.2467 | 4.3008
20 | 0 | 1.36 | 1.9234 | 2.3556 | 2.72 | 3.0411 | 3.3314 | 3.5983 | 3.8467 | 4.0801 | 4.3008 | 5.2673 | 6.0822 | 6.8001 | 7.4491 | 8.046 | 8.6015 | 9.1233 | 9.6168 | 10.0862 | 10.5347 | 10.9648 | 11.3787 | 11.7781 | 12.1644 | 12.5387 | 12.9023 | 13.2558 | 13.6002 | 13.936 | 14.264 | 14.5846 | 14.8983 | 15.2055 | 15.5066 | 15.802 | 16.092 | 16.3768 | 16.6568 | 16.9321 | 17.203 | 17.4698 | 17.7325 | 17.9914 | 18.2466 | 18.4982 | 18.7466 | 18.9916 | 19.2336
100 | 0 | 3.0411 | 4.3008 | 5.2673 | 6.0822 | 6.8001 | 7.4491 | 8.046 | 8.6015 | 9.1233 | 9.6168 | 11.7781 | 13.6002 | 15.2055 | 16.6568 | 17.9914 | 19.2336 | 20.4003 | 21.5038 | 22.5534 | 23.5562 | 24.5181 | 25.4436 | 26.3366 | 27.2004 | 28.0375 | 28.8503 | 29.6409 | 30.4109 | 31.1619 | 31.8953 | 32.6121 | 33.3135 | 34.0005 | 34.6738 | 35.3343 | 35.9827 | 36.6196 | 37.2456 | 37.8613 | 38.4671 | 39.0636 | 39.651 | 40.2299 | 40.8006 | 41.3633 | 41.9186 | 42.4666 | 43.0076
1000 | 0 | 9.6168 | 13.6002 | 16.6568 | 19.2336 | 21.5038 | 23.5562 | 25.4436 | 27.2004 | 28.8503 | 30.4109 | 37.2456 | 43.0076 | 48.0839 | 52.6733 | 56.8937 | 60.8219 | 64.5113 | 68.0009 | 71.32 | 74.4913 | 77.533 | 80.4598 | 83.2838 | 86.0151 | 88.6624 | 91.2328 | 93.7328 | 96.1678 | 98.5427 | 100.8617 | 103.1285 | 105.3466 | 107.5189 | 109.6482 | 111.7369 | 113.7873 | 115.8014 | 117.781 | 119.728 | 121.6437 | 123.5298 | 125.3875 | 127.2181 | 129.0227 | 130.8024 | 132.5582 | 134.2911 | 136.0018
2000 | 0 | 13.6002 | 19.2336 | 23.5562 | 27.2004 | 30.4109 | 33.3135 | 35.9827 | 38.4671 | 40.8006 | 43.0076 | 52.6733 | 60.8219 | 68.0009 | 74.4913 | 80.4598 | 86.0151 | 91.2328 | 96.1678 | 100.8617 | 105.3466 | 109.6482 | 113.7873 | 117.781 | 121.6437 | 125.3875 | 129.0227 | 132.5582 | 136.0018 | 139.3604 | 142.6399 | 145.8457 | 148.9825 | 152.0547 | 155.066 | 158.0199 | 160.9195 | 163.7679 | 166.5676 | 169.3209 | 172.0302 | 174.6975 | 177.3247 | 179.9135 | 182.4656 | 184.9825 | 187.4656 | 189.9162 | 192.3356
5000 | 0 | 21.5038 | 30.4109 | 37.2456 | 43.0076 | 48.0839 | 52.6733 | 56.8937 | 60.8219 | 64.5113 | 68.0009 | 83.2838 | 96.1678 | 107.5189 | 117.781 | 127.2181 | 136.0018 | 144.2517 | 152.0547 | 159.4763 | 166.5676 | 173.369 | 179.9135 | 186.2282 | 192.3356 | 198.255 | 204.0028 | 209.5929 | 215.0378 | 220.3482 | 225.5335 | 230.6023 | 235.5621 | 240.4196 | 245.1808 | 249.8513 | 254.4361 | 258.9398 | 263.3664 | 267.7199 | 272.0037 | 276.221 | 280.375 | 284.4683 | 288.5035 | 292.483 | 296.4091 | 300.2839 | 304.1094

## Slide 7
Options for n-on-p Read-out
p-substrate
Deep n-well
P+
p-well
Charge signal
Electronics (NMOS only)
P+
p-substrate
n+
p-well
Charge signal
Electronics (NMOS only)
n+
CCPD (HVCMOS)
DMAPS-A
“MAPS” like
CMOS with additional implants
CMOS with twin or triple wells
p-substrate
Deep n-well
P+
p-well
Charge signal
Electronics (full CMOS)
P+
nw
p-substrate
n+
p-well
Charge signal
Electronics (full CMOS)
n+
nw
deep p-well
Electronics inside charge collection well
Collection node with large fill factor  rad. hard
Large sensor capacitance (DNW/PW junction!)  x-talk, noise & speed (power) penalties
Full CMOS with isolation between NW and DNW
Electronics outside charge collection well
Very small sensor capacitance  low power
Potentially less rad. hard (longer drift lengths)
Full CMOS with additional deep-p implant

## Slide 8
Possible scenarios for Active Sensors
Hybrid Pixels with “smart” diodes:
  HR- or HV-CMOS as a sensor (8”)
  Standard FE chip
  CCPD (HVCMOS) on FE-I4
CMOS Active Sensor + Digital R/O chip
  HR- or HV-CMOS sensor + CSA (+Discriminator)
  Dedicated “digital only” FE chip
Monolithic Active Pixel Sensor
  MAPS usually on epi substrate  diffusion signal, not suited for HL-LHC
  HR- material (charge collection by drift)  Fully depleted MAPS (DMAPS)
Diode + full analog processing
Digital only FE chip
Wafer to wafer bonding
Diode + preamp
FE chip
Diode + Amp + Digital

## Slide 9
Active Pixel Sensors on HV-CMOS process
Parameters
Depletion (small)
Low leakage
Possible high resolution
Limited use of PMOS
I. Peric

## Slide 10
CCPD + FE-I4 (HV2FEI4)
An active sensor!

## Slide 11
Monolithic technology requirements for LHC
High-resistive substrate (>1kOhm-cm)
Isolated PMOS and NMOS transistors (deep n-well/p-well)
Good breakdown performance
Thinning
Backside implantation and implant activation
Backside metallization (if needed)

## Slide 12
Simple device cross-section
High signal (full depletion possible)
Fast (collection by drift)
Small pixels
Only NMOS in active area
Input capacitnce dominated by deep-nwell tp pwell capacitance
Pros
Cons

## Slide 13
Electrostatic Potential (HV)

## Slide 14
Depletion Evolution with Voltage
Hole Density @ Oxide Charge 1e+12 cm-2 + Fluence 1e+15 Neq/cm2
Hole Density @ no radiation

## Slide 15
Charge Collections
Electron Density @ 200V (no radiation)
Current on collecting electrode @200V

## Slide 16
Charge Collections Efficiency
Fluence (Neq/cm2) | Back Voltage [V] | CCE [%]
0 | 100/200 | 100
1e14 | 100 | 96
1e14 | 200 | 97
1e15 | 100 | 75
1e15 | 200 | 80

## Slide 17
ESPROS Photonic CMOS™ Process
There is more to this in this technology 

## Slide 18
EPCB01 - overview
DMAPS pixels
Deep N-well pixels
Chip size: 1.4×1.4 mm2
First 50um, back side processed, full CMOS, “fully depleted”
(>2kOhm-cm substrate).
Design&Testing:
Y. Fu,
M. Havranek,
T. Hemperek,
T. Kisisita,
H. Kruger,
T. Oberman

## Slide 19
EPCB01 - Functional Blocks
Deep N-well pixels
  3T readout
  Analog Output
DMAPS pixels
  Pixel Charge Sensitive Amplifier (CSA)
    continuous discharge
    reset
  Pixel Comparator
    asynchronous
    dynamic
  Tuning DAC
  Digital Sift Register Readout
Custom Pads
Transistors

## Slide 20
EPCB01 - Test system
MIO
GPAC
DUT
EPCB01
FPGA Multi-IO (MIO) board
General Purpose Analog Card
- universality → can be used for other DUTs
- provides bias voltages and currents for DUT
- provides power supply for the DUT
- distributes digital signals from MIO to DUT
Board carrying DUT
EPCB01

## Slide 21
EPCB01 - Pixel Array Readout
CSA- switched reset
dynamic comparator
CSA – continuous discharge asynchronous comparator

## Slide 22
EPCB01 - Pixel Array
Pixel size: 40×40 µm2
Sensing area: 20×20 µm2
PIXEL
SENSOR
RESISTOR
CSA
Q-INJ.
HIT OR
TDAC
COMP
CDS

## Slide 23
EPCB01 - Pixel Array Bias Configurations
AC coupled
resistor bias
AC coupled
self bias
DC coupled

## Slide 24
EPCB01

## Slide 25
EPCB01 – more measurements

## Slide 26
Pegasus
Parameters:
  180nm CMOS (TowerJazz)
  Different wafer materials
    18µm HR epi
    40µm HR epi
    HR bulk
  50 x 50 µm2 and 25 x 25µm2 pixels
thanks to W. Dulinski, M. Kachel (IPHC)

## Slide 27
Pegasus - Electrostatic Potential (TCAD example)

## Slide 28
PEGASUS - First signs of life
Fe55 Spectra for 18µm epi
Sr90 and Fe55 Spectra for 18µm epi
M. Kachel (IPHC)

## Slide 29
FD-SOI
Parameters
Almost perfect technology but due to back gate effect not radiation hard.

## Slide 30
HV-SOI
Layout
First signs of life
Concept
Design&Testing:
T. Hemperek,
T. Kisisita,
H. Krueger

## Slide 31
Low cost hybrid
Low cost sensor on 8” process with under bump metallization
Front-end chip with bumps (150um pitch)
Low cost flip chip process
Cost: < 30$ cm2
8” FE-I4 type sensor is planed

## Slide 32
More to come
150nm – submitted Q4 2012
  full CMOS
  n-type > 2kOhm-cm substrate
  thinned
  back implanted
180nm – submitted Q1 2013
  full CMOS
  p-type > 1kOhm-cm substrate
  full wafers -> thinning/back implanting possible
180nm - submitted Q1 2013
  full CMOS
  p-type - initially 100 Ohm-cm
  very HV isolation guaranteed
130nm – submission Q4 2013
  HV-CMOS(CCPD)/full CMOS
  p-type >3kOhm-cm
  full wafers -> thinning/back implanting possible
150nm - submission Q1 2014
  HV-CMOS(CCPD)/full CMOS/ possibly T3
  p-type >2kOhm-cm (~4-5k Ohm-cm)
  thinned
  back implanted
  full wafers

## Slide 33
Conclusions
Depleted Monolitic Detectors:
- more radiation tolerance
- will take space of hybrids/strips for less dymandingapplication
- as a accitve sensor layer for ultra fast enviroments
First promising results from various technologies
More technologies to be studied and improved.
Question, comments, suggestions:
hemperek@uni-bonn.de