## Slide 1
Comparison of the charge collection measurements for sensors from ATLAS and CMS campaigns
Alexander Dierlamm

## Slide 2: Samples
ATLAS
  n-in-p FZ strip sensors from HPK
    pitch: 74.5µm
    strip length: 8mm
    # of strips: 104
    sensor size: 1cm x 1cm
    thickness: 320µm
    Vfd: 175V
    [O]: “standard FZ” …
CMS
  n-in-p FZ strip sensors from HPK
    pitch: 80µm
    strip length: 33mm
    # of strips: 256
    sensor size: 3.5cm x 2.25cm
    thickness: 320µm
    Vfd: 250V
    [O]: ~8-9e16cm-3
ATLAS data from
S. Kuehn, et al., Signal and charge collection efficiency of n-in-p strip detectors after mixed irradiation to HL-LHC fluences, NIM A 730 (2013) 58–61.
80µm
24µm
6µm

## Slide 3: Irradiations
ATLAS
CMS
280MeV pions
23MeV protons (within HHA)
Reactor neutrons
Radius / cm | p fluence / 1015neq/cm² | n fluence / 1015neq/cm² | Sum / 1015neq/cm²
60 | 0.3 | 0.4 | 0.7
20 | 1.0 | 0.5 | 1.5
15 | 1.5 | 0.6 | 2.1
Annealing during pion irradiation ~3weeks@RT
23MeV protons
Reactor neutrons

## Slide 4: Charged hadrons – I
Lowest fluence: ~1e15neq/cm²
p-stop (P) and p-spray (Y) versions quite similar
Quite large difference for low voltages
Probably similar max. signal
BUT: annealing time much different!
  ATLAS: 3 weeks @ RT
  CMS: 10min @ 60°C (~50heq@RT)

## Slide 5: Charged hadrons – II
Annealing study available by CMS for 1.5e15neq/cm² mixed irradiation
Looks like ~500heq is the optimal annealing time generating max. signal at lower voltages
ATLAS and CMS measurements agree for same annealing!
Still, irradiations not same: ATLAS: MeV p + pions CMS: MeV p + neutrons
Equivalent annealing at RT in h

## Slide 6: Mixed
Fluence: 2.1e15neq/cm²
Good agreement for similar annealing time
Remember:
  ATLAS used mainly pions as charged hadrons
   minor influence on CC

## Slide 7: Annealing
Similar trend to drop after long annealing
Drop appears at different times for diff. fluence !?
CM not seen by CMS (too short annealing?)
@60°C
pre-annealing of 3weeks@RT ~ 120min@60°C
ATLAS annealing presented by Susanne on 21st RD50 Workshop Nov. 2012:
https://indico.cern.ch/event/200290/session/3/contribution/36/material/slides/0.pdf
720min
140min
430min
270min
Annealing @60°C
F=2.1e15neq/cm²
F=1.5e15neq/cm²

## Slide 8: Equivalent annealing – comments
Annealing can be different for
  different parameters (Ileak, Vfd, CC)
  different materials (FZ, MCz, …)
Unique scaling not possible
  Convention: scale with leakage current
    Reference: PhD of Michael Moll
    Tool:
  Consequence:
    Temperature scaling of CC and Vfd annealing can be different due to different defects involved
    Need to check CC annealing close to RT!
    http://ikcms02.fzk.de/irradiation/annealing/EqAnnealingTimeAtRT.php
G. Casse,18th RD50 Workshop, Liverpool 23-25 July 2011

## Slide 9: Annealing of different materials
p-in-n type material shows early drop
300µm material shows pronounced maximum at fixed bias voltage (600V)
MCz materials shows almost no effect of CC annealing
CC for GeV () or MeV (▼) proton irradiation similar, but Neff not!  Need to study final material!

## Slide 10: Comparison to CNM sensors
CNM samples
  pitch: 90µm
  strip length: 10.5mm
  # of strips: 64
  sensor size: 2.57cm x 0.85cm
  thickness: 270µm
  Vfd: 60V
  [O]: ???
FZ from CNM without deep-diffusion; expected to have lower [O]
Signal similar to CMS HPK results

## Slide 11: protons vs. neutrons
Initially neutron irradiated sensors show less charge than MeV proton irradiated sensors
NIEL violation for FZ with [O]~9e16cm-3 ?

## Slide 12: Conclusion
Overall quite similar results
Need to be careful with accelerated annealing
Different radiation particle types create different Neff
  can also alter CC, but does not have to
  depends on [O]
  leakage current still scales well with NIEL
Investigate carefully the final material to be built into the detector!
Silicon ≠ Silicon

## Slide 13: BACKUP

## Slide 14: CMS HPK [O]

## Slide 15: CNM Sensors Layout