## Slide 1: Reducing power dissipation in sc cavities by thermal cycling
ARD-ST1 Superconducting RF Science and Technology
Julia Vogt (HZB)
Motivation
Superconducting RF technology enables a variety of future projects due to its low power dissipation.
Even the few watts dissipated in SRF cavities have to be cooled away. Cryoplants for SRF accelerator projects are large, complex and costly.
Reduction of cavity surface resistance is one central point in todays research.
We observed in horizontal tests that the residual resistance and hence the dissipated power can be reduced by up to a factor of 2.5 simply by changing the cooling conditions during the superconducting phase transition. If this effect can be repeated in cw LINACs (e.g. LCLSII or if XFEL operates cw) the impact on investment and operation costs is enormous.
Cx3
Cx1
Cx2
ΔT = 155 K
Time [h]
Cavity temperature [K]
Ambient magnetic flux present during cooldown causes additional power dissipation. Hence the earth magnetic field is shielded. We believe that the temperature difference along the cavity-tank-system induces additional magnetic flux inside the shielding by thermoelectric effect which gets trapped during the phase transition.
Coworkers and Acknowledgment
[1] S. Aull, O. Kugeler and J. Knobloch, Phys. Rev. ST Accel. Beams 15, 2012
[2] J. Vogt, O. Kugeler and J. Knobloch, Phys. Rev. ST Accel. Beams 16, 2013
These studies have been performed and supported by O. Kugeler and J. Knobloch. We thank our engineers André Frahm, Axel Hellwig, Sascha Klauke, Dirk Pflückhahn, Stefan Rotterdam and Michael Schuster for patient support.
Literature
We demonstrated an improvement of Rres of an SRF cavity by up to a factor of 2.5 by thermal cycling. We believe a temperature gradient along a cavity leads to thermally induced magnetic field that gets trapped in the sc material. Thermal cycling diminishes the effects by reducing the ΔT prior to the phase transition. We were able to gather further evidence for this effect in a model system. A decreased Rres reduces cryo costs significantly and hence the proposed cycling procedure may enable new accelerator concepts and applications. Even existing SRF accelerators could implement a similar procedure to minimize the amount of trapped flux and hence the cryo load.
... with a model system
Heater
Heater
4.2 K
Cernox sensors
Niobium rod
Titanium short
Fluxgate magnetometer
We designed a model system to simulate the thermoelectric properties of the cavity-tank-/ niobium-titanium-system consisting of a niobium rod with a titanium short.
The impact of a temperature gradient during sc phase transition is evident in the model system as well as in the cavity-tank-system.
Helium outlet
Helium inlet
Cernox 1
Cernox 2
Cernox 3
Helium tank
(titanium)
TESLA cavity
(niobium)
Temp. difference at phase transition [K]
Magnetic field trapped in the sc material (in equil.) after phase transition [µT]
Level of ambient field
T1
T2
Termoelectric current
IΔT = ΔU/R = ΔT ∙ ΔS/R
Hypothesis
Checking the hypothesis ...
... with a cavity
Conclusion and Application
Decrease in
trapped flux
Cx3
Cx1
Cx2
ΔT = 155 K
Cavity temperature [K]
Time [h]
Cavity temperature [K]
Time [min]
ΔT = 4 K
Cavity temperature [K]
Time [min]
ΔT = 91 K
Cycle 3:
Breeding the effect
Initial cooldown
Cycle 2:
Suppressing the effect
Surface resistance (= losses)
as a function of the inverse operating temperature for different temperature differences during cooldown:
Residual resistance (= losses we can influence) due to, presumably, trapped magnetic flux as a function of temperature difference during cooldown:
Residual resistance [nΩ]
Temp. difference at phase transition [K]
Surface resistance [nΩ]
Inverse operating temperature [1/K]
ΔT = 155 K
ΔT = 91 K
ΔT = 67 K
ΔT = 47 K
ΔT = 4 K
1.8K
Helium out
Helium in
Cx1
Cx2
Cx3
Decrease in
trapped flux
Helium out
Helium in
Helium out
Helium in
Heater
Heater
Heater