## Slide 1: Ultra-fast YBCO THz detectors
DTS - Monitoring of the electrical field of Coherent Synchrotron Radiation
Juliane Raasch (KIT)
Detector technology
Pulsed Laser Deposition
Length of detecting element (EBL, IBE & wet etching)
Antenna & coplanar design (EBL & IBE)
EBL – Electron Beam Lithography
IBE – Ion Beam Etching
Principle of detector operation
Absorbed photon induces rf current
Generation of magnetic flux quanta (vortices)
Lorentz force
 Displacement of vortex lattice
Measurable voltage transient
 Picosecond response time
 Zero-bias current operation
 Electrical field sensitivity
Fast and sensitive direct THz detectors for CSR
Study of Coherent Synchrotron Radiation (CSR) requires ultra-fast THz direct detection system
High-temperature superconductor YBa2Cu3O7-x (YBCO):
Intrinsic response time < 2ps
Broad dynamic range > 30 dB
Broad band THz antenna: 30 GHz – 2.5 THz
Ultra-fast THz detection: Experimental setup
Detector operation: Experimental results
Filling pattern in low-alpha operation at ANKA
Monitoring of the pulse shape of single CSR THz pulses
Zero bias operation: detection of the electrical field
Simulation
E. Roussel, PhLAM,
Université de Lille
Experiment