## Slide 1: Pixelized gaseous detectors
Helmholtz Alliance “Physics at the Terascale”
4th Detector Workshop DESY 18.3.2011
Klaus Desch University of Bonn

## Slide 2: Motivation
Micro-structuring of semiconductor detectors led to breakthrough in
charged particle tracking  silicon strip + pixel detector
Q: Can gaseous detectors also benefit from extremely fine-grained readout?
A1: (for thin planar detectors)
diffusion of drifting electrons limits spatial resolution
 typical diffusion coefficient D ~ o(100) μm/√cm
 o(30) μm for single electron after 1 mm drift
+ average over o(10) electrons for a single tracklet
 o(10) μm single point for a thin planar detector („GOSSIP“)

## Slide 3: Motivation
Q: Can gaseous detectors also benefit from extremely fine-grained readout?
A2: (for long drift distances, e.g. TPC)
 to first order no advantage over pad-based r/o for p-resolution but
- identify (and remove) short δ-tracks for track reconstruction
- clearly superior for double track resolution (dense jets...)
- lower occupancy  BG tolerance
- dE/dx by cluster counting
- (potentially simpler readout)
A3: (for x-ray photon identification, BG suppression, rare event searches)
 clear distinction of photons / m.i.p.s / alphas / ...
 reconstruction of photoelectron „tracks“

## Slide 4: Detector Technologies
Clearly, micro-structured readout needs micro-structured gas-amplification
MPGDs (GEMs, Micromegas)
Pioneering example: Bellazini et al (X-ray polarimeter using 1 „special“ GEM + dedicated CMOS pixel chip)

## Slide 5: Detector Technologies
First „large area“ ( 2.8 x 5.6 cm2, 500k „channels“) tracking devices (EUDET):
3-GEM
8 Timepix
InGrid
8 Timepix
NIKHEF Saclay Twente
Bonn Freiburg

## Slide 6: Detector Technologies
3-GEM
8 (2x4) Timepix
InGrid
8 Timepix „Octopuce“
underneath
a 3-GEM
stack
Bonn Freiburg
NIKHEF Saclay Twente

## Slide 7: Detector Technologies
Both GEMs and InGrids work nicely
Major GEM advantage: amplification field(s) seperated from CMOS electronics
Major GEM disadvantage: diffusion in GEM stack spreads charge over o (100) pixels  need (very) high gain
Look at InGrids
= a micromegas grid produced through postprocessing on a CMOS substrate (so far, the Timepix chip)
pioneered by
NIKHEF + Twente U. (Mesa+)

## Slide 8: How is it done?
1. Preliminary analysis and cleaning of chip surface
7. Development of SU-8
Chip
2. Deposition of protection layer
3. Deposition (spin coating) of SU-8 (50 μm polymer photoresist)
4. Exposition and baking of SU-8
5. Deposition of thin Al film (critical)
6. Patterning of Al to form the Grid

## Slide 9: Single chips / 3x3 chip squares at Twente
facilities at Twente U can (at most) handle 4 inch wafers
practically at most 3x3 chips can be handled at once
several days of processing (+ working) time for one run
Try to find a place which can manufacture Ingrids on a 8 inch wafer scale
Best candidate currently: (Berlin)

## Slide 10: 1st attempt at IZM: „GEMGrids“
Technically simpler – BCB can be etched Avoid cross-linking of photo-resist during Al sputtering

## Slide 11: 1st attempt at IZM: „GEMGrids“

## Slide 12: „GEMGrids“ – work (in principle)
first signals
seen in Bonn setup
with 55-Fe source
challenges / problems
limited yield (~ 1 / 6 structures working so far...)
sparking at the edges
limited HV  limited efficiency to be understood
T. Krautscheid, Bonn

## Slide 13: 2nd road at IZM: Ingrids
transfer original „Twente“ process to 8´´
very successful 1st attempt
on dummy wafers
development after dicing
extremely regular...
IZM+Y.Bilevych,Bonn

## Slide 14: Steps to go
mask design for Timepix wafer (done)
spark protection layer (proven materials aSi, SixNy) not available at IZM
patterning of protection layer (shadow mask)
 hope for 1st Timepix wafer processed in next few months

## Slide 15: Protection of CMOS chip
potential showstopper: sparks, large signals, HV breakdowns can kill
input stage of CSA of CMOS pixel chip  protection
on chip?
on detector: SiProt
Amorphous Si or SixNy
7 μm protection layer
- finite (but large) resistivity (1011-1014 Ωcm)
reduce local E-field
charge-up at high rate  reduction of signal
vital for stable operation (unprotected Ingrids typically die after few h from α-induced discharges)

## Slide 16: Radiation damage and ageing?
„Sensor“: No radiation damage of (gas can be replaced)
CMOS: same as for Si pixels (go to small feature sizes)
Ageing of amplification strucuture?
In general, planar structures more robust than wires (no 1/r dependence of E-field)
Preliminary tests done at NIKHEF:
Irradiation with 8 keV X-rays: No rate effects up to anode current density of 0.2 μA / mm2  very fast track counting possible!
After 0.3 Coulomb/mm2:
 (eq. 3.7 x 1016 MIPs/cm2)
deposit of carbon polymer on anode is clearly visible. Micromegas is clean (?!)
Little deposit on cathode, and……
Chamber still worked!
H. van der Graaf, NIKHEF

## Slide 17: Readout chips
Timepix as main work horse so far
Limitations
designed for imaging
no sparse readout (want on-chip 0 suppression)
can measure only time or charge (TOT) for a given pixel (want both)
time (=z position) accuracy limited by clock frequency (~50 MHz)
Timepix-2 (IBM 130nm) under design by Medipix-3 collaboration (designed by CERN,NIKHEF,Bonn)
- completely data driven readout (compatible with both LHC and LC conditions)
- on pixel fast (640 MHz) oscillator (only active if hit)
- Si through via capability for backside connection (no wire bonds inside gas volume)
(some compromises to also serve e.g. LHC-b Velopix needs, e.g. leakage current comp.)

## Slide 18: GOSSIPO-3 test chip
small test chip (NIKHEF,BN) to test basic features of single pixel cell
1mm
2mm
Fast oscillator works as expected
 1.6 ns time resolution

## Slide 19: Ideas for ATLAS: GridPix Tracker

## Slide 20
Ideas for ATLAS: GridPix Tracker

## Slide 21: Ideas for ATLAS: GOSSIP Vertexdetector
CMOS pixel array
MIP
InGrid
Drift gap: 1 mm
Max drift time: 16 ns
MIP
CMOS pixel chip
Cathode foil
Gas On Slimmed Si-Pixels
van der Graaf

## Slide 22: First „Twente“ InGrids at work in Bonn
single InGrid in TPC protoptye
cosmic track
in He/CO2 70/30
(not yet fully efficient)
very preliminary

## Slide 23: First „Twente“ Ingrids at work in Bonn
X-Ray detector for rare event searches (CAST)
Photoelectron-“Track“
Background
image of 55Fe source
single InGrid
2 cm drift gap
Gas: He-Isob 95/5
later: Xe

## Slide 24: Summary and Outlook
Pixelized gaseous detector are still in their infancy
Fascinating potential
- TPCs
- planar vertex / tracking detectors
- TR (identification of single TR photons along with the track)
- X ray polarimetry / WIMP searches / UV photon detection ...
Proofs of principle done
Lots of work ahead – expect full InGrid+Timepix wafer soon, Timepix2 submission by e.o.y.
Synergy with aspects of Si-pixels (thinning, STV, common ASICs, ...)
Lot of fun ahead... interested to join?